## Slide 1: Understanding the crystal shape in the growth of nanostructures
Rajrupa Paul, Jehyeok Ryu, Hoda Shirzad & Elias Stutz
Seminar presentation for MSE-649 Crystal growth by epitaxy
August 28th, 2020

## Slide 2: Motivation : Why understanding the crystal faceting is crucial?
shapes control can improve optical, electrical, and catalytic properties in case of metallic nanoparticles
the control of morphology and crystalline quality allows for the optimization of devices for a large variety of semiconductor structures
crystal faceting and morphology-dependent properties are also interesting for organic compounds used in molecular recognition and in medical applications

## Slide 3: Facet-dependent Properties

## Slide 4: Facet dependent properties
Interactions of charged molecules with metal oxide crystals exposing different surface facets.
Photographs of methylene blue solutions taken after dispersing Ag2O (a) octapods, (b) cubes, (c) octahedra, and (d) hexapods with stirring for 60 min. (e) Photograph of a methylene blue solution mixed with rhombic dodecahedral Cu2O nanocrystals and stirred for 30 min. SEM images of the respective particles are shown below the photographs. Scale bars are all equal to 100 nm. Remarkably, Ag2O octahedra and hexapods and Cu2O rhombic dodecahedra have floated to the top of the solution due to repulsive electrostatic interactions between the positively charged methylene blue molecules and the positively charged {111} and {110} faces of Ag2O and Cu2O crystals.

## Slide 5: Facet dependent properties
Face-selective etching and deposition processes on the surfaces of nanocrystals
a) SEM image showing the formation of two types of Cu2O nanoframes with empty {100} faces (type I) and {110} faces (type II) and nanocages resulting from crystal growth and face-selective etching processes. (b) SEM image of hollow Cu2O cubes with empty {110} edges. (c) SEM image of edge-truncated octahedral Ag2O crystals after the controlled etching by NH3 to yield etched {100} corners and {110} edges. The inset shows rhombicu-boctahedral Ag2O crystals with etched square {100} faces. (d) SEM image of rhombicuboctahedral Cu2O microcrystals with Cu nanoparticles selectively deposited on the {111} faces.

## Slide 6: Facet dependent properties
Facet-dependent electrical conductivity of Cu2O nanocrystals
. Am. Chem. Soc. 2011, 133, 4, 1052–1057

## Slide 7: ECS: equilibrium crystal shape
Wulff’s Theorem : for a crystal at equilibrium, there exists a point in the interior such that its perpendicular distance hi from the ith face is proportional to γi: (γ1/h1) = (γ2/h2) = ...
Total surface energy
Minimizing the energy:

## Slide 8: ECS: equilibrium crystal shape
Wulff and Winterbottom Construction
minimizing the total surface energy when the crystals place on solid substrates.

## Slide 9: Modelling crystal shapes

## Slide 10: Description of the model
Describe all equations, variables and parameters with respect to the ϕ field.
Solve evolution with a finite element method.
is neglected
Cryst. Growth Des., 2787 (2015)
Notes: The diffusion of adatoms follows the gradient of chemical potential along the surface

## Slide 11: Showcasing the Phase-Field model: ECS
Cryst. Growth Des., 2787 (2015)
Surface energy minimal in the directions of the 4 vertices of a tetrahedron
Notes: Self similarity

## Slide 12: Showcasing the Phase-Field model: KCS
PSSB, 1800518 (2019)
Adatom lifetime maximized on {111} facets

## Slide 13: Thermodynamics VS kinetics
Equilibrium Crystal Shape
Kinetic Crystal Shape
Surface diffusion VS deposition dynamics
Surface energy VS adatom incorporation rates
Balance between the kinetics and energetic contributions

## Slide 14: Interactions between γ and τ
interrupting
growth
Tends towards ECS
Tends towards KCS
γ favors {10} facets
τ favors {11} facets
PSSB, 1800518 (2019)

## Slide 15: Interactions between τ and F
An increased magnitude of both factors drives growth towards the kinetic regime
Faceting from τ (n) dominates for small particles
The balance between different contributions is local
Kinetically controlled
Thermodynamically controlled
PSSB, 1800518 (2019)
Notes: Faceting from τ (n) dominates foronly when:
F/M is low
Size does not exceed diffusion length
More important for small particles

## Slide 16: Strong Anisotropy
Surface Science 454–456 (2000) 94–100
Chemical Potential
Ginzburg-Landau energy functional

## Slide 17: Modelling Strongly Anisotropic Systems
Proc. R. Soc. A (2009)
= 0.06
= 0.2
= 0.3

## Slide 18: Surface Energy Density
Here:
Cryst. Growth Des., 2787 (2015)

## Slide 19: Evolution from Sphere toward the ECS
Cryst. Growth Des., 2787 (2015)

## Slide 20: Morphologies of Metastable Structures
Cryst. Growth Des., 2787 (2015)
Cryst. Growth Des. 2010, 10, 2509

## Slide 21: Morphologies of Metastable Structures
Chem. Eur. J. 2005, 11, 454 – 463
Cryst. Growth Des., 2787 (2015)

## Slide 22: Introduction

## Slide 25: Possible two index facet combination

## Slide 26: Possible two index facet combination

## Slide 27: Possible two index facet combination

## Slide 28: Side-facets with various Temperature (Method I)

## Slide 29: Side-facets with varying other parameter (Method I)

## Slide 30: Side-facets with other pre-growth method (Method II)

## Slide 31: Summary
Facet-Dependent properties
ECS: Wulff and Winterbottom construction
The relative magnitude of κ, γ, τ and v controls the growth regime (κγ/τv), which may change over time
Understanding strong anisotropy
Understanding metastable nanostructures with phase field model
MOCVD and VLS based side-facet engineering: Temperature, Growth rate.
Other affecting parameter: Thermal decomposition, Reduced diffusion length

## Slide 32: Thank you for your attention