## Slide 1: Electron Microscopy
4. TEM
Electron diffraction
Basics: interactions, basic modes, Diffraction: elastic scattering theory, reciprocal space, diffraction pattern,
Laue zones
Diffraction phenomena
XRD x-ray diffraction

## Slide 2: Typical TEM
EPFL: Philips CM300
300’000V

## Slide 3: Signals from a thin sample
Specimen
Incident beam
Auger electrons
Backscattered electrons BSE
secondary electrons SE
Characteristic X-rays
visible light
“absorbed” electrons
electron-hole pairs
elastically scattered electrons
direct beam
inelastically scattered electrons
Bremsstrahlung
X-rays
1-100 nm

## Slide 4: Interaction of high energetic electrons with matter
biological samples,
polymers
crystalline structure,
defect analysis,
high-resolution TEM
chemical analysis,
spectroscopy

## Slide 5: Interaction -> contrast
EDS, element maps
STEM-DF
Thin section of mouse brain: mass contrast of stained membrane structures
(G.Knott)
Dark field image of differently ordered domains:
Diffraction contrast
High-resolution image:
Image contrast due to interference between transmitted and diffracted beam
Element distribution maps
Of Nb3Sn superconductor

## Slide 6: Two basic operation modes Diffraction <-> Image
Diffraction Mode
Image Mode

## Slide 7
SEM
TEM
holey Carbon film
(K,Nb)TaO3
Nano-rods

## Slide 8: Shape, lattice parameters, defects, lattice planes
(K,Nb)O3
Nano-rods
Bright field image
dark field image
Diffraction pattern
High-resolution image

## Slide 9: Diffraction theory
Introduction to electron diffraction
Elastic scattering theory
Basic crystallography & symmetry
Electron diffraction theory
Intensity in the electron diffraction pattern
Thanks to Dr. Duncan Alexander for slides

## Slide 10: Why use electron diffraction?
Diffraction: constructive and destructive interference of waves
electrons interact very strongly with matter => strong diffraction intensity (can take patterns in seconds, unlike X-ray diffraction)
diffraction from only selected set of planes in one pattern - e.g. only 2D information
wavelength of fast moving electrons much smaller than spacing of atomic planes => diffraction from atomic planes (e.g. 200 kV e-, λ = 0.0025 nm)
spatially-localized information (≳ 200 nm for selected-area diffraction; 2 nm possible with convergent-beam electron diffraction)
orientation information
close relationship to diffraction contrast in imaging
immediate in the TEM!
limited accuracy of measurement - e.g. 2-3%
intensity of reflections difficult to interpret because of dynamical effects
( diffraction from only selected set of planes in one pattern - e.g. only 2D information)
( limited accuracy of measurement - e.g. 2-3%)
( intensity of reflections difficult to interpret because of dynamical effects)

## Slide 11: Image formation
BaTiO3 nanocrystals (Psaltis lab)

## Slide 12: Area selection
Insert selected area aperture to choose region of interest
BaTiO3 nanocrystals (Psaltis lab)

## Slide 13: Take selected-area diffraction pattern
Press “D” for diffraction on microscope console - alter strength of intermediate lens and focus diffraction pattern on to screen
Find cubic BaTiO3 aligned on [0 0 1] zone axis

## Slide 14: Scatter range of electrons, neutrons and X-rays
(99% of intensity lost)

## Slide 15: electron, neutron X-ray scattering
wave | Wavelength l | Source | Scattering at | Differentiation of | Sample size
X-rays | 0.07nm 0.15nm | X-ray tubes synchrotrons | Electron cloud | Lattice parameters Unit cell | 0.1mm
Electrons | 2pm @300keV | e guns (SEM/TEM) | Potential distribution (electrons & nucleus) | Lattice parameters, Orientations | 0.1um
Neutrons (1) | ~0.1nm | Nuclear reactors | Nuclear scattering (nucleus) | LP, isotopes | m
Neutrons (2) | “ | “ | Magnetic spin (outer electrons) | Oxidation states | m
Scattering power: n : X-ray : e = 1 : 10 : 104