## Slide 1: Scattering theory - Atomic scattering factor
Consider coherent elastic scattering of electrons from atom
Differential elastic scattering cross section:
Atomic scattering factor for electrons
The Mott-Bethe formula is used to calculate electron form factors from X-ray form factors (fx)

## Slide 2: Scattering theory - Huygen’s principle
Atoms closer together => scattering angles greater
=> Reciprocity!
Periodic array of scattering centres (atoms)
Plane electron wave generates secondary wavelets
Secondary wavelets interfere => strong direct beam and multiple orders of diffracted beams from constructive interference

## Slide 3: Basic crystallography Crystals: translational periodicity & symmetry
Repetition of translated structure to infinity

## Slide 4: Crystallography: the unit cell
Unit cell is the smallest repeating unit of the crystal lattice
Has a lattice point on each corner (and perhaps more elsewhere)
Defined by lattice parameters a, b, c along axes x, y, z and angles between crystallographic axes: α = b^c; β = a^c; γ = a^b

## Slide 5: Building a crystal structure
Use example of CuZn brass
Choose the unit cell - for CuZn: primitive cubic (lattice point on each corner)
Choose the motif - Cu: 0, 0, 0; Zn: ½,½,½
Structure = lattice +motif => Start applying motif to each lattice point

## Slide 6: Building a crystal structure
Use example of CuZn brass
Choose the unit cell - for CuZn: primitive cubic (lattice point on each corner)
Choose the motif - Cu: 0, 0, 0; Zn: ½,½,½
Structure = lattice +motif => Start applying motif to each lattice point
Extend lattice further in to space

## Slide 7: Diffraction theory - Bragg law
Path difference between reflection from planes distance dhkl apart = 2dhklsinθ
Electron diffraction: λ ~ 0.001 nm
therefore: λ << dhkl
=> small angle approximation: nλ ≈ 2dhklθ
Reciprocity: scattering angle θ ~ dhkl-1
2dhklsinθ = λ/2 - destructive interference
2dhklsinθ = λ - constructive interference
=> Bragg law:
nλ = 2dhklsinθ

## Slide 8: Bragg’s law
2 sinq dhkl = n l
Distance between lattice planes
d
Incoming wave
Outgoing wave
q
l
q
Difference in path
“1”
“2”
“1”
“2”
dhkl = n l/2 sinq
k
k’
g = k-k’
Elastic diffraction
|k| = |k’|
Periodic arrangement of lattice planes:
g : reciprocal lattice vector

## Slide 9: Multi-beam scattering condition
Electron beam parallel to low-index crystal orientation [U V W] = zone axis
Crystal “viewed down” zone axis is like diffraction grating with planes parallel to e-beam
In diffraction pattern obtain spots perpendicular to plane orientation
Example: primitive cubic with e-beam parallel to [0 0 1] zone axis
Note reciprocal relationship: smaller plane spacing => larger indices (h k l) & greater scattering angle on diffraction pattern from (0 0 0) direct beam
2 x 2 unit cells

## Slide 10: The reciprocal lattice
For scattering from plane (h k l) the diffraction vector: ghkl = ha* + kb* + lc*
rn = n1a + n2b + n3c
Real lattice vector:
In diffraction we are working in “reciprocal space”; useful to transform the crystal lattice in to a “reciprocal lattice” that represents the crystal in reciprocal space:
r* = m1a* + m2b* + m3c*
Reciprocal lattice vector:
a*b = a*c = b*c = b*a = c*a = c*b = 0
a*a = b*b = c*c = 1
a* = (b ^ c)/VC
where:
i.e.
VC: volume of unit cell
Plane spacing:

## Slide 11
kI: incident beam wave vector
Ewald sphere
Reciprocal space: sphere radius 1/λ represents possible scattering wave vectors intersecting reciprocal space
Electron diffraction: radius of sphere very large compared to reciprocal lattice => sphere circumference almost flat
kI
A vector in reciprocal space:
ghkl = h a* + k b* + l c*
diffraction if : kI – kD = g and |kI| =|kD|
Bragg and elastic scattering
real space
reciprocal space
a*
b*
Bragg: dhkl = l/2 sinq = 1/ |g|

## Slide 12
kI: incident beam wave vector
kD: diffracted wave vector
Ewald sphere
Reciprocal space: sphere radius 1/λ represents possible scattering wave vectors intersecting reciprocal space
Electron diffraction: radius of sphere very large compared to reciprocal lattice => sphere circumference almost flat
kI
kD
A vector in reciprocal space:
ghkl = h a* + k b* + l c*
diffraction if : kI – kD = g and |kI| =|kD|
Bragg and elastic scattering
real space
reciprocal space
a*
b*

## Slide 13: Laue Zones

## Slide 14
Laue zones
J.-P. Morniroli

## Slide 15: Ewald Sphere : Laue Zones (ZOLZ+FOLZ)
a=2.0mrad
s=0.2
ZOLZ
6-fold
FOLZ
3-fold
Source: P.A. Buffat

## Slide 16: Ewald Sphere: Laue Zones (ZOLZ+FOLZ) tilted sample
a=2.0mrad
s=0.2
ZOLZ
6-fold
FOLZ
3-fold

## Slide 17: Dynamical scattering
For interpretation of intensities in diffraction pattern, single scattering would be ideal - i.e. “kinematical” scattering
However, in electron diffraction there is often multiple elastic scattering:
i.e. “dynamical” behaviour
This dynamical scattering has a high probability because a Bragg-scattered beam is at the perfect angle to be Bragg-scattered again (and again...)
As a result, scattering of different beams is not independent from each other

## Slide 18: Dynamical scattering thickness fringes

## Slide 19: Symmetry information
Zone axis SADPs have symmetry closely related to symmetry of crystal lattice
Example: FCC aluminium
[0 0 1]
[1 1 0]
[1 1 1]
4-fold rotation axis
2-fold rotation axis
6-fold rotation axis - but [1 1 1] actually 3-fold axis
Need third dimension for true symmetry!