## Slide 1: Twinning in diffraction
Example: Co-Ni-Al shape memory FCC twins observed on [1 1 0] zone axis
Images provided by Barbora Bartová, CIME
(1 1 1) close-packed twin planes overlap in SADP

## Slide 2: Epitaxy and orientation relationships
SADP excellent tool for studying orientation relationships across interfaces
Example: Mn-doped ZnO on sapphire
Sapphire substrate
Sapphire + film
Zone axes:
[1 -1 0]ZnO // [0 -1 0]sapphire
Planes:
c-planeZnO // c-planesapphire

## Slide 3: Ring diffraction patterns
If selected area aperture selects numerous, randomly-oriented nanocrystals,
SADP consists of rings sampling all possible diffracting planes
- like powder X-ray diffraction
Example: “needles” of contaminant cubic MnZnO3 - which XRD failed to observe!

## Slide 4: Ring diffraction patterns
Larger crystals => more “spotty” patterns
Example: ZnO nanocrystals ~20 nm in diameter

## Slide 5: XRD
X-ray diffraction

## Slide 6: Laue Method

## Slide 7: Debeye-Scherrer

## Slide 8: X-ray tube

## Slide 9: Diffractometer

## Slide 14: References
“Transmission Electron Microscopy”, Williams & Carter, Plenum Press
http://www.doitpoms.ac.uk
“Transmission Electron Microscopy: Physics of Image Formation and Microanalysis (Springer Series in Optical Sciences)”, Reimer, Springer Publishing
“Large-Angle Convergent-Beam Electron Diffraction Applications to Crystal Defects”, Morniroli, Taylor & Francis Publishing
http://crystals.ethz.ch/icsd - access to crystal structure file database Can download CIF file and import to JEMS
Web-based Electron Microscopy APplication Software (WebEMAPS) http://emaps.mrl.uiuc.edu/
JEMS Electron Microscopy Software Java version http://cimewww.epfl.ch/people/stadelmann/jemsWebSite/jems.html
“Electron diffraction in the electron microscope”, J. W. Edington, Macmillan Publishers Ltd
http://escher.epfl.ch/eCrystallography