## Slide 1: MICRO-373: TP introduction
Spring semester 2024
Professor:
Ileana-Cristina Benea-Chelmus
Teaching assistants:
Francesco Bertot
Jiawen Liu
23/02/2024
Topic 1: Integrated photonic chip
IN
Micro heater
OUT
Antenna

## Slide 2: Professor and TAs
Professor: Ileana-Cristina Benea-Chelmus
TAs:
Jiawen Liu
Francesco Bertot
Zahra Basiri (backup)

## Slide 3: Integrated photonics: overview
K. Sengupta, et al., Nat. Electronics 1, 622–635 (2018), https://doi.org/10.1038/s41928-018-0173-2
Compact high-frequency components with large variety of applications

## Slide 4: Integrated photonics: overview
Compact high-frequency components with large variety of applications
K. Sengupta, et al., Nat. Electronics 1, 622–635 (2018), https://doi.org/10.1038/s41928-018-0173-2
E. Pelucchi, et al., Nat Rev Phys 4, 194–208 (2022). https://doi.org/10.1038/s42254-021-00398-z
Cointegration and compatibility with multiple alternative technologies

## Slide 5: Silicon-on-insulator (SOI) integrated photonics
Top Si device layer
220 nm
Silicon substrate
High refractive index contrast: @ 1550 nm nSi = 3.45, nSiO2 = 1.45
https://www.computerbase.de/2021-06/rohlinge-globalfoundries-sichert-sich-soi-wafer-von-globalwafers
https://www.siegertwafer.de/SOI-Wafer.html
P. Steglich, et al., Photoptics 2015, https://doi.org/10.13140/RG.2.1.1147.8565
SOI waveguides (WG): strip and slot geometry
Silicon-On-Insulator (SOI) platform for cutting-edge technologies
Buried oxide (BOX)
2 - 3 µm
SiO2
Strip WG
Slot WG
SiO2 cladding
Si core
Si rails
Optical field confinement (λ = 1550 nm)
SiO2
SiO2
450 nm
500 nm
220 nm

## Slide 6: SOI waveguides and components
Field confinement and discretization into modes:
SiO2
y
x
Si
Fixed distribution in (x,y) plane
Propagation along z
Prop. constant:
Main parameter is , defined by geometry, tunable (in our case) using micro-heaters

## Slide 7: SOI waveguides and components
Field confinement and discretization into modes:
Fixed distribution in (x,y) plane
Propagation along z
Mach-Zehnders interferometers (MZI)
Multi-Mode interferometers (MMI)
Couplers and ring resonators
X-coupler
10 μm
100 μm
Si
SiO2
Prop. constant:
SiO2
y
x
Si
Main parameter is , defined by geometry, tunable (in our case) using micro-heaters
100 μm
Au antenna
Grating coupler

## Slide 8: SOI waveguides and components
Field confinement and discretization into modes:
Fixed distribution in (x,y) plane
Propagation along z
Mach-Zehnders interferometers (MZI)
Multi-Mode interferometers (MMI)
Couplers and ring resonators
X-coupler
10 μm
100 μm
Si
SiO2
Au antenna
200 nm
Si
SiO2
Prop. constant:
Main parameter is , defined by geometry, tunable (in our case) using micro-heaters
100 μm
SiO2
y
x
Si
Grating coupler

## Slide 9: Complete GDS design example
Every layer is a lithography step!
1 mm

## Slide 10: What we will create together
Layer 1: waveguides
Layer 2: heaters
Final result:
Requires precise alignment

## Slide 11: Fabrication process flow
1. Starting point: SOI wafer
220 nm
2 μm
725 μm
2. First E-beam lithography for waveguides
ZEP resist spin coating, exposure and development
3. Si dry etching and resist stripping
Si
SiO2
ZEP
2 μm
200 nm
200 nm
Si
SiO2
Si
SiO2
Si
SiO2
Y-splitter

## Slide 12: Fabrication process flow
1. Starting point: SOI wafer
220 nm
2 μm
725 μm
2. First E-beam lithography for waveguides
ZEP resist spin coating, exposure and development
3. Si dry etching and resist stripping
Si
SiO2
ZEP
200 nm
3 μm
Si
SiO2
Si
SiO2
Grating coupler
3.5. Additional Si shallow etch (only 70 nm) performed by TAs
Si
Atomic Force Microscope

## Slide 13: Fabrication process flow
1. Starting point: SOI wafer
10 μm
220 nm
2 μm
725 μm
5. Second E-beam lithography for heaters
2. First E-beam lithography for waveguides
ZEP resist spin coating, exposure and development
3. Si dry etching and resist stripping
4. SiO2 cladding PECVD
MMA/PMMA resist double layer spin coating, exposure and development
6. Heaters (Ti-Au) deposition and lift-off
Si
SiO2
ZEP
MMA
PMMA
Ti
Au

## Slide 14: Fabrication process flow: final results
100 μm
SiO2
Au
SiO2
Au
500 nm
SiO2
Au
500 nm
Heater
MZI
X-coupler
y-splitter

## Slide 15: Characterization: setup in HYLAB laboratories
PMF
OF
TLS
PC
OF
PM
Characterization of the waveguides in transmission:
Acronims:
TLS = Tunable Laser Source
PMF = Polarization maintaining fiber
PC = Polarization controller
OF = Optical fiber
PM = Power Meter

## Slide 16: Typical transmission spectra
50 nm
Simple waveguide:
Ang
MZM with heater tuning nm:
Si
SiO2
V+
V-
Out 1
Out 2
In

## Slide 17: Typical transmission spectra
Ring resonators:
Transmission measurements
Wavelength (nm)
dB
Radius=100 µm
Radius=200 µm
CST simulation
SEM image
10 µm

## Slide 18: Organization of the semester
Week | Date | Step
1 | 01 – Mar | Theory/simulation + start GDS
2 | 08 – Mar | GDS creation
3 | 15 – Mar (CMi 1) | E-beam litho for waveguides
4 | 22 – Mar (Cmi 2) | Si dry etching + resist strip
5 | 12 – Apr (Cmi 3) | SEM + AFM
6 | 19 – Apr (Cmi 4) | E-beam litho for heaters
7 | 26 – Apr (Cmi 5) | Heaters deposition and lift-off
8 | 03 – May (Cmi 6) | SEM + Reflectometry
9 | 10 – May | Transmission measurements
10 | 17 – May | Transmission measurements
11 | 24 – May | Data analysis + report
12 | 31 – May | Report + final presentation prep
Sessions on Friday 14h15 to 18h
More details on the process flow and the tools used in cleanroom on Moodle
Transmission measurements in HYLAB laboratories, BM3237 and BM3239
Report submission due on June 7th, one week after the last session: follow guidelines on Moodle

## Slide 19: Preparation for first session
For mask layout visualization: download K-layout from https://www.klayout.de/build.html selecting the most recent version
  Try to open the GDS example found on Moodle and play with layers and components
For mask layout creation: we will use Python packages, so be ready to work on the Python environment you prefer.
  Our main choice is Spyder, launched through Anaconda. In this case, you can download it from www.anaconda.com
  A potential alternative is Jupyter Notebook, always launched through Anaconda
Prepare any question you want to ask to us!

## Slide 20: MICRO-373: TP introduction
Spring semester 2024
Professor:
Ileana-Cristina Benea-Chelmus
Teaching assistants:
Francesco Bertot
Jiawen Liu
23/02/2024
Topic 1: Integrated photonic chip
IN
Micro heater
X-coupler
OUT