20.64% Efficient and Stable Binary Organic Solar Cells via Thermodynamic-Engineered Interlayer Diffusion and Exciton Generation

Kangbo Sun1,$, Yufei Wang1,*,$, Guangye Zhang1,*,$, Chuanlin Gao1, Xiwen Ling1, Jianan Zheng1, Jiaxu Che1, Chen Xie1,  Zhibo Wang2, Huawei Hu2, Peng You1, Peigang Han1, Shunpu Li1, and Yiwang Chen3*

1 College of New Materials and New Energies, Shenzhen Technology University, Shenzhen, China

2 State Key Laboratory for Modiﬁcation of Chemical Fibers and Polymer Materials, College of Materials Science and Engineering, Donghua University, Shanghai, China

3 College of Chemistry and Chemical Engineering/Institute of Polymers and Energy Chemistry, Nanchang University, Nanchang, China

$ These authors contribute equally in this paper.

* Correspondence:

Yufei Wang

wangyufei@sztu.edu.cn

Guangye Zhang

zhangguangye@sztu.edu.cn

Yiwang Chen

ywchen@ncu.edu.cn

Keywords: organic solar cells, device engineering, interlayer diffusion, sequential processing, non-radiative recombination.

Materials

D18 was purchased from Hyper, Inc. eC9, eC9-4F, L8-BO and PNDIT-F3N were purchased from eFlexPV Limited. 2PACZ was acquired from the TCI. All the other reagents and chemicals were purchased from Sigma Aldrich or Aladdin and used as received.

Device Fabrication. Organic solar cells (OSCs) with the structure of ITO/2PACz or PEDOT:PSS/D18/acceptor/PNDIT-F3N/Ag were fabricated. Indium tin oxide (ITO) glass substrates were sequentially cleaned with detergent, deionized water, and isopropanol, followed by drying in an oven. Subsequently, the ITO substrates were treated with UV-ozone for 25 minutes for the PEDOT:PSS-based devices, while the 2PACz-based OSC utilized plasma cleaner treatment for ITO substrates. First, regarding the hole transport layer (PEDOT:PSS or 2PACZ) prepared on the ITO/Glass substrate, PEDOT:PSS was spin-coated onto clean ITO-coated glass substrates (5000 rpm for 30 s) and baked at 160 ℃ for 15 min. 2PACz was dissolved in ethanol with a concentration of 0.27 mg/mL. The 2PACz solution (100 µL for a 1.5 × 1.5 cm2 substrate) was applied directly onto the ITO substrate for 30 s followed by a spin-coating step at 3000 rpm for 30 s. The ITO/2PACZ substrate was then placed onto a hotplate and annealed at 100℃ for 5 min. The D18 donor material was dissolved in chloroform at a concentration of 5 mg/mL and heated at 80 °C under continuous stirring for approximately 1 hour. The acceptor materials (eC9, L8-BO, and eC9-4F) were separately dissolved in chloroform at 7.5 mg/mL, followed by heating at 50 °C for 1 hour with sustained agitation. The detailed preparation protocols for SqP films using three distinct processing methods are described as follows.

For the conventional method, the substrate with the hole transport layer was maintained at ambient temperature (~29.7 °C).  Herein, the D18 solution (2800 rpm, 20s) and acceptor solution (3000 rpm, 20s) were cooled for 5 minutes to room temperature for subsequent sequentially spin-coating process under room-temperature conditions.

For the HS process, the donor solution and acceptor solution were cooled for 5 minutes to room temperature for subsequent spin-coating process. Firstly, placing the substrate with the hole transport layer on a uniform heating stage (with an optimal temperature of 70 ℃) for preheating. After preheating, the substrate was quickly transferred onto the chuck of the spin coater, at which point its surface temperature dropped to approximately 59.1 ℃. Subsequently, the pre-spinning stage was initiated, during which the substrate temperature gradually decreased. Once the temperature reached ~50 °C, a D18 solution (at room temperature) was immediately spin-coated onto the hole transport layer at 2800 rpm for 20 seconds. When the substrate surface temperature naturally cooled to 36.4 °C through high-speed rotation of the spin coater, the acceptor solution (also at room temperature) was promptly spin-coated onto the D18 donor layer at 3000 rpm for 20 seconds. The temperature drop of the HS method occurred entirely through natural cooling without any external intervention or auxiliary cooling methods.

For the hot-solution method, the D18 donor solution was preheated at 80°C for 5 minutes on a temperature-controlled hotplate, while the acceptor solution was maintained at ambient conditions. The deposition sequence began with immediate spin-coating of the preheated D18 solution onto the hole-transport-layer-coated substrate at room temperature, followed by spin-coating of the room-temperature acceptor solution onto the formed D18 donor layer after a precisely controlled 20-second interval.

For all of the devices, a methanol with 0.5% vol acetic acid blend solution of PNDIT-F3N at a concentration of 0.5 mg mL-1 was spin-coated onto the active layer at 2000 rpm for 30 s. Finally, around 100 nm of Ag was evaporated under 1×10-4 Pa through a shadow mask. Then, the encapsulation was carried out.

Device characterization. The encapsulated devices were comprehensively characterized through sequential measurements: Current density-voltage (J-V) curves were recorded under AM 1.5G illumination (100 mW·cm⁻²) using an Enlitech solar simulator coupled with a Keithley 2400 Source Meter, with light intensity calibrated through a KG5-filtered reference silicon diode to eliminate spectral mismatch. Concurrent optical microscopy (Olympus BX51) precisely defined the active device area as 4.01 mm². External quantum efficiency (EQE) measurements employed an Enlitech QE-S system featuring a 300 W xenon lamp monochromator, while frequency-dependent impedance spectroscopy and photo-CELIV analyses were conducted using a commercial Paios platform (FLUXiM AG) to probe charge transport dynamics. All electrical measurements were performed under nitrogen atmosphere to prevent environmental degradation.

Atomic force microscopy (AFM). AFM measurements were performed by using a Scanning Probe Microscope Dimension 3100 in tapping mode under atmosphere conditions at room temperature. All film samples were spin-cast on glass/ITO substrates.

Grazing-incidence wide-angle X-ray scattering (GIWAXS) measurements: Grazing-incidence wide-angle X-ray scattering (GIWAXS) measurements were conducted at the BL16B1 beamline of the Shanghai Synchrotron Radiation Facility (SSRF). Thin-film specimens were spin-coated onto silicon substrates using identical processing parameters and precursor solutions as those employed in device fabrication. A monochromatic 10 keV X-ray beam (λ = 0.124 nm) was incident at a grazing angle of 0.15° with 30-second exposure time to optimize scattering signal intensity. Diffraction patterns were recorded using a Dectris Pilatus 1M photon-counting detector positioned 220 mm downstream. The two-dimensional scattering data were processed through azimuthal integration using the Nika software package (v2.64) to generate quantitative one-dimensional (1D) intensity profiles. Crystallographic coherence lengths were derived via Scherrer analysis:CCL = 2πK/FWHM，where K represents the dimensionless shape factor (0.9 for spherical crystallites), FWHM denotes the full-width-at-half-maximum of diffraction peaks (radians), and θ corresponds to the Bragg angle of respective lattice planes.

SCLC Measurements: Unipolar charge transport devices were fabricated with tailored architectures: Electron-only devices (ITO/ZnO/D18/eC9/PNDIT-F3N/Ag) and dual-configuration hole-only devices (ITO/PEDOT:PSS/D18/MoO₃/Ag and ITO/ZnO/D18/eC9/PNDIT-F3N/Ag) were prepared with controlled active layer thicknesses of 60 nm for pristine D18 and 100 nm for D18:eC9 blend layers. Current density-voltage (J-V) characterization under dark conditions (0-8 V bias range) enabled space-charge-limited current (SCLC) analysis via the Mott-Gurney formalism, where carrier mobilities were derived through numerical fitting of the equationJ=9ε0εrμV28d3，where J is referred current density, εr stands for the relative dielectric constant in the organic photoactive layer (3.00), ε0 represents the vacuum permittivity of 8.85×10−12 F m−1, d is the organic layer thickness (100 nm), V is the applied voltage, and μ expresses mobility.

Transient photovoltage (TPV) and transient photocurrent (TPC) measurements:  In TPV measurements, the OSCs devices were maintained under background light bias using a focused quartz tungsten-halogen lamp with an intensity comparable to operational conditions (i.e., achieving a device voltage matching the open-circuit voltage under solar illumination). Photoexcitation was generated by 8 ns pulses from a laser system (Oriental Spectra, NLD520) tuned to 518 nm wavelength with a spectral width of 3 nm. The TPV signals were recorded at open-circuit conditions using a digital oscilloscope. For TPC measurements, signals were acquired under short-circuit conditions using the same excitation wavelength but without background light bias.

Deep level transient spectroscopy measurement (DLTS): DLTS was performed using a current-based simulation method. The transient current response was analyzed by applying a negative pressure -3 V to the device in the dark. The transient current reached its maximum response at t = 0.1s regardless of the bias voltage, with the peak gradually rising at 0.1s as the bias voltage increased. In addition to the displacement current generated by the circuit, there is also the current emitted by the discrete energy trap. The following equation was used to estimate the defect distributions in organic semiconductors. Considering the dependence of carrier transport position in the device, the current peak in the first 0.1 μs is mainly caused by the displacement current, so the fitting of 0.1 ~ 10 μs at room temperature dominated. The trapped defect state volume density Nt of the discrete energy trap can be expressed as:

jtet=2 ×1τte×q×d×Nt×exp⁡(−tτte)

where jtet is the trap emission current, τte the catch-trap emission time constant, q the elementary charge, d the film thickness, and Nt the trap state density.

FTPS-EQE and EL-EQE measurements. Fourier-transform photocurrent spectroscopy external quantum efficiency (FTPS-EQE) measurements were conducted using a PECT-600 integrated system (Enlitech) with phase-sensitive detection, where the photoresponse signal was amplified through a Stanford Research SR830 lock-in amplifier at 17 Hz modulation frequency. Electroluminescence external quantum efficiency (EL-EQE) characterization was performed under controlled carrier injection using a REPS-Pro voltage/current source (Enlitech), with devices fabricated under optimized conditions (active layer thickness: 100±5 nm, electrode alignment: <2 μm offset). The EL-EQE voltage sweep protocol spanned from 0 V to 1.8 V (0.1 V step, 500 ms dwell time) to systematically probe the recombination dynamics across the operational bias range. Both characterization techniques employed thermoelectrically cooled InGaAs detectors (900-1600 nm range) with NIST-traceable calibration, ensuring wavelength-dependent quantum efficiency accuracy within ±1.5% were carried out from 0 to 1.8 V.

Film-depth-dependent light absorption spectroscopy (FLAS): Perform depth dependent light absorption analysis using a low-energy in-situ spectroscopic etching system (PU100, Shaanxi Puguang Weishi Co., Ltd., China). The plasma etching process operates at 100 W RF power and 10 Pa pressure, achieving a controlled material removal rate of 0.8 nm/s while maintaining the integrity of the subsurface structure. Real time optical monitoring is achieved through a fiber coupled spectrometer (350-850nm spectral range, 1nm resolution) to capture continuous absorption spectra during the layer by layer material ablation process. The film surface was incrementally etched by the soft ion source, without damage to the materials underneath the surface, which was in situ monitored by a spectrometer. From the evolution of the spectra and the Beer–Lambert’s Law, film-depth-dependent absorption spectra were extracted.

Maximum power point tracking (MPPT) measurements: The devices photostabilities were measured by using the solar cell stability test system (PR-SCCS, PURI Materials, China), and PURI2400-8Q as the source meters to record the solar-cells characteristics in an ambient atmosphere, which were conducted under continuous 100 mw cm-2 illumination provided by LED-solar simulators (PR-LEDSUN-8C, PURI Materials, China, with spectrum ranging from 350nm to 900 nm). And the results were automatically recorded by the aging test software (PR-SCCS-MPPT, PURI Materials, China).

Figure S1. The energy levels of D18 and eC9 acquired from the reference. [1]

Figure S2. The temperature variation of the preparation of D18/eC9 film surface with spin coating time. Herein, D18 and eC9 solution are spin-coated on the silicon wafer under room temperature (~31℃) in turn.

Figure S3. The variation of substrate surface temperature with spin coating time during the preparation of D18/eC9 films. Herein, D18 solution are preheated under 80℃ before spin-coating, while eC9 solution are directly spin-coated on the D18 film.

Figure S4. Time-dependent surface temperature profile of the substrate under the whole SqP film fabrication process. Herein, D18 solution are preheated under 80℃ before spin-coating, while eC9 solution are directly spin-coated on the D18 film.

Figure S5. Time-dependent surface temperature profiles of the substrates during the entire SqP film fabrication processes, including ambient-temperature fabrication, HS method, and hot-solution technique on a) ITO substrate, and b) Si substrate.

Surface energy calculation of film

The solid surface energy using Owen Method was based on the following model:

γ=γd+γp                                                    (1)

γl=γlD+γlP                                                   (2)

where γs stands for the surface of the solid, which consists of the polarity force γp and dispersion force γd, and γl refers to the surface energy of the liquid with the corresponding polarity force γlP and dispersion force γlD. According to the following equation, the γp and γd of measured film can be acquired.

γl1+cosθ=2γdγlD1/2+2(γpγlP)1/2                          (3)

In this work, the water (H2O) and ethylene glycol (EG) are used as the testing liquids to extract the γp and γd. The contact angles and surface energies of different films are illustrated in Table S1.

Figure S6. a) Contact angle images of pure D18, eC9 and SqP films. Top region is water contact angle, ethylene glycol contact angle is located in bottom region. b) Statistical analysis of surface energy and its components for D18, eC9 and SqP films.

Table S1. Contact angles and surface tensions

| Film | Contact angle [°] |  | γd[mN m-1] | γp[mN m-1] | γ [mN m-1] |
| --- | --- | --- | --- | --- | --- |
|  | H2O | EG |  |  |  |
| D18 | 102.5 | 75.6 | 24.55 | 0.57 | 25.12 |
| D18 HS | 102.6 | 74.7 | 26.15 | 0.41 | 26.55 |
| eC9 | 92.8 | 63.9 | 28.05 | 1.92 | 29.97 |

Figure S7. a,b) Absorption spectra at representative times of D18 and D18 HS film during spin-coating process. c) In situ 2D absorption spectroscopy monitoring the formation of D18 films during spin-coating, herein, D18 solution was preheat under 80℃, the horizontal scale bar denotes absorption intensity. d) Absorption spectra at representative times of D18 hot-solution during spin-coating process.

Figure S8. Extracted D18 liquid phase and nucleation time from the formation process of D18, D18-HS D18-hot solution film.

Figure S9. a) Normalized absorption spectra of D18 and D18 HS films wavelength ranging from 400 to 700nm. b) Normalized absorption spectra of D18 and D18 HS films wavelength ranging from 560 to 700nm.

Figure S10. a,b) Absorption spectra at representative times of D18/eC9 and D18 HS/eC9 film during eC9 solution spin-coating process. c) In situ 2D absorption spectroscopy and d) corresponding absorption spectra at representative times monitoring the formation of D18/eC9 films during eC9 solution spin-coating process, herein, D18 solution was preheat under 80℃.

Figure S11. Statistics of D18 secondary nucleation kinetics characteristic time and eC9 nucleation characteristic time based on the in-situ absorption of SqP films during later acceptor solution spin-coating process.

Figure S12. AFM height images and phase images of the D18 and D18 HS film.

Figure S13. High resolution TEM images of the D18 and D18 HS films.

Figure S14. AFM height images and phase images of the D18 and D18 HS film after CF washing.

Figure S15. a) Absorption spectra of films before and after CF washed. a) D18/eC9 and D18 HS/eC9. b) D18, D18 HS hot-solution casted D18 films. Herein, the data is measured using UV absorption spectrometer.

Figure S16. GIWAXS line profiles of D18/eC9 and D18 HS/eC9 films across the IP and OOP directions.

Table S2. GIWAXS peak information of out-of-plane (010) and in plane (100) of SqP films.

| Sample | Direction | q (Å-1) | d-spacing (Å) | FWHM (Å-1) | CCL (Å) |
| --- | --- | --- | --- | --- | --- |
| D18/eC9 | IP | 0.308 | 20.40 | 0.054 | 104.72 |
|  | OOP | 1.702 | 3.69 | 0.168 | 33.66 |
| D18 HS/eC9 | IP | 0.311 | 20.20 | 0.053 | 106.70 |
|  | OOP | 1.715 | 3.66 | 0.153 | 36.96 |

Figure S17. Depth-dependent absorption spectra of ITO/PEDOT:PSS/active layer/PNDIT-F3N samples under etching time: a) D18:eC9, b) HS-casted D18:eC9 films, c) D18/eC9 SqP and d) D18 HS/eC9 SqP films.

Figure S18. Normalized absorption spectra of pristine eC9 films.

Figure S19. The integration of exciton generation rates over film depth direction.

Figure S20. J−V curves of SqP OSCs based on D18/eC9 and D18 HS/eC9 under different substrate temperature.

Table S3. Device parameters of D18/eC9 and D18 HS/eC9 devices casted at different substrate temperature.

| Condition | VOC [V] | JSC [mA cm-2] | FF [%] | PCE [%] |
| --- | --- | --- | --- | --- |
| Control | 0.857 | 27.75 | 79.37 | 18.89 |
| 40℃ HS | 0.863 | 27.77 | 79.82 | 19.12 |
| 50℃ HS | 0.868 | 28.10 | 81.94 | 19.75 |
| 60℃ HS | 0.861 | 28.20 | 79.37 | 19.27 |
| 70℃ HS | 0.861 | 27.25 | 79.17 | 18.57 |

Figure S21. J−V curves of 10 independent devices for each condition of a) D18/eC9 and b) D18 HS/eC9. The distribution of photovoltaic parameters across ten independently fabricated devices for c) VOC, d) JSC, e) FF and f) PCE.

Figure S22. a) J-V curves curves and b) corresponding EQE spectra of D18/eC9 devices based on the hot-solution method and the combined method.

Table S4. Photovoltaic parameters of D18/eC9 devices with PEDOT:PSS as the hole transport layer.

| Condition | VOC[V] | JSC [mA cm-2] | FF [%] | PCE [%] |
| --- | --- | --- | --- | --- |
| hot-solution (80 ℃) | 0.861 | 27.87 | 79.75 | 19.14 |
| hot-solution (80 ℃) & hot-substrate (50 ℃) | 0.862 | 26.62 | 79.80 | 18.31 |

Figure S23. JSC versus illumination intensity relationship of pristine SqP devices and HS-treated D18/eC9 OSCs.

Figure S24. Dark current curves of D18/eC9 and D18 HS/eC9 devices.

Figure S25. The equivalent circuit for fitting impedance spectroscopy. Rs corresponds to the electrode resistance including ITO and Ag. Parallel R1 and C1 correspond to the bulk resistance and capacitance of the active layer. Parallel R2 and C2 correspond to resistance and capacitance of the PEDOT:PSS and PNDIT-F3N interlayer.

Table S5. Fitting Parameters of impedance spectroscopy using equivalent circuit.

| Condition | Rs [Ω] |  | C1 [nF] |  | R1 [Ω] |  | C2 [nF] |  | R2 [Ω] |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Value [Ω] | Error [%] | Value [nF] | Error [%] | Value [Ω] | Error [%] | Value [nF] | Error [%] | Value [Ω] | Error [%] |
| D18/eC9 | 29.86 | 3.42 | 4.72 | 2.50 | 105.2 | 2.58 | 3.05 | 0.46 | 5165 | 0.28 |
| D18 HS/eC9 | 33.28 | 1.69 | 17.43 | 7.20 | 17.34 | 4.39 | 4.31 | 0.33 | 1694 | 0.17 |

Figure S26. DLTS datas and fitting curves of D18/eC9 and D18 HS/eC9 devices.

Figure S27. J−V curves of hole-only (ITO/PEDOT:PSS/film/MoO3/Ag) and electron-only (ITO/ZnO/film/PNDIT-F3N/Ag) devices. a) Hole-only curves for D18 and D18 HS films. b) Hole-only curves and c) electron-only curves for D18/eC9 and D18 HS/eC9 films.

Figure S28. Semi-logarithmic plots of normalized EL and measured EQE by FTPS as a function of energy for devices based on D18/eC9 and D18 HS/eC9 SqP devices.

Table S6. Detailed Eloss parameters in D18/eC9 and D18 HS/eC9 SqP devices

| Condition | VOCa) (V) | Egb) (eV) | qVloss (eV) | VOC SQ c) (V) | VOC rad d) (V) | ΔE1 (eV) | ΔE2e) (eV) | ΔE3f) (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| D18/eC9 | 0.850 | 1.391 | 0.542 | 1.131 | 1.081 | 0.261 | 0.050 | 0.231 |
| D18 HS/eC9 | 0.871 | 1.404 | 0.533 | 1.142 | 1.085 | 0.262 | 0.057 | 0.214 |

a) VOC: measured in the voltage loss test without an aperture.

b) Eg: optical bandgaps, via the derivatives of the EQE spectra (dEQE/dE).

c) V𝑜𝑐𝑆𝑄: Schokley-Queisser limit to VOC.

d) V𝑜𝑐𝑟𝑎𝑑: radiative limit to Voc, measured using EQEEL

e) ∆E2 ((VocSQ-Vocrad): voltage losses due to non-ideal absorption (it was calculated from EL and FTPS measurements).

f) ∆E3 (∆𝑉𝑜𝑐 𝑛𝑜𝑛−𝑟𝑎𝑑): voltage losses due to non-radiative recombination only.

Figure S29. The chemical structures of L8-BO and BTP-eC9-4F acceptors.

Figure S30. The EQE spectra of D18/eC9 casted by different method on 2PACZ hole transport layer.

Figure S31. The EQE spectra of D18/eC9-4F and D18 HS/eC9-4F devices using 2PACZ hole transport layer, the active layer thickness is 100nm.

Figure S32. The EQE spectra of 2PACZ-casted OSCs based on D18/L8-BO system.

Figure S33. The EQE spectra of thick-film OSCs based on D18/eC9-4F system with or without HS method.

Figure S34. Certificate of the D18 HS/L8-BO device issued by South China National Center of Metrology, China.

Figure S35. Morphological evolution of D18/eC9 films deposited on (a, c) PEDOT:PSS and (b, d) 2PACZ layers, as characterized by (a, c) AFM height images and (b, d) corresponding phase images.

Reference

[1] J. Tang, C. Liao, Y. Duan, X. Xu, M. Deng, L. Yu, R. Li, Q. Peng, Angew. Chem. Int. Ed. 2022, 134, e202213252.