## Slide 1: Advanced materials processing with intelligent systems Light materials interaction
Sergey Shevchik & Patrik Hoffmann

## Slide 2: Content
Light meets materials
  Reflection
  Transmission
  Scattering
  Absorption
Time scales of effects
  Fluorescence
  Heating

## Slide 3: Light absorption
Light that is absorbed makes a photon disappear !
  Where is the energy going?
Time scales of effects
  Fluorescence
  Heating

## Slide 4: Absorption & Fluorescence
http://micro.magnet.fsu.edu/primer/techniques/fluorescence/fluorescenceintro.html
!
non-radiative transition → transformation into heat
Absorption & fluorescence in a single molecule, ion, atom

## Slide 5: Contents
Absorbed light  Heat
Heat flow (heat equation)
Notes: Thermal – black body emission – Planks law

## Slide 6: Heat
Heat flows from warm to cold, Fourier law
Heat = energy contained in excited phonons (lattice vibrations)
for liquids: additionally in rotation of molecules

## Slide 7: Heat flux
Which parameters determine the final state (temperature distribution) ?
Which parameters influence the dynamics of the flow?
thermal capacity, density/mass
thermal capacity, thermal conductivity, density
Notes: HEAT FLOW
finger toching the oven – burned finger

## Slide 8: How heat can be transported?
Other (indirect) means?

## Slide 9: Phase Transition
evaporation needs much more (5x-10x) energy than melting and heating the material !!!

## Slide 10: Transport Phenomena
Heat flow
Materials flow (diffusion)
Viscosity
Heat flow
Mass flow
Momentum flow
Driving force for transport are spatial inhomogeneities, i.e. gradients
System state
Transported quantity
Material property

## Slide 11: Heat flow
form of the equation in case the external heat source is present
how temperature field changes in time
based on existing temperature distribution
and external heat sources and heat losses

## Slide 12: Heat Source – Laser Irradiation
Heat flux
  Laser heating depends on a large number of parameters
    Optical properties of material (R, a, ..)
    Heat transport in and out of irradiation zone
    Heat storage in and out of zone
    Phase transition Enthalpies
    Chemical reaction Enthalpies
    …

## Slide 13: Laser (light) Source Term
the intensity distribution of the laser light in the xy-plane.
the (maximum) laser light intensity not reflected from surface (z=0).
in simplified case α(T)=const
heat distribution in depth

## Slide 14: Anurag Singhania Master thesis 2020 Computational result: approach 1
Wafer at ambient temperature Preheated wafer
0.1 ms

## Slide 15: Anurag Singhania Master thesis 2020 Experimental results
10 W, substrate preheated to 820 C, varying pulse durations
5 ms 2 ms 1ms 0.75 ms 0.5 ms 0.25 ms

## Slide 16: Anurag Singhania Master thesis 2020 Experimental results
Effect of preheating wafer
Diameter of the melt zone increases roughly 2 to 3 times irrespective of the pulse duration
Height of material expulsion in the center increases significantly with increase in the pulse duration

## Slide 17: Heat Losses and Other Terms
Conduction
Convection
Radiation
Phase transitions
Chemical reactions

## Slide 18: Free Convection
For surface A > 1cm2
air
liquid
cooling by gas convention is not very efficient

## Slide 19: Laser Welding
Liquid convection still plays an important role in “slow” processes.
e.g. welding (drilling, cutting)
Sample movement
welded seam
melt
laser beam

## Slide 20: Forced Convection
Free convection is negligible if:
Ratio of buoyancy to viscous forces
Ratio of inertia and viscous forces
g = gravitational acceleration m/s2
b = volumetric expansion coefficient K-1
 = kinematic viscosity m2/s
F.P. Incropera, D.P. DeWitt; Fundamentals of Heat and Mass Transfer; John Wiley & Sons, NY, 4th ed. 1996
/ 1

## Slide 21: Radiation Cooling
increases very strongly with temperature!!!
maybe important in some cases.
Stefan–Boltzmann law

## Slide 22: Phase changes & Chemical reactions
DHm= 2-10 kcal/mol
DHv= 50-100 kcal/mol

## Slide 23: Comparison: Convection - Radiation
Example:
emissivity 0.4

## Slide 24: Thermal Penetration Depth
Pulsed laser irradiation results in a temperature rise in the material to a limited depth.
D =
Heat diffusivity
κ – heat conductivity
ρ – material density
Cp – heat capacity
Thermal penetration depth

## Slide 25: Table of material properties
good metal
good metal
ceramics
water & polymer
0.086
“bad” metal
“bad” metal

## Slide 26: Cooling/heating terms
Convection may play a role for cooling of the whole machined piece of material – not relevant for machining
Radiation may have contribution at very high temperatures
In most cases cooling of the laser machined region takes place by heat conduction in the piece

## Slide 27: Heat equation moving substrate
Heat source
Energy deposited, consumed or absorbed by unit of volume
Mass density
Specific heat at constant pressure
Relative speed of sample to beam
Thermal conductivity
Heat diffusivity
heating of the material
heat conducted away
heat brought by moving

## Slide 28: Heat flow in 3 dimension
m = dimension of problem (m = 1, 2, 3)
Q = total energy deposited
r = mass density per distance, surface or volume (g/cmm)
Solution:

## Slide 29: Laser Welding
What is the dimensionality of the heat flow problem at each of the stages?
Melt zone
Laser beam
sample

## Slide 30: Result of linearized heat equation
Semi-infinite substrate
Si, l = 514 nm
  All optimized to get
  Tmax in center of 287°C
case | Waist w0 (mm) | Power (mW)
a | 1 | 173.5
b | 5 | 574
C | 15 | 1535
Distance from spot center r (mm)

## Slide 31: Result of numerical heat flow simulations
Semi-infinite substrate
Si, l = 514 nm
temperature dependence of heat conductivity and reflectivity is important to consider!!!!

## Slide 32: Heat Accumulation - Effect of the Repetition Rate
Polyimide α~105cm-1@308nm - absorption on the surface Effect will be visible only at high rep.rate
Photoresist Vacrel 8230 α~5000cm-1@308nm – deep light penetration effect visible at low rep.rate

## Slide 33: Heat Accumulation
high repetition rate  results in heat accumulation effect and increase in ablation rate
Burns F.C. and Cain S.R.; J. Phys. D. Appl. Phys., 29 (1996) 1349
Polyimide α~105cm-1@308nm - absorption on the surface Effect will be visible only at high rep.rate

## Slide 34: Complete heat transfert through wall/window
window
wall
T1
T2

## Slide 36: ns-machining vs. fs-machining
ns
fs

## Slide 37: Ultrafast Laser Pulses
cool lattice
for τ<1-10 ps pulses - light absorption is faster than heat transfer from electron to atoms
heating rate is very high – heat penetration is low

## Slide 38: fs-laser machining
Diamant
Glas
Zahnschmelz
Speziallegierungen
Silizium
Kupfer