## Slide 2
Conduction  keyhole
Pores removal
Conduction 
unstable keyhole
Deep keyhole
Yet another explanation: Dynamic transients taking place inside the material at high velocities
All videos from Empa- LAMP
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 3
One way to tackle these difficulties: Add sensors
General Setup
Sensors
Acoustic
Piezo optical fibre
High speed imaging
Optical sensors
You name it!
OES
Photo-diode
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 4
0
1
2
3
4
5
6
Frequency (MHz)
0
1.4
AE
BR
Supervised learning
  Infers a function from labelled training data.
  Typical supervised learning
    Support Vector Machine (SVM)
    Decision tree (Random forest, gradient boost)
    Deep Neural Network (CNN, SCNN, …)
    Laplacian Graph (single kernel, multi-kernel (Empa))
Unsupervised (e.g. k-mean, autoencoders)
Reinforcement learning (game Go)
One way to tackle these difficulties: Signal processing
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 5: But linking signal to event is a real challenge
Aluminum plate 2mm thick,
no gas shielding, room temperature
Keyhole experiment with defects
Laser 1070 nm, pulse length 10 ms,
laser spot  30 mm
ESRF ID19 X-ray beam
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 6
Classification tasks
Pore formation
(e)
Process runs
Get signal from the workpiece
Analysis of the signals
Prediction of the defects creation
Tune the laser power
Ideally no human intervention!
Machine learning / Artificial intelligence
Human
intelligence
Sensors
You name it!
The final objective: Realise the dreams of companies
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 7
A laser physicist
A material scientist
An excellent technician/ engineer
An optics specialist
A process engineer
What is the team to achieve this goal?
An acoustic specialist
A conductor /
A translator
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 8: Contents of the lecture
Laser processing
  Laser Principles
  Laser types (e.g. fs, ps, ns, ms, continuous)
Sensors
  Acoustics (use, type, else)
  Optics
  Opto-acoustic (in particular Fiber Bragg Grating)
  Visual
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 9: Contents of the lecture
Data acquisition
  Principles
  Possibilities, limits
Introduction to machine learning
  Linear regression
  Supervised methods
  Semi-supervised methods
  Unupservised methods
  Reinforcement learning
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 10: Contents of the lecture
A complete example of the approach for
  Laser welding
  Additive manufacturing
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.

## Slide 11: So le’ts start?
Materials processing with intelligent systems (MICRO-457) Shevchik S. & Hoffmann P.