## Slide 1: Advanced materials processing with intelligent systems Light materials interaction
Sergey Shevchik & Patrik Hoffmann
References:
https://micro.magnet.fsu.edu/primer/virtual/virtual.html

## Slide 2: Content

## Slide 3: Content
Light meets materials
  Reflection
  Absorption
  Transmission
  Scattering

## Slide 4: Light meets material
Light meets materials
  Reflexion
  Absorption
  Transmission
  Scattering

## Slide 5: Fresnel Equations
Light intensity (Power) coefficients:
In case of normal incidence:
Do not forget to use complex refractive index, if absorption is present!
, etc.
normal incidence
general case

## Slide 6: Fresnel coefficients
The materials refractive index determines the fraction of reflected light R
  The reflexion coefficient R is polarization dependent:
  n1,2 refractive index of medium 1 et 2
  θi incident angle
  θt transmitted angle
Can the reflected light intensity be calculated?

## Slide 7: Polarisation
What is polarization?
For linearly polarized light:
  s – polarisation Ʇ (senkrecht; german for perpendicular)
    Electric field vector perpendicular to light propagation plane
  p - polarisation II (parallel)
    Electric field vector lies in the light propagation plane
  polarization filters are often used in photographie

## Slide 8: Angle de Brewster
with Snell-Descartes law

## Slide 9: Reflection
Brewster Angle
Excited dipoles cannot reemit light in the direction parallel to the dipole vector  no reflected light if,

## Slide 10: Reflection
machining under Brewster angle (increase absorption for metals)

## Slide 11: Diffuse reflectance
https://micro.magnet.fsu.edu/primer/java/reflection/specular/index.html

## Slide 12: Optical properties of Metals
Metals are shiny and typically not transparent
What would be the best laser for metal processing?

## Slide 13: Electrons in Metal
acceleration
damping
“spring” (returning force) term is not present
E-field driving force
in metal electrons are not bounded  free-electron plasma
dielectric constant for free-electron plasma (in first approximation for metals):
plasma frequency

## Slide 14: Theoretical Plasma Frequencies
reflectivity of free-electron gas and real metal (Al)

## Slide 15: Frequency Dependence
Frequency dependence of dielectric function, refractive index, Reflectance and absorption coefficient for free-electron plasma (metal)
(for ħp=8.3 eV, Ne=5x1022 cm-3, ħ/τ=0.02 eV)
Notes: plasma frequency of Au and Cu are in the visible range

## Slide 16: Dielectric Constant and Conductivity
conductivity and plasma frequency of a metal are directly linked
(link between optical and electrical properties)

## Slide 17: Reflection of Al, Ag & Au
Notes: Reflection coeffician can not be in [µm]!!!!!!!!!!!

## Slide 18: Reflection coefficients and penetration depth for some Materials
for metals for frequencies between: 1/τe <  < p (optical, vis.)
Notes: mark the rows (materials), (diaelectric, good/bad metels, …)
optical , thermal penetratin depthe
AgCl – fibers for CO2 laser

## Slide 19: dependances
Index of refraction is wavelength dependent
Reflection depends on polarisation
589 nm sodium Na line
  n1,2 indice de réfraction des milieux 1 et 2

## Slide 20: Light meets material
Light meets materials
  Reflexion
  Absorption
  Transmission
  Scattering

## Slide 21: Light absorption
Light that is absorbed makes a photon disappear !
  Where is the energy going?
Light that is deviated only, does not loose energy!
  Reflection
  Transmission
  Scattering

## Slide 22: Absorption
Light meets materials
  Absorption

## Slide 23: Absorption – Transmission index of refraction

## Slide 24: Absorption – Transmission index of refraction

## Slide 25: Transmission Spectra (Fused Silica)
Synthetic Grade Fused Silica (SiO2, 10 mm)
Almaz Optics Inc. http://www.almazoptics.com
Absorption due to electronic band to band transitions (band gap)
Absorption due to excitation of lattice vibrations (phonons)

## Slide 26: Transmission Spectra (Silicon)
Calculated transmission profiles of hyperpure Fz Silicon (Si) at 293K for substrate thicknesses between 1.0 and 3.5mm
Tydex J.S.Co http://www.tydex.ru
Silicon (5 mm) transmission. (pure and oxygen contaminated) Arrows point to the oxygen absorption peaks.
Absorption due to electronic band to band transitions (band gap)
Absorption due to excitation of lattice vibrations (phonons)
Notes: hide explanations to let students interpret the spectra

## Slide 27: Electronic absorption: Energy Levels

## Slide 28: Light absorption in a Gaseous Molecule
By TCReuter - Own work, CC BY-SA 4.0, https://commons.wikimedia.org/w/index.php?curid=49416990

## Slide 29: Sodium D-line
Cold sodium vapor (300°C) emits only light at 589,00nm and 589,59nm this sodium - D-line for doublet is almost monochromatic

## Slide 30: Sodium D-line – why is it a doublet ?
What happens if you put the Na vapor in a magnetic field ?
Could not have asked Pieter Zeeman when he discovered the effect in 1896 !

## Slide 31: Absorption
macroscopic (“black box”) description of absorption
Absorption | Wavelength (nm)
electronic molecular(s, p) | 10-150 – 1000-2000
electronic interband | 150 – 1000-2000
vibrational | 900 – 10’000
rotational | > 10’000
Types of Absorption /Excitation

## Slide 32: Absorption & Fluorescence
http://micro.magnet.fsu.edu/primer/techniques/fluorescence/fluorescenceintro.html
!
non-radiative transition → transformation into heat
Absorption & fluorescence in a single molecule, ion, atom

## Slide 33: Band Structure of Solids
http://en.wikipedia.org/wiki/Band_structure
Notes: electrons not a gas but occupy certain quantum states – which overlap into a band
electron are fermions

## Slide 34: Band Gap Absorption
Only photons with energy larger than the band gap of material are absorbed
Inter band absorption grates free charge carriers – new centers of absorption
hn
+
=

## Slide 35: Fluorescein
Formula of Fluorescein

## Slide 36: Absorption/Luminescence Centers in Solids
Energy Level Diagram of Nd3+-ion in YAG crystal
Emission spectrum of Nd3+-ion in YAG crystal

## Slide 37: Emission of Luminescent Lamp
emission of luminescent lamp is composed of narrow line emission of a mixture of phosphors

## Slide 38: Vibronic Transitions and Infrared Spectroscopy
Vibration of a di-atomic molecule
Selection rules for oscillation to be visible in IR spectroscopy: the dipole moment of a molecule have to change when undergoing the transition
quantized harmonic oscillator
quantized unharmonic oscillator
Notes: PERKIN_ELMER spectroscopy tutorial

## Slide 39: Infrared Spectroscopy

## Slide 40: Schematic of Infrared Spectroscopy
En pivotant le réseau (en anglais grating, prisme réflectif), la longueur d’onde arrivant sur l’échantillon est scannée.
L’absorption dans l’échantillon varie avec la longueur d’onde.
On obtient sur le détecteur un spectre IR.
Aujourd’hui on utilise la transformée de Fourier dans les machines, pour augmenter la vitesse et la precision.

## Slide 41: Electronic and Vibronic Trasitions
electronic and vibronic transition often interact – broadening of the transitions (emission / absorption peaks)

## Slide 42: Absorption
for linear absorption lost intensity in a thin layer is proportional to incident intensity
which results in a Beer-Lambert law
 - absorption coefficient
l=1/ - penetration depth (characteristic absorption length)

## Slide 43: Measures of Absorption
complex refractive index and complex dielectric constant:
optical density – a logarithmic unit:
absorption coefficient and extinction coefficient

## Slide 44: Partially transparent scattering media

## Slide 45: Kubelka - Munk

## Slide 46: Kubelka - Munk

## Slide 47: Scattering
λ~d  Mie Scattering
λ>>d  Rayleigh Scattering
Notes: demostration: laser sapphire and aluminium ceramics

## Slide 48: Effective Medium Approximation
1 - inclusion dielectric constant
0 - matrix medium dielectric constant
eff – effective dielectric constant
1 – volume fraction of inclusions
formula valid only for low concentraitions 1 and small difference between 1 and 0
Maxwell-Garnett Equation