## Slide 2
Introduction
Additive Manufacturing of optical components
Inkjet printing.
Vat-polymerization: DLP, SLA.
Two-photon polymerization.
Volumetric additive manufacturing VAM.
Sequential slow process: 0D, 1D, 2D 3D.
Planar substrate: stepped surfaces, supporting structures.
Shuai Peng et al 2023 Int. J. Extrem. Manuf. 5 035007
VAM suffers from layer-like artifacts: Striations - Self-writing waveguide effect.
Opt. Lett. 47, 1279-1282 (2022)

## Slide 3
Strategies for VAM
Opt. Lett. 47, 1279-1282 (2022)
Flood illumination
Post-processing: silica-embedded polymer
Science 376,308-312(2022).
Int. J. Extrem. Manuf. 5 (2023) 035007
Thin-film of uncured photoresin

## Slide 4
Methods
No index-matching bath
No low etendue.
No software correction for scattering, dose blurring or cylindrical lens effect.
No additional post-processing.
3D ray tracing.
Nat Commun 11, 852 (2020)
8:2 Diurethane dimethacrylate (DUDMA) : poly(ethylene glycol) Diacrylate (PEGDA-700) + Ethyl (2,4,6-trimethylbenzoyl) phenylphosphinate (TPO-L).
About 1 min to print.
Telecentric lens f/#=4.64, etendue =
Pixel size at the focal plane same as pixel size of DMD: 10.8 µm

## Slide 5
Tomographic Projection Calculation
Short depth of field: Dose delivered ≠ Target Dimensional errors
Correction using 3D ray tracing 3DRT:
Pixel at projector
Coordinates at print volume
Tomographic projection of the target
Compute light dose delivered
Compare
Modify
19 rays per pixel
20 iterations
Results
Evaluation of Printed Lens Imaging Performance
Target: Plano-convex lens THORLABS: 3.1 mm radius of curvature, 1.5 mm center thickness, 3 mm diameter. N-BK7
 | Glass lens | VAM printed
Michelson contrast (G 4) | 0.51–0.21 | 0.48–0.16
Smallest element | G 5, E 6, 8.77 µm | G 5, E 5, 9.84 µm
Laser spot size | 7.0 ± 0.4 µm | 14.0 ± 0.4 µm
1 min in isopropanol + 20 min in isopropanol + air dry + Flood exposure in vacuum (405 nm) 5 min.
Post-processing

## Slide 6
Results
Evaluation of Printed Lens Imaging Performance
 | Glass lens | VAM printed
Radius of curvature | 3.1 mm | 2.94 ± 0.01 mm
Deviation from curve | 0.95 µm - 3λ/2 | 2 µm – 3.1 λ
Refractive index | 1.515 | 1.5051
RMS surface roughness |  | 0.53 nm 10x10 µm2
Diameter | 3.00 mm | 2.81 mm
Elimination of Striations and Printing of Microlens Arrays
3x3 biconvex microlens array (MLA). each lenslet has a spherical surface with a radius of curvature of 1 mm (effective focal length D 1.57 mm) and fills a 1 mm x 1 mm square aperture.

## Slide 7
Results
Optical fiber overprinting
Ball lens (diameter 3mm)is printed with a supporting structure to enable overprinting to the optical fiber (PMMA, diameter D 0.5 mm, NA D 0.23).
Reduction in beam divergence (5.4 deg versus 13.5 deg for the fiber).
Ball lens diameter 2.73 mm instead of 3 mm.
Fiber to lens separation 1.00 mm instead of 0.84 mm.
Intensity variations due to poor cleavage of the fiber end.
Differential Interference Contrast Measurement of the Disk
From simulation of dose contrast, the spatial resolution limit is 172.8 µm.