## Slide 1
Question 1:
You are studying how cancer cells adhere to a nanostructured titanium implant surface. You have access to:
AFM (contact, tapping, force spectroscopy)
STM (Scanning Tunneling Microscopy)
FluidFM (hollow AFM cantilever with pressure control)
Which technique(s) would you choose for each goal and why? a) Visualize roughness b) Measure cell–surface adhesion forces c) Inject dye inside a cell
Explain why STM is not suitable for this biological sample.
Explain the difference between AFM contact mode and non-contact mode, and which is better for imaging soft biological samples.
What information does force–distance curve give in AFM? Name two parameters.
Question 2:
You functionalize a SiO₂ surface with a hydrated polymer brush to reduce protein fouling. You monitor deposition using QCM-D and ellipsometry simultaneously. You observe:
QCM-D: large decrease in frequency + large dissipation → soft, hydrated layer
Ellipsometry: thickness = 12 nm (dry thickness)
Adding protein solution gives small additional mass in QCM-D, but no change in ellipsometric thickness
Why does QCM-D detect more mass than ellipsometry?
Why does the hydrated polymer give a large dissipation?
Why might proteins show strong QCM-D signal but no ellipsometry signal?
Propose one application where combining QCM-D + ellipsometry is powerful.
Given a frequency change of –20 Hz, calculate the wet thickness using the Sauerbrey equation and compare it to the 12 nm ellipsometric thickness.
Question 3:
You immobilize a receptor on a gold SPR chip to study binding of a new therapeutic protein.You observe:
SPR: real-time binding curves; equilibrium constant measurable
OWLS: similar binding curves but lower signal noise
Ellipsometry: only thickness change, no kinetic resolution
Why do SPR and OWLS give real-time binding curves but ellipsometry does not?
Why does SPR only work on gold while ellipsometry and OWLS work on many substrates?
Compare what physical property each technique measures (refractive index, mass, angle shift…).
Which technique would you choose to measure: a) kinetics (k_on / k_off) b) absolute thickness c) adsorption in a highly hydrated, soft film d) binding on an insulating substrate (e.g., glass)

## Slide 2: Question 1
Q1 — Which technique for which goal?
Image roughness: AFM (tapping mode)
Measure cell adhesion forces: AFM force spectroscopy
Inject dye to one cell: FluidFM (hollow cantilever)
Q2 — Why STM is not suitable?
Needs conductive, very clean, very rigid surfaces
Biology is soft + in liquid → STM cannot work
Q3 — Contact vs non-contact AFM
Contact: tip touches sample, good resolution but damages soft samples
Non-contact/tapping: gentler, better for cells
Q4 — Force–distance curve gives:
Adhesion force, stiffness, snap-in

## Slide 3: Question 2
Q1 — Why does QCM-D measure more mass?
Detects wet mass (polymer + trapped water)
Ellipsometry measures dry thickness only
Q2 — Why large dissipation?
Polymer brush is soft, hydrated, moves with liquid
Q3 — Why proteins visible in QCM-D only?
Proteins enter the wet polymer layer → increase mass
Do not thicken the dry layer → ellipsometry unchanged
Q4 — Application of QCM + ellipsometry?
Studying polymer hydration
Antifouling coatings
Protein adsorption in real time
Q5
Sauerbrey constant: 17.7 ng/cm²/Hz Density ≈ 1 g/cm³
Mass per area: Δm = 20 Hz × 17.7 ng/cm² = 354 ng/cm²
Convert to thickness: Thickness = mass/density = 354 ng/cm² = 3.54 nm (wet thickness)
QCM-D wet thickness ≈ 3.5 nm
Ellipsometry dry thickness = 12 nm
This is exactly what is expected:
QCM-D measures the wet dynamic layer, not the total dry polymer height
Ellipsometry measures only the dry polymer height (12 nm)
→ This contrast is why combining both techniques is powerful.

## Slide 4: Question 3
Q1 — Why SPR & OWLS show real-time binding?
SPR and OWLS measure resonant optical conditions. When proteins bind, they change the local refractive index, which causes the resonant angle/mode to shift continuously in real time.
These resonant methods have fast time resolution (~10–100 Hz). → They track binding as it happens.
Ellipsometry does NOT measure a resonance. It measures the change in polarization (Ψ, Δ) after reflection. To extract thickness or refractive index, you must:
  record polarization change
  fit it through an optical model
This process makes ellipsometry: slower less sensitive to small dynamic changes not suitable for real-time kinetics
→ Therefore: ellipsometry gives only end-point thickness, not kinetic curves.
Q2 — Why SPR only on gold?
Surface plasmons require gold
OWLS and ellipsometry work on glass, polymers, silica
Q3 — What each technique measures?
SPR: refractive index at gold surface
OWLS: refractive index in waveguide
Ellipsometry: film thickness + optical properties
Q4 — Which technique for what?
Kinetics: SPR or OWLS
Thickness: Ellipsometry
Hydrated films: QCM-D or OWLS
Insulating substrate: OWLS or ellipsometry