## Slide 1
Question 1 – You are tasked with designing a set of quantum dots for multiplexed biological imaging, where each color must be bright, and stable in water.
How would you choose the surface ligand chemistry to fulfill the requirements?
What size range would you target for blue vs. red emission, and why?
How would molecule adsorption and chemical etching effect optical properties of quantum dots?
Question 2 – AuNP-based sensors rely on Localized Surface Plasmon Resonance (LSPR) — the collective oscillation of conduction electrons in a metal nanoparticle when excited by light. When molecules bind to the receptors on the AuNP surface, they form a layer (or cause clustering) that changes the local refractive index (RI) around the nanoparticle.
How would changes in particle aggregation state, or local refractive index affect plasmon resonance?
What experimental conditions could unintentionally shift the color?
Compared to spherical gold nanoparticles (10-80 nm) that always show red color in suspension, why gold nanorod suspension can present different colors from red to purple? What factor determines the color?
Question 3 – Two catalysts are used for CO oxidation: Pt(111) and Au(111). Experimental results show that Pt readily activates O₂ while Au does not. Using MO theory explain:
Why O₂ adsorbs molecularly on Au but dissociatively on Pt
How this leads to differences in CO oxidation rates

## Slide 2
Question 1
Ligands / surface chemistry: exchange native hydrophobic ligands for bifunctional ligands (PEGylated thiols, zwitterionic ligands, or amphiphilic polymers) to make QDs water-soluble and reduce protein adsorption.
Use short PEG or zwitterions for biocompatibility and minimal nonspecific binding.
Encapsulation: silica coating, polymer shells, or lipid/micelle encapsulation can dramatically improve colloidal & chemical stability and reduce leaching.
Size targets
Blue emission (~450 nm): very small cores (~2–3 nm, depending on material); Green (~520 nm): intermediate size (~3–4 nm); Red (~620+ nm): larger cores (~4–6+ nm).
Adsorbed molecule has a refractive index and polarizability that modifies the dielectric environment. This changes exciton binding energy and can shift the emission (generally small red shift as dielectric increases).
Chemical etching can remove atoms from the QD surface → effective size decreases → quantum confinement increases → blue shift (this is irreversible if atoms are lost).

## Slide 3
Q3 - Gold nanorods are anisotropic, so electrons can oscillate Transversely (short axis) → fixed ~520 nm; and Longitudinally (long axis) → strongly geometry-dependent— shifts dramatically with aspect ratio (AR = length/diameter)
In Longitudinal mode, electrons oscillate along the long axis, experiencing less restoring force  lower resonance energy
By tuning the aspect ratio, the resonance energy can be tuned, showing color shift.
Q1 - Aggregation couples plasmons → large red-shift and broadening of extinction peak; color often changes from red to blue/purple; Local refractive index: increasing local RI near particle surface (protein adsorption, binding of analyte with higher RI) → red-shift of LSPR peak.
Question 2
Q2 - pH / ionic strength: high salt screens electrostatic repulsion → aggregation and/or ligand desorption leading to color change; Protein corona: thick protein layers increase effective RI and change stability; sometimes causes small red-shifts and slower kinetics; Temperature: Nearly all liquids decrease in refractive index (RI) as temperature increases. Lower RI → blue-shift of plasmon resonance.

## Slide 4
Basic MO picture of O₂
O₂’s frontier (lowest unoccupied) antibonding orbitals are the π* orbitals (sometimes cartoons simplify to “σ* / antibonding” but the important frontier orbitals for O₂ are π*).
To break the O–O bond you need to populate these π* orbitals (fill antibonding states) so the bond order decreases and the molecule dissociates.
How the metal surface interacts with O₂
A metal surface has a continuum of states (bands). For transition metals the d-band lies near the Fermi level and strongly controls chemisorption.
Two interactions are important:
  Donation from O₂ occupied orbitals into empty metal states (σ → metal).
  Back-donation from filled metal d-states into the empty O₂ π* orbitals.
Pt(111)
Pt has a relatively high d-band center (closer to the Fermi level) and a high density of d-states available for back-donation.
Strong overlap between Pt d-states and O₂ π* → significant back-donation into π*.
Populating π* weakens the O–O bond (reduces bond order) and makes dissociation energetically favorable → dissociative adsorption.
Result: O atoms bound to the surface (high coverage of atomic O under suitable conditions).
Au(111)
Au has a d-band center much lower (further below EF) and a much smaller density of d-states at the Fermi level available for back-donation.
Overlap with O₂ π* is weak → little back-donation, so π* stays largely unpopulated.
O₂ therefore remains largely intact or only weakly chemisorbed (molecular adsorption) with minimal weakening of O–O bond.
Result: O₂ is not efficiently dissociated on extended Au(111) → low activity for reactions that need atomic oxygen.
Question 3

## Slide 5
How this leads to differences in CO oxidation rates
On Pt(111)
O₂ dissociation is facile → abundant surface O atoms.
CO and O meet on the surface and react with relatively low activation energy.
Therefore high CO oxidation rates on Pt under many conditions.
On Au(111)
O₂ remains molecular → atomic O is scarce.
If O₂ cannot easily dissociate, the rate-limiting step is O₂ activation/dissociation (very slow).
Therefore low CO oxidation rate on flat Au(111).
Question 3