## Slide 1
Question 1:
A waxed car windshield causes rain to bead and roll off easily. An anti-fog coating on eyeglasses does the opposite: water spreads evenly into a thin film.
What physical property of the surface is different between the two cases?
Why is the “best” property different for windshields vs. glasses?
Suggest two real-life applications (other than these) where hydrophobic or hydrophilic coatings are useful.
How can engineers/scientists actively change this property in practice? (methods)
If surfactants from rain or cleaning products accumulate on the waxed windshield, what happens to its behavior?
Question 2:
Pure water cannot form stable bubbles. Adding a small amount of soap or detergent suddenly allows large, stable bubbles to form.
At the molecular level, why do surfactants make bubbles possible?
Why do bubbles still eventually collapse, even with surfactants?
Give three examples where surfactants are essential in everyday life or industry.
What happens if surfactant concentration is too high?
Question 3:
When painting a plastic wall, the paint beads up and does not adhere properly. In inkjet printing, ink spreads too much on plain paper, making letters blurry, but prints sharply on photo paper.
How does contact angle influence paint adhesion and ink spreading?
For the plastic wall: what modification would improve paint adhesion?
For photo paper: what modification prevents ink from spreading too much?
Suggest two other industries where controlling wettability is critical.
What general methods exist to increase vs. decrease wettability?

## Slide 2: Question 1
Property: Surface energy → controls wettability and contact angle.
Reason:
  Windshields: hydrophobicity makes droplets bead and roll off, improving visibility.
  Glasses: hydrophilicity prevents droplets, avoids visual distortion.
Examples:
  Hydrophobic: waterproof clothing, smartphone screens, food packaging.
  Hydrophilic: lab slides for microscopy, anti-fog mirrors, microfluidics.
Methods:
  Apply coatings (waxes, fluoropolymers → hydrophobic; surfactant sprays or TiO₂ films → hydrophilic).
  Modify surface chemistry (plasma, UV-ozone → increases hydrophilicity).
  Engineer micro/nanotextures (lotus-like hydrophobic or TiO₂-like hydrophilic).
Effect of surfactants: They lower water’s surface tension → droplets bead less → windshield appears less hydrophobic, performance reduced.

## Slide 3: Question 2
Mechanism: Surfactants reduce surface tension by aligning at the air–water interface (polar head in water, hydrophobic tail in air). This stabilizes the thin water film.
Collapse: Water drains and evaporates from the thin film; eventually the film becomes too thin and ruptures.
Examples:
  Household detergents (cleaning, foaming).
  Food industry (whipped cream, ice cream foams).
  Oil recovery and emulsification.
  Medical: pulmonary surfactants in the lungs reduce alveolar surface tension.
Too high concentration: Micelles form; excess surfactant reduces bubble stability or prevents foaming (“oversaturation” effect).

## Slide 4: Question 3
Influence:
  High contact angle (hydrophobic) → liquid beads, poor adhesion.
  Low contact angle (hydrophilic) → liquid spreads, good adhesion, but risk of excessive spreading.
Plastic wall: Plasma or chemical surface treatment to increase surface energy, reduce contact angle, improve paint wetting.
Photo paper: Apply hydrophobic coating to limit spreading and keep ink dots defined.
Examples:
  Packaging (to make cardboard waterproof).
  Biomedical devices (control of protein/cell adhesion).
  Waterproof textiles (Gore-Tex membranes).
  Microelectronics (photoresist coating).
Methods:
  Increase wettability: plasma treatment, UV-ozone, chemical oxidation.
  Decrease wettability: hydrophobic coatings, silanization, fluoropolymer films, surface texturing.