## Slide 1
Question 1:
You are working for a company that grows synthetic sapphire (Al₂O₃) and diamond for high-value optics and jewelry. You observe that under standard conditions, sapphire crystals are hexagonal prisms, while diamond crystals are octahedral. Recently, a customer asked for flatter diamond plates and elongated sapphire rods for laser optics.
1. Why do diamond and sapphire naturally adopt different crystal habits?
Consider their crystal structures and the surface energies of their main planes.
2. Using the Wulff principle qualitatively, explain what happens to the shape if we can lower the surface energy of one specific plane?
For example, what if the {100} planes of diamond become lower in energy than {111}?
3. In real synthesis, how can scientists or engineers control relative surface energies to tune morphology?
4. Why is understanding crystal planes and morphology important in gemstone or optical applications?
Question 2:
You work in a lab studying NaCl (table salt) crystals used in optical components. Your colleague notices that after long exposure to radiation, the normally transparent crystal becomes light purple. At the same time, when NaCl is heated very close to its melting point, it starts to leak sodium at the surface, and its mechanical strength drops slightly.
1. What kinds of “broken bonds” or point defects could appear in a NaCl crystal? 2. Why do defects appear even when the crystal is not damaged or irradiated?
3. What probably happens at the atomic level when NaCl turns purple after irradiation? 4. Why might heating NaCl close to its melting point make it leak sodium at the surface?
5. Are defects always bad? Give one useful example where point defects improve a material’s performance.
Question 3:
Your company grows large silicon crystals for microelectronics. Perfect single crystals are needed for wafers, but sometimes you observe:
- Slip lines after mechanical stress (1D dislocations).
- Small-angle grain boundaries between slightly misoriented zones (2D).
- Tiny voids inside the crystal after high-temperature annealing (3D).
Engineers must decide which defects can be tolerated and which must be eliminated.
1. Why do these extended defects appear, even when the crystal initially looks perfect? 2. Why might the crystal prefer to create a defect instead of staying “perfect”?
3. Give one example of how extended defects can be useful, and harmful in real materials.
4. If you were an engineer producing these crystals, how might you reduce or control extended defects?

## Slide 2: Question 1
Different habits:
  Diamond has an fcc lattice; its lowest-energy planes are {111} → octahedral shape predicted by the Wulff construction.
  Sapphire (Al₂O₃, hexagonal) has lowest-energy basal (0001) and prismatic {101̅0} planes → hexagonal prisms.
  Each material’s symmetry and bonding determine which planes minimize surface energy.
Changing one plane’s energy:
  If {100} in diamond becomes relatively lower in energy (e.g., by adsorbing hydrogen or oxygen), Wulff shape shifts → cubic or plate-like crystals instead of octahedra.
  The Wulff construction essentially re-weights which faces are expressed based on their γ(hkl).
Controlling surface energies:
  Additives or gases in growth environment selectively adsorb on certain planes (H₂, O₂, surfactants, metal catalysts).
  Temperature and supersaturation change growth rates and stability of different faces.
  Impurities or dopants can pin or stabilize particular surfaces.
  Post-growth etching/polishing can expose or remove selected facets.
Importance in gemstones and optics:
  Optical anisotropy and brilliance depend on crystal facets.
  Mechanical strength and cleavage relate to specific planes.
  Controlled morphology reduces defects and internal stress in optical crystals.
  Understanding the Wulff concept allows engineers to design shapes for function (flat windows, rods, facets) instead of relying only on cutting.

## Slide 3: Question 2
Possible defects:
  Vacancies: missing Na⁺ or Cl⁻ ions → broken bonds.
  Interstitials: extra ions in the lattice.
  Impurities: foreign atoms replacing Na⁺ or Cl⁻ (extrinsic).
  All involve dangling or missing bonds around them.
Why they appear:
  At any temperature, atoms vibrate → occasionally one escapes its site.
  This costs bond energy, but increases disorder → the crystal accepts some defects as part of equilibrium.
Coloration (F-centers):
  Radiation knocks out a Cl⁻, leaving a vacancy that traps an electron.
  The trapped electron absorbs visible light → the crystal appears purple.
  This shows how a simple point defect changes an optical property.
Heating effect:
  At high temperature, ions move more easily → defects become mobile.
  Na⁺ vacancies and Na⁺ interstitials migrate to the surface → loss of sodium and slight weakening of the structure.
Useful defects:
  In semiconductors, dopants create controlled defects that enable conductivity.
  In ionic conductors, vacancies help ions move → batteries, fuel cells.
  In ceramics, defects allow sintering and densification.

## Slide 4: Question 3
Origin:
  High temperature, mechanical stress, or impurity gradients cause local strain.
  To relieve internal stress and minimize total energy, the crystal forms extended defects (dislocations, boundaries, voids).
  Point defects can migrate and cluster → forming dislocation lines or voids.
Energy reason:
  Keeping all bonds “perfect” under strain costs more energy than creating a few dislocations.
  The system sacrifices local perfection to achieve lower total energy — same principle as with surfaces and point defects.
Examples:
  Useful: Dislocations allow metals to deform (ductility); grain boundaries block dislocation motion (strengthening).
  Harmful: Grain boundaries reduce electrical conductivity; voids weaken materials or cause failure.
Control strategies:
  Slow, uniform cooling to reduce thermal stress.
  Annealing to allow defects to reorganize or annihilate.
  Controlled impurity content.