## Slide 1
Question 1:
You are working at an aerospace company analyzing the microstructure of an aluminum alloy. Under the microscope, you see small grains of different orientations separated by grain boundaries. When the alloy is slowly cooled after casting, grains grow larger. When it’s rapidly quenched, grains remain small.
Why do metals form many small grains instead of one perfect single crystal after solidification?
Why does grain growth occur during slow cooling but not after quenching?
Grain boundaries cost energy — so why does the material still form them?
How does grain size influence mechanical properties like strength or ductility?
Give one example of a process where engineers intentionally control grain size, and why.
Question 2:
You work in a materials lab preparing samples for microscopy. Under optical microscopy, you can see grain boundaries after etching. Under scanning electron microscopy (SEM), the contrast between grains is much clearer. Your colleague now proposes to use transmission electron microscopy (TEM) to study the same sample.
What information can you get from optical microscopy vs. SEM vs. TEM about grain boundaries?
Why do we need to etch the surface to see grains optically, but not in SEM or TEM?
What does the electron beam allow us to see that light cannot?
Give one reason why TEM sample preparation is challenging.
In which cases would TEM be necessary rather than optical/SEM?
Question 3:
You work in the semiconductor industry, fabricating microchips that contain thousands of copper interconnects embedded in silicon and silicon oxide layers. During high-temperature processing, engineers observe that atoms diffuse across the Cu/Si interface, sometimes forming brittle compounds that degrade performance.
What type of interface is Cu/Si: homophase or heterophase?
Why is this interface important to the reliability of a microelectronic device?
Why might atoms diffuse across the Cu/Si interface at high temperature?
What problems can arise from this interdiffusion?
How could engineers reduce or control the interdiffusion and stabilize the interface?

## Slide 2: Question 1
Nucleation happens at many sites → many grains form simultaneously → misoriented crystals meet and create grain boundaries.
Slow cooling allows atoms to diffuse → grains coarsen to reduce total boundary area. Quenching freezes structure before boundaries can move.
Boundaries cost energy, but many nuclei form faster → lowers overall free energy of solidification → kinetics wins over surface energy minimization.
Fine grains → more boundaries → block dislocation motion → stronger (Hall–Petch). Coarse grains → fewer boundaries → softer, more ductile.
Examples:
  Grain refinement in aircraft aluminum for strength.
  Large grains in turbine blades for creep resistance.

## Slide 3: Question 2
Optical: grain size and shape at the micron scale. SEM: surface topography, phase contrast, grain boundary grooves. TEM: atomic-scale structure, dislocation networks, crystallographic orientation.
Etching reveals grain boundaries by attacking high-energy regions → visible under optical light. SEM/TEM detect contrast intrinsically via electron interactions.
Electrons have much shorter wavelength than visible light → resolution in nanometers → allows imaging of atomic columns and interfaces.
TEM samples must be <100 nm thick, difficult to prepare without damaging the structure.
TEM is essential to study nanoscale interfaces, precipitates, or misfit dislocations — beyond optical/SEM resolution.

## Slide 4: Question 3
Type of interface:
  It’s a heterophase interface: two different materials (metal + semiconductor).
  There’s a lattice mismatch and different bonding nature (metallic vs covalent).
Importance:
  The Cu/Si interface determines electrical contact quality, resistance, and mechanical stability.
  Poor interface quality → signal loss, short circuits, or delamination.
Diffusion reason:
  At high T, atoms gain mobility → copper diffuses into silicon and reacts → forms Cu–Si compounds (silicides).
  This occurs because the system lowers its total energy by forming a new phase, even though it damages performance.
Problems caused:
  Formation of brittle intermetallics → cracking under thermal stress.
  Changes in electrical properties (increased resistance).
  Contamination of silicon → device failure.
Control methods:
  Introduce a barrier layer (e.g., TaN, TiN) between Cu and Si → reduces diffusion.
  Optimize process temperature and time.
  Engineer the interface structure (smooth, clean surfaces reduce defect-driven diffusion).