## Slide 1
Question 1 - Your group prepared alkanethiol SAMs on gold for biosensing. XPS shows unexpected oxygen peaks and STM images show poor order.
- What possible chemical or physical causes could explain these observations?
- Please verify your hypothesis by using surface characterization technology.
- Suggest procedural modifications to improve SAM quality and reproducibility.
Question 2 – You are functionalizing three different surfaces – gold, SiO2, and Al2O3 – using thiol-based, Silane-based, and carboxylic acid-based SAM.
- Pair the substrate surface and SAM method.
- Compare the bonding mechanism, stability, molecular order, and of three SAMs.
- Choose correct surface characterization techniques to verify successful SAM formation, and monolayer/multilayer formation.
Question 3 – You attempt to deposit a silane monolayer on quartz. However, repeated trials give inconsistent contact angles and XPS signals.
What factors likely cause this variability?
Suggest some surface characterization methods to characterize the silane-SAM.
Propose some modified steps to achieve a more reproducible, homogeneous silane-SAM.

## Slide 2
Question 1
Oxidation of thiols or metal surface → oxygen signal (O1s) and sulfonate or sulfoxide formation.
Adsorbed adventitious contaminants (water, organics) from air or solvent.
Multilayer/physisorbed material (not a single ordered SAM) due to excess concentration or poor rinsing.
Incomplete surface cleaning / gold surface contamination before SAM assembly.
SAM disorder from mobility of thiols
XPS
Look at S 2p region: well-formed Au–S should show S 2p doublet at binding energies characteristic of thiolate (~161–163 eV depending on referencing). Oxidized sulfur appears at higher BE (e.g., 167–170 eV for sulfonates).
O 1s peak ~531–533 eV: check shape and chemical shift. If O1s intensity correlates with C1s peaks consistent with adsorbed organics, contamination is likely. If you see peaks consistent with sulfate/sulfonate, that implies thiol oxidation.
C 1s: strong peak at ~284.8 eV for hydrocarbon chains; shoulder peaks at higher BE may indicate C–O, C=O (contaminants or oxidation).
EDX  confirm if there are larger contaminant patches or residues (e.g., from deposition residues). Lack of signal changes doesn’t rule out SAM issues.
Contact angle  Ordered methyl-terminated SAMs: high static contact angle; Compare before/after cleaning and to a clean Au control.
STM  Look for domain size and registry; small domains / irregular packing indicate disorder.
Clean Au more thoroughly (UV-ozone/ piranha).
Prepare SAM in freshly degassed, dry solvent and under inert atmosphere (N₂/glovebox) to avoid oxidation.
Use fresh thiol solutions at correct concentration and immersion times; rinse thoroughly and sonicate briefly in clean solvent if multilayers suspected.
Use backfilling / annealing protocols to improve ordering (anneal gently if substrate tolerates).
Use longer-chain alkanethiols for greater lateral van der Waals stabilization if mobility is an issue.

## Slide 3
Question 2
Thiol  Au; Silane  SiO2; Carboxylic acid  Al2O3.
Binding mechanism
Covalent chemisorption: Au–S bond
Hydrolysis + condensation → Si–O–Si covalent network with surface
Electrostatic interaction or weak H-bonding (acid–base reaction)
Stability & molecular order: Au-thiol > SiO2-Silane > Carboxylic-Al2O3
Thiol–Au  STM, XPS
Silane–SiO2  XPS, Contact angle, SIMS
Carboxylic–Al₂O₃  XPS, Contact angle, SIMS

## Slide 4
Question 3
Humidity
Surface cleanliness
Excess concentration
Temperature
Contact angle, XPS, SIMS
Thoroughly clean and hydroxylate quartz
Work in a clean, dry, controlled-humidity setup
Use fresh silane
Rinse immediately after deposition
Annealing in dry N2