## Slide 1: Material Science at Large Scale Facilities (MSE-435): Case studies
September 30, 2025

## Slide 2: Case study 1: Thermal fatigue in micro-electronics
Today, device manufacturers face the challenge of designing smart power devices tailored to meet the demanding requirements of emerging automotive applications. These devices need to conduct high power densities at rapid switching frequencies while maintaining a small footprint [1]. The small device dimensions result in elevated junction temperatures during short circuit events with strong current pulses as fast as 200 µs. At these timescales, heat dissipation via the packaging becomes ineffective, and in order to protect Si from thermal runaway, it is common to use ~20 µm thick Cu metallizations to reduce operation temperatures [2]. However, previous investigations [3] have revealed that despite the thick metallizations, the ultra-short pulses can lead to peak temperatures of up to 350°C within the Cu. During the device’s lifetime, multiple heating pulses may induce thermomechanical fatigue of the Cu metallization.
[1] D. Dibra, M. Stecher, S. Decker, A. Lindemann, J. Lutz, C. Kadow, On the Origin of Thermal Runaway in a Trench Power MOSFET, IEEE Trans. Electron Devices 58 (2011) 3477–3484. https://doi.org/10.1109/TED.2011.2160867.
[2] W. Robl, M. Melzl, B. Weidgans, R. Hofmann, M. Stecher, Last Metal Copper Metallization for Power Devices, IEEE Trans. Semicond. Manuf. 21 (2008) 358–362. https://doi.org/10.1109/TSM.2008.2001210.
[3] M. Nelhiebel, R. Illing, Th. Detzel, S. Wöhlert, B. Auer, S. Lanzerstorfer, M. Rogalli, W. Robl, S. Decker, J. Fugger, M. Ladurner, Effective and reliable heat management for power devices exposed to cyclic short overload pulses, Microelectron. Reliab. 53 (2013) 1745–1749. https://doi.org/10.1016/j.microrel.2013.07.123.

## Slide 3: Case study 2: Kevlar yarns
Description | Linear Density (g/1000 m) / nr of Filaments | Breaking Tenacity (mN/tex) | Modulus (GPa) | Elongation at Break (%)
low modulus | 1680 f1000 | 2115 | 60 | 4.16
middle | 1680 f1000 | 2350 | 91 | 3.45
high | 1610 f1000 | 2135 | 105 | 2.7
ballistic | 550 f500 | 2600 | 100 | 3.5
Aramid yarns, often known by one of its trademark name Kevlar, are aromatic polyamids (poly-para-phenylene terephtalamide, PPTA) are high-performance synthetic yarns, which typically show high strength, high modulus and toughness. The multi-filament yarns are used for several applications such as structural reinforcement and bullet-resistant vests. Different mechanical properties can be achieved depending on processing conditions, see table 1 for four different commercial aramid yarns.
In the past, microscopy methods and X-ray techniques have been crucial to determine the presence of a complex fibrillar structure within the aramid fibers [1,2,3]. Studies indicate that the tensile properties of the filaments correlate with structural parameters within the fibers [3], the modulus being related to both micro-distortions (i.e. para-crystalllinity) and structural orientation [2,3]. However more research is needed in terms of nano structure and its role in the materials properties, in particular towards properties such as the toughness which is an important property for ballistic applications. Another research interest is to investigate not only the yarn itself, but composite materials made with such yarns.
​​[1] Rao, Y., Waddon, A. J., & Farris, R. J. (2001). Structure-property relation in poly(p-phenylene terephthalamide) (PPTA) fibers. Polymer, 42(13), 5937–5946. https://doi.org/10.1016/S0032-3861(00)00905-8
[2] Pauw, B. R., Vigild, M. E., Mortensen, K., Andreasen, J. W., Klop, E. A., Breiby, D. W., & Bunk, O. (2010). Strain-induced internal fibrillation in looped aramid filaments. Polymer, 51(20), 4589–4598. https://doi.org/10.1016/j.polymer.2010.07.045
[3] Roenbeck, M. R., Cline, J., Wu, V., Afshari, M., Kellner, S., Martin, P., Londono, J. D., Clinger, L. E., Reichert, D., Lustig, S. R., & Strawhecker, K. E. (2019). Structure–property relationships of aramid fibers via X-ray scattering and atomic force microscopy. Journal of Materials Science, 54(8), 6668–6683. https://doi.org/10.1007/s10853-018-03282-x

## Slide 4: Case study 3: High-density polyethylene (HDPE) under shear flow
High-density polyethylene (HDPE), a thermoplastic polymer, is commonly used in many packaging applications. The production process of choice is typically injection molding, where HDPE is melted at high temperatures and injected into a mold to create the required shape. HDPE is a semi-crystalline polymer which can form different morphologies, such as spherulites, where crystal chains extend radially from nucleation centers, elongated spherulites or shish-kebab microstructure [1]: extended crystal chains (shish) surrounded by folded lamellar crystals (kebab). An increased density of shish-kebab has been correlated with superior mechanical properties [2]. To optimize the process of injection molding in specific applications, it would therefore be interesting to different parameters to further understand these structure-property relationships and their dependence on these parameters [3].
[1] Odell, J. A., Grubb, D. T. & Keller, A. A new route to high modulus polyethylene by lamellar structures nucleated onto fibrous substrates with general implications for crystallization behavior. Polymer 19, 617–626 (1978).
[2] Keller, A., Kolnaar, H. W. H. Flow-induced orientation and structure formation. In Processing of Polymers. Vol. 18 (eds Meijer, H. E. H.) 189–268 (Wiley-VCH, New York, NY, USA, 1997).
[3] Mordal, K., Dobrakowski, K., & Kwiatkowski, D. (2018). Effect of Selected Injection Conditions on the Mechanical Properties and Structure of HDPE. In Fibres and Textiles in Eastern Europe (Vol. 26, Issue 5(131), pp. 93–98). Walter de Gruyter GmbH. https://doi.org/10.5604/01.3001.0012.2538

## Slide 5: Case study 4: Extracellular matrix (ECM)
The extracellular matrix (ECM) is a complex network of macromolecules that provide structural and biochemical support to cells in the body. While it performs vital functions in the body, abnormalities in the ECM have been implicated to play an active or passive role in many pathological conditions, like cancer and fibrosis. The tumour microenvironment (TME) contains diverse ECM components that interact with cancer cells to facilitate tumour growth and metastasis [1]. The changing functional role of ECM in such cases manifests as a change in its structure [1, 2]. Furthermore, there is evidence of higher concentrations of certain elements as well as changes in their chemical forms, in certain cancers [3]. Therefore, a careful investigation into the composition and organization of the TME can help in a broad understanding of evolution of cancer and potentially identify biomarkers in specific cancer types.
[1] Popova, N. V., & Jücker, M. (2022). The Functional Role of Extracellular Matrix Proteins in Cancer. In Cancers (Vol. 14, Issue 1, p. 238). MDPI AG. https://doi.org/10.3390/cancers14010238
[2] Winkler, J., Abisoye-Ogunniyan, A., Metcalf, K. J., & Werb, Z. (2020). Concepts of extracellular matrix remodelling in tumour progression and metastasis. In Nature Communications (Vol. 11, Issue 1). Springer Science and Business Media LLC. https://doi.org/10.1038/s41467-020-18794-x
[3] Sohrabi, M., Nikkhah, M., Sohrabi, M., Rezaee Farimani, A., Mirasgari Shahi, M., Ziaie, H., Shirmardi, S., Kohi, Z., Salehpour, D., Safarnezhad Tameshkel, F., Hajibaba, M., Zamani, F., Ajdarkosh, H., Sohrabi, M., & Gholami, A. (2021). Evaluating tissue levels of the eight trace elements and heavy metals among esophagus and gastric cancer patients: A comparison between cancerous and non-cancerous tissues. In Journal of Trace Elements in Medicine and Biology (Vol. 68, p. 126761). Elsevier BV. https://doi.org/10.1016/j.jtemb.2021.126761

## Slide 6: Case study 5: Low-carbon cement
The cement industry is responsible for 7-8% of global CO2 emissions per year, primarily because clinker production in Portland cement is an extremely energy-intensive process. Low-carbon cement (LCC) presents a sustainable alternative where the clinker content is reduced by using supplementary cementitious materials (SCMs) like fly ash, slag and calcined clay. Despite these obvious benefits, one hindrance is the poorly understood hydration kinetics and the changing nano/microstructure, especially in multicomponent systems. A thorough understanding of the mechanism of hydration and the structural evolution (both spatially and chemically resolved) that determine the properties of the LCC, will be a significant step forward.
[1] Winnefeld, F., Epifania, E., Montagnaro, F., & Gartner, E. M. (2019). Further studies of the hydration of MgO-hydromagnesite blends. In Cement and Concrete Research (Vol. 126, p. 105912). Elsevier BV. https://doi.org/10.1016/j.cemconres.2019.105912

## Slide 7: Case study 6: Iron mining for steel production
Iron is a critical raw material for steel production, and its extraction from ores such as hematite (Fe₂O₃) and magnetite (Fe₃O₄) forms the foundation of global industrial development. The extraction and processing of iron ore are influenced by a variety of factors, including the iron content, mineral composition, and the presence of impurities such as sulfur (S), phosphorus (P), and carbon (C) [1]. Additionally, valuable trace elements like chromium (Cr), nickel (Ni), and copper (Cu) may be present in ores, offering opportunities for secondary revenue streams. Exploring the quality of iron ores (composition as well as structure) using advanced large-scale facilities could offer valuable insights into their viability for industrial use.
[1] Park, J., Kim, E., Suh, I., & Lee, J. (2021). A Short Review of the Effect of Iron Ore Selection on Mineral Phases of Iron Ore Sinter. In Minerals (Vol. 12, Issue 1, p. 35). MDPI AG. https://doi.org/10.3390/min12010035

## Slide 8: Case Study 7: Hip-implants: considerations for long term success
Total hip arthroplasty is a surgical procedure to replace the damaged part of the hip with an artificial analogue. The hip joint is a ball-and-socket joint, for its replacement exist different combinations of materials for the head, cup and steam. Commonly used materials are CoCrMo-Alumina, Ti6Al4V-Alumina, and CoCrMo-Ti6Al4V for the stem/head interface. Several studies have raised awareness for the problem of wear debris formation in the stem and head interface, such as inflammatory reaction in the tissues, necrosis or osteolysis. However, limited studies have been done so for predicting wear in the stem and head interface [1].
Further investigating the structural properties of the hip implant material interface during different stages of wear- and surface-fatigue could shed light onto the importance of different damage mechanisms and the relationship to the material nano- and microstructure [2]. In addition to the implant material itself, the osseointegration of the implant into the structure of the surrounding bone is an important factor for implant stability [3], meaning that the structures of the bone on multiple scales [4] need to adapt to the new surrounding to distribute the changes in stress and strain during loading.
[1] Manish Belwanshi, Pratesh Jayaswal, Amit Aherwar. Wear and fatigue behaviour investigation of hip implant head-stem interface using finite element analysis,
Materials Today: Proceedings. Volume 56, Part 5, 2022, https://doi.org/10.1016/j.matpr.2021.10.188.
[2] Wear- and Surface-Fatigue-Mediated Damage during Fretting in a High-Strength Titanium Alloy. Yanlin Tong, Ke Hua, Fan Zhang, Qing Zhou, Hongxing Wu, and Haifeng Wang. ACS Applied Engineering Materials 2023 1 (1), 200-213 https://doi.org/10.1021/acsaenm.2c00042
[3] Apostu D, Lucaciu O, Berce C, Lucaciu D, Cosma D. Current methods of preventing aseptic loosening and improving osseointegration of titanium implants in cementless total hip arthroplasty: a review. Journal of International Medical Research. 2017;46(6):2104-2119. doi:10.1177/0300060517732697
[4] Georgiadis, M., Guizar-Sicairos, M., Zwahlen, A., Trüssel, A. J., Bunk, O., Müller, R., & Schneider, P. (2015). 3D scanning SAXS: A novel method for the assessment of bone ultrastructure orientation. Bone, 71, 42–52. https://doi.org/10.1016/j.bone.2014.10.002

## Slide 9: Case study 8: Controlled anisotropy in extrusion 3D printing
3D printing, has become significantly more commonplace in tissue engineering over the past decade, as a variety of new printing materials have been developed. In extrusion-based printing, materials are used for applications that range from cell free printing to cell-laden bioinks that mimic natural tissues [1]. A widespread characteristic of natural tissues is its structural anisotropy originating from components that exhibit a well-defined organization of cells and extracellular matrix [2].
Apart from its occurrence in biological tissues, anisotropy is often desired in an engineering context, as it affects electrical and thermal conductivity, optical properties, mechanical performance, or magnetic properties. In 3D printing, anisotropy can be introduced by the shear and extensional forces during extrusion which can reach relatively high alignment. However, alignment using shear is limited to the printing direction and the shear forces created are limited by the nozzle diameter and flow rate in it. As an alternative, extrusion-based 3D printing of lyotropic liquid crystals is a promising technique to produce well-defined anisotropic structure. As the printing of larger objects requires a significant amount of time, changes in the environmental conditions can lead to small changes in structure, potentially altering the material performance. Therefore, deeper knowledge to understand this defects during and directly after printing would bed highly desirable [3].
[1] J. K. Placone, A. J. Engler, Recent Advances in Extrusion-Based 3D Printing for Biomedical Applications. Adv. Healthcare Mater. 2018, 7, 1701161. https://doi.org/10.1002/adhm.201701161
[2] Mostert, D., van der Putten, C., Sahlgren, C.M. et al. Bioengineering structural anisotropy in living tissues. Nat Rev Bioeng 3, 727–741 (2025). https://doi.org/10.1038/s44222-025-00338-x
[3] Rodriguez-Palomo, A., Lutz-Bueno, V., Guizar-Sicairos, M., Kádár, R., Andersson, M., & Liebi, M. (2021). Nanostructure and anisotropy of 3D printed lyotropic liquid crystals studied by scattering and birefringence imaging. Additive Manufacturing, 47, 102289. https://doi.org/https://doi.org/10.1016/j.addma.2021.102289

## Slide 10: Case study 9: Local magnetization in iron oxide nanoparticles
Magnetic iron oxide nanoparticles offer unique potential for various technological, biomedical, or environmental applications thanks to the size-, shape- and material-dependent tunability of their magnetic properties. To optimize particles for a specific application, it is crucial to understand the relationship between their structural and magnetic properties [1].
The commonly accepted macrospin model including surface spin is sufficient to explain a large fraction of macroscopic phenomena [2]. But yet a certain degree of magnetic disorder is probably present in the particle core. It was found that the lower-than-expected macroscopic magnetization in nanoparticles results not only from surface spin effects, but also from reduced magnetization inside the uniformly magnetized core as compared to the bulk material [3]. This amount of spin disorder found in the nanoparticle interior is significant [2].
Combined, these findings illustrate that for a comprehensive understanding of the macroscopic performance of magnetic nanoparticles, it is indispensable to consider both structural and spin disorder on a variety of length scales and especially to develop a better understanding of the core region [2].
[1] Using small-angle scattering to guide functional magnetic nanoparticle design. D. Honecker, M. Bersweiler, S. Erokhin, D. Berkov, K. Chesnel, D. A. Venero, A. Qdemat, S. Disch, J. K. Jochum, A. Michels and P. Bender, Nanoscale Adv., 2022, 4 , 1026 —1059 DOI https://doi.org/10.1039/D1NA00482D
[2] A. Lak, S. Disch, P. Bender, Embracing Defects and Disorder in Magnetic Nanoparticles. Adv. Sci. 2021, 8, 2002682. https://doi.org/10.1002/advs.202002682
[3] Disch, S. et al. Quantitative spatial magnetization distribution in iron oxide nanocubes and nanospheres by polarized small-angle neutron scattering. New J. Phys. 14, 13025 (2012). DOI 10.1088/1367-2630/14/1/013025

## Slide 11: Case study 10: Nanocellulose/metal-organic frameworks composites
Nanocellulose (NC) is widely utilized in various fields due to its high surface area, excellent mechanical strength, and environmental friendliness [1], but it has a low electric conductivity. Metal-organic frameworks (MOFs) are an appealing upgrade because they posses in addition good electrical conductivity, highly flexible pore size, changeable surface chemistry, and good chemical and thermal strength [2].
Traditional synthesis methods include solvothermal and non-solvothermal methods. The solvothermal method involves carrying out reactions at temperatures above the solvent's boiling point in sealed chemical reactors under high pressure created by solvent vapor or a pump. Common MOFs synthesized using this method include UiO-67, ZIF-9, MIL-74, and others [2].
Although researchers have invested a great deal of effort in studying a variety of NC/MOF composites, the fine structure of these materials remains difficult to control due to a limited understanding of the precise mechanisms of the transformation process. Therefore, there is still a need to study the fine structure of a series of these composites, resulting from different reaction conditions, in order to deduce further information about the formation mechanisms of NC/MOF [2].
[1] Thomas, B. et al. Nanocellulose, a Versatile Green Platform: From Biosources to Materials and Their Applications. Chem. Rev. 118, 11575–11625 (2018). https://doi.org/10.1021/acs.chemrev.7b00627
[2] Qi, J. et al. Nanocellulose/metal-organic frameworks composites for advanced energy storage of electrodes and separators. Chem. Eng. J. 500, 157318 (2024). https://doi.org/10.1016/j.cej.2024.157318

## Slide 12: Case study 11: Calcium carbonate mineralization
Calcium carbonate (CaCO3) is used by a large variety of marine organisms, corals and mollusks as examples, as structural material for their exo- and endoskeletons [1]. The anhydrous crystalline calcium carbonate (CaCO3) polymorphs, which form under ambient conditions, are calcite, aragonite, and vaterite. Their crystallization in both abiotic and biotic systems is often preceded by the formation and subsequent transformation of amorphous calcium carbonate (ACC). Many biomineralizing organisms utilize the ACC pathway to precisely control the particle shape and crystalline polymorph during the formation of their shells or spines etc. For example, sea urchin larvae produce highly elongated single crystals of calcite by the controlled deposition and transformation of ACC within a biological membrane. Such natural biological processes can be used to manipulate the shape and size of synthetic calcium carbonate particles [2].
There are still many open questions about the structure on the micro and nano scale for specific organisms and for the understanding of the relevant biosynthesis pathways that form them. Every new answer obtained has the potential to aid the development of biomimetic structures that can replicate some of the marvelous features of its natural analogues [3].
[1] Bach, L. T.: Reconsidering the role of carbonate ion concentration in calcification by marine organisms, Biogeosciences, 12, 4939–4951, https://doi.org/10.5194/bg-12-4939-2015, 2015.
[2] Bots, P., Benning, L. G., Rodriguez-Blanco, J.-D., Roncal-Herrero, T., & Shaw, S. (2012). Mechanistic Insights into the Crystallization of Amorphous Calcium Carbonate (ACC). Crystal Growth & Design, 12(7), 3806–3814. https://doi.org/10.1021/cg300676b
[3] Wang, Y., Liu, Z., Pan, H., & Tang, R. (2023). Biomineralization inspired crystal growth for biomimetic materials preparation. Journal of Crystal Growth, 603, 127029. https://doi.org/https://doi.org/10.1016/j.jcrysgro.2022.127029

## Slide 13: Case study 12: Structure of the heart and pathologies
The mechanical performance of the heart is astonishing, doing an uninterrupted period of work during our whole lives. This feat is based on the special micro and nanostructure of the heart tissue. On the microscale, individual cells and their surrounding extracellular matrix (ECM) exhibit dynamic reciprocity, with mechanical feedback moving bidirectionally. On the nanometer scale, molecular features of cells and the ECM show remarkable sensitivity to mechanical cues. Given the inherent challenges in observing, quantifying, and reconstituting this nanoscale environment, it is not surprising that this landscape has been understudied compared to larger length scales [1]. Therefore, by in-depth analysis of healthy and diseased hearts on these small length scales, valuable insights can be gained about the normal function and about disease progression.
Cardiomyopathy, as an example of a heart disease, is an anatomic and pathologic diagnosis associated with muscle or electrical dysfunction of the heart, that manifest with both structural and functional alterations, usually in the form of ventricular hypertrophy or dilatation [2]. Cardiomyopathies represent a heterogeneous group of diseases that often lead to progressive heart failure with significant morbidity and mortality [3].
[1] Singh, J.P., Young, J.L. The cardiac nanoenvironment: form and function at the nanoscale. Biophys Rev 13, 625–636 (2021). https://doi.org/10.1007/s12551-021-00834-5
[2] Skreb, N., Loncaric, F., Li, K.Y.C. et al. Synchrotron-based X-ray 3D phase contrast imaging and analysis of transmural myocardial tissue from heart failure patients. Sci Rep 15, 25867 (2025). https://doi.org/10.1038/s41598-025-04012-5
[3] Wexler RK, Elton T, Pleister A, Feldman D. Cardiomyopathy: an overview. Am Fam Physician. 2009 May 1;79(9):778-84. PMID: 20141097; PMCID: PMC2999879.

## Slide 14: Case study 13: Assembly of molecular catalysts onto carbon nanotubes
In the last decades, nanosized and nanostructured materials gained relevance in the catalysis field due to their large surface to volume ratio as well as the possibility to offer reactive sites with complex chemical composition. In addition, the dimensions and geometry of these catalysts are critical to their performance. For this purpose, a vast analysis using complementary techniques is strongly recommended [1].
A particular class of nanostructured materials, multiwalled carbon nanotubes (MWNT), providing a well-adapted platform for supporting catalyst adsorption. One area where their properties are becoming important is electrocatalysis which is becoming a key enabling technology for renewable energy production, but the anticipated shortage of an increasing number of critical elements, especially metals like platin, has triggered a shift towards molecularly-defined materials with lower metal loadings but enhanced performance [2].
Such molecular catalysts show powerful catalytic efficiency and unsurpassed selectivity in many reactions of interest. As their implementation in electrocatalytic devices requires their immobilization onto a conductive support, controlling the grafting chemistry and its impact on their distribution at the surface is highly important [2]. For the development of novel applications that use different molecular catalysts, this control of the grafting chemistry requires appropriate information about the structure of the catalyst distribution on the surface, ideally in a wet environment.
[1] Herrera, F., Rumi, G., Steinberg, P. Y., Wolosiuk, A., & Angelomé, P. C. (2023). Small Angle Scattering Techniques for the Study of Catalysts and Catalytic Processes. ChemCatChem, 15(17), e202300490. https://doi.org/https://doi.org/10.1002/cctc.202300490.
[2] Ghedjatti, A., Coutard, N., Calvillo, L., Granozzi, G., Reuillard, B., Artero, V., Guetaz, L., Lyonnard, S., Okuno, H., & Chenevier, P. (2021). How do H2 oxidation molecular catalysts assemble onto carbon nanotube electrodes? A crosstalk between electrochemical and multi-physical characterization techniques. Chem. Sci., 12(48), 15916–15927. https://doi.org/10.1039/D1SC05168G

## Slide 15: For any questions:
Contact: dominique.windisch@epfl.ch