Problems. #3– Semiconductor devices II – Spring 2023 (Ionescu)

Problem 1: Tunnel FET as Steep Slope Switch basics

The Tunnel FET is a gated p-i-n diode device operating in reversed bias regime and exploiting quantum-mechanical band-to-band tunneling. Select the correct properties of this steep slope device:

- Dennard scaling rules applies to both MOSFETs and Tunnel FETs.

- A Tunnel FET with InAs source and same geometry and dimensions as an all-silicon Tunnel FET has a higher Ion current.

- An optimized Tunnel FET (high Ion and low Ioff) should be asymmetrical from the point of drain and source materials because an identical band-gap at source and drain can never optimize both Ion and Ioff.

- The temperature dependence trend of subthreshold characteristics of Tunnel FET is very similar to the one of MOSFETs made of same semiconductor material; the subthreshold slope degrades with the temperature increase.

- The quantum- mechanical tunneling effec exploited Tunnel FETs involves probability calculations for electrons to tunnel through a thin energy barrier.

- Carrier mobility plays a key role in the transport characteristics of Tunnel FETs. Therefore materials with higher carrier mobility like III-V and Ge are suitable for these devices.

- The effect of dimension (gate length, for instance) variability is expected to be quasi-identical on the Id-Vg and Id-Vd characteristics of Tunnel FETs and MOSFETs (consider how these characteristics change when the channel length is divided by a factor of x2, for instance).

- The Electron-Hole Bilayer Tunnel FET is a Density of States switch that can achieve a steeper transition between off and on than a conventional Tunnel FET because the gate-controlled electrostatic field and the tunneling paths are aligned.

- Tunnel FET exploits a discrete charge conduction principle (electrons tunnel one by one from the conduction to the valence band).

- Tunnel FET can be scaled more aggressively that MOSFET because they have no short channel effects.

Problem 2: Trap-assisted tunneling effect, digital, analog, sensor and other applications of Tunnel FETs.

Select the correct statements about the Tunnel FETs from the list below:

- Trap-Assisted Tunneling (TAT) is a phenomenon that depends on the density of electrically-active traps at both the oxide-to-channel interface and at the tunneling junctions. These densities of traps should be lower than 1012 eV-1cm-2 to have a good tunnel FET.

- Trap-Assisted Tunneling (TAT) is a phenomenon that does not depends on temperature but only on the energy levels of traps.

- Trap-Assisted Tunneling (TAT) is cancelled when the temperature is increasing.

- The steep-slope of Tunnel FETs is normally steeper at higher levels of currents.

- At low voltage and low current levels Tunnel FETs can offer higher analog amplification than CMOS. Support your answer with an approximate calculation of gm/Id limit at 300K in MOSFETs and compare it with what a Tunnel FET with a slope of 10mV/decade at 300K can achieve as gm/Id.

- Tunnel FET can be used to design more energy efficient hybrid CMOS-TFET multi-core processor architecture. The computing tasks assigned to Tunnel FETs are the ones requiring high-performance (HP) specifications.

- Leakage, Ioff, current of Tunnel FETs decreases at cryogenic (sub-77K) temperatures.

- A charge sensor exploiting a tunnel FET operated in the sub-Vth region of Id-VG characteristics would offer a better current sensitivity to an elementary charge variation on the device gate.

- Tunnel FET otput characteristics do saturate by pinch-off, like in MOSFETs. In case you disagree with this statement, what do you think is the saturation mechanisms of Id-Vd of tunnel FETs.

- Tunnel FETs cannot be used for cryogenic applications, such as quantum computing since they are not stable at lower temperatures.

Problem 3:

At the end of problems/questions #1 and #2:

- Enumerate five (5) major advantages of tunnel FETs compared to MOSFETs.

- Enumerate five (5) major disadvantages of tunnel FETs compared to MOSFETs