## Slide 1
MICRO-722: 3D Printing with light
Paper Presentation-Temporal focusing in 2PP
06.03.2023
Buse Ünlü

## Slide 2
MICRO-722: 3D Printing with light
Article

## Slide 3
MICRO-722: 3D Printing with light
Continuous, layer-by-layer projection two-photon lithography system
Patterning rates up to 4 kHz
100X, NA 1.49
800 nm laser
22 nm bandwidth, 5 kHz repetition rate
Desired angular dispersion
(separate-colored beams )
Adjacently fabricated metamateriallike 3D unit cell
Vertical stage speed of 100 μm s−1
-Schematic of spatiotemporal printing system-
laser pulse stretched in time

## Slide 4
MICRO-722: 3D Printing with light
Numerical model for spatiotemporal focusing
- Confining the patterned light sheet to a thin region for controlled print layer thickness
- Monochromatic coherent Fourier optics with paraxial approximations
Phase term used to represent the DMD dispersion (1D grating effect);
Phase term of pulse front tilt (diffracting off the DMD);
-Incident angle of the laser (to achieve a blazed diffraction order)
 3.65 fs μm−1 delay across the pulse area

## Slide 5
MICRO-722: 3D Printing with light
Numerical model for spatiotemporal focusing
-1.52×2.28 mm2 rectangular pattern
Print thin 2D planes on the scale of single micrometer thickness
Time domain pulse profile

## Slide 6
MICRO-722: 3D Printing with light
3D Printed Structures
-Using continuous, layer-by-layer projection two-photon lithography system
100 μm s−1 stage speed along the vertical (z) direction, 120-144 W cm−2 laser intensity.
Hemisphere (< 120 ms)
1 mm2 area in 6.2 min.
Chicago’s Cloud Gate sculpture
Curved surfaces
Complex, curved features
Aspherical geometries
Sharper features with a square cross-section
Complex trefoil knot
within 319 ms

## Slide 7
MICRO-722: 3D Printing with light
Scalability and large volume printing
Rapid 3D printing of macroscale metamaterial-like structures
Straight and curved components in all 3 dimensions, close separations along the z direction
15 × 15 × 15 unit
Vertical stage speed: 400 μm s−1
Stage translation speed between units: 1 mm s-1
Laser intensity: 216-312 W cm−2
42 × 42 × 42 unit
Printing speed: 1 mm s−1
Printing speed: 400 m s−1

## Slide 8
MICRO-722: 3D Printing with light
Voxel Printing Rate
Vertical stage speed: 1 mm s-1
Pattern exposure time for each layer: 500 µs
Linewidth = 380 nm
Line height = 2470 nm
Woodpile structure
1425 nm voxel size
~0.28 µm3
Voxel print rate
= 3.2 × 106 voxels s−1
Vincent Hahn et al. Adv. Funct. Mater. 2020, 30, 1907795
2PP: Two-Photon Printing
EBID: Electron-Beam-Induced Deposition
SLS: Selective Laser Sintering
EHDP: Electrohydrodynamic (redox) Printing
DIW: Direct Ink Writing
FFF: Fused Filament Fabrication
IJ: Inkjet 3D Printing
(P)SL: (Projection Microstereolithography
CLIP: Continuos Liquid Interphase Printing
CAL: Computed Axial Lithography
16 × 16-pixel unit on the DMD  printed voxel as a result of the 16 pixel wide patterns in the woodpile

## Slide 9
MICRO-722: 3D Printing with light
Structuring potential of projection two-photon lithography
Tuning structure characteristics using grayscale projection
Micropillars
Grayscale values
Lower grayscale values  Less crosslinking of the photoresist  Larger amount of shrinkage
Nonuniform shrinkage  Residual stresses  A curvature of the pillars

## Slide 10
MICRO-722: 3D Printing with light
Summary & Discussion
A continuous, layer-by-layer projection 2PL system for high-speed fabrication of polymer 3D structures with micron and submicron scale features.
Complex 3D geometries including smooth, curved surfaces - in a continuous fashion on the millisecond timescale
Numerical model
    Dispersion effects from the DMD
    Pulsefront tilt imparted on the laser pulse
Rapid (1.08 × 10−3 mm3 s−1) 3D printing of a metamaterial-like structure of millimetre-scale
    Capable of printing arbitrary 3D structures

## Slide 11
THANK YOU FOR YOUR ATTENTION!
Any Questions?

## Slide 12
MICRO-722: 3D Printing with light

## Slide 13
MICRO-722: 3D Printing with light
Papagiakoumou, E. et al, Nat Methods 17, 571–581 (2020).
So, Peter T. C. et al. Multiphoton Microscopy and Fluorescence Lifetime Imaging: Applications in Biology and Medicine, edited by Karsten König, Berlin, Boston: De Gruyter, 2018, pp. 103-140.