## Slide 1
6 - Introduction to electrochemical syntheses

## Slide 2
Brief history of electrochemical deposition:
1780’s: Galvani: birth of electrochemistry
1799: Volta invented the first voltaic pile
1802: Brugnatelli performed the first metal electroplating
1834: Faraday law on the charge and matter quantities
1897: J. J. Thomson discovers the electron
1905: Tafel equation:
1911: Rutherford-Bohr model of the atom
1930: Butler-Volmer model:
1935 – 1965: Eyring: modern theory of electrochemical activation energy
Burton-Cabrera-Frank model of real surfaces (surface defects)
1954: Lorenz: surface diffusion of adions (adsorbed ions)
1958: Bockris: surface site-dependent charge transfer
1965: Dickson: microscopic study of nucleation and growth
1970-1980: Hills: nucleation and growth models (Prog./Inst. – 2D/3D)

## Slide 3
An important tool to process materials at the atomic scale:
Surface treatments
Separation and purification
Chemical synthesis
Additive manufacturing
Substrative manufacturing
Analyses (electrolytes and electrodes)
Electrochemical techniques can be classified as:
Substractive processes
Conversion processes
Additive processes
Analytical methods

## Slide 4
Substractive processes
Electrolytic dissolution
EC-induced dissolution
A Faradaic current converts solid compounds from an electrode surface into solvated species.
Typically anodic / oxidation:
Rarely cathodic / reduction:

## Slide 5
Substractive processes
Electrolytic dissolution
EC-induced dissolution
A Faradaic current converts solid compounds from an electrode surface into solvated species.
Typically anodic / oxidation:
Applications: Electropolishing, electrochemical machining, electroleaching, dealloying, surface cleaning/activation
Electropolishing

## Slide 6
Substractive processes
Electrolytic dissolution
EC-induced dissolution
A Faradaic current converts solid compounds from an electrode surface into solvated species.
Typically anodic / oxidation:
Applications: Electropolishing, electrochemical machining, electroleaching, dealloying, surface cleaning/activation
Electrochemical machining

## Slide 7
Substractive processes
Electrolytic dissolution
EC-induced dissolution
A Faradaic current converts solid compounds from an electrode surface into solvated species.
Typically anodic / oxidation:
Applications: Electropolishing, electrochemical machining, electroleaching, dealloying, surface cleaning/activation
Electroleaching

## Slide 8
Substractive processes
Electrolytic dissolution
EC-induced dissolution
A Faradaic current converts solid compounds from an electrode surface into solvated species.
Typically anodic / oxidation:
Applications: Electropolishing, electrochemical machining, electroleaching, dealloying, surface cleaning/activation
Dealloying

## Slide 9
Substractive processes
Electrolytic dissolution
EC-induced dissolution
A Faradaic current converts solid compounds from an electrode surface into solvated species.
Typically anodic / oxidation:
Applications: Electropolishing, electrochemical machining, electroleaching, dealloying, surface cleaning/activation
Cleaning and activation of surfaces
Red/Ox of contaminants
Surface restructuring

## Slide 10
Substractive processes
Electrolytic dissolution
EC-induced dissolution
Electrochemical reactions induce local changes of chemical conditions leading to the dissolution of solid species.
Electrochemical etching of silicon
e.g., H2O2 reduction on silver particles
Applications: Silicon microcomponents and surface nanostructuring,
surface cleaning

## Slide 11
Substractive processes
Electrolytic dissolution
EC-induced dissolution
Electrochemical reactions induce local changes of chemical conditions leading to the dissolution of solid species.
Applications: Silicon microcomponents and surface nanostructuring,
surface cleaning
Cleaning and activation of surfaces
desorption
adsorption
Desorption
Reactive radicals

## Slide 12
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Growth of an oxide layer onto a metal electrode by anodic oxidation.
Applications: Protective coatings, nanoporous oxides, decorative, tribology, nanostructures
Highly ordered nanopore arrays
Anodisation of aluminum
Other examples
Anodic coatings

## Slide 13
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Electrosynthesis of NaOH
Chemical transformation where electrodes are used to assist electron transfer reactions.
Anodic, cathodic, EC & C coupled reactions
Applications: Synthesis of added-value products (acids & bases, energy vectors, organics)

## Slide 14
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Bioelectrolysis cells
Chemical transformation where electrodes are used to assist electron transfer reactions.
Anodic, cathodic, EC & C coupled reactions
Applications: Synthesis of added-value products (acids & bases, energy vectors, organics)

## Slide 15
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Organic electrochemistry
Chemical transformation where electrodes are used to assist electron transfer reactions.
Anodic, cathodic, EC & C coupled reactions
Applications: Synthesis of added-value products (acids & bases, energy vectors, organics)

## Slide 16
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Photoelectrochemical redox flow battery
Conversion of chemical potential into electrical energy and vice versa.
Anodic + cathodic, photons, phonons
Applications: Batteries, fuel cells, redox flow, light and heat harvesting, synthetic fuels

## Slide 17
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Thermoelectrochemical cells
Conversion of chemical potential into electrical energy and vice versa.
Anodic + cathodic, photons, phonons
Applications: Batteries, fuel cells, redox flow, light and heat harvesting, synthetic fuels

## Slide 18
Conversion processes
Anodisation
Electrosynthesis
Energy conversion and storage
Ion transfer
Intercalation and extraction of ions.
Separation membrane
Electrochemical transfer junction
Applications: deionization, ion separation, waste treatment and recycling

## Slide 19
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
A Faradaic current converts solvated ions (e- acceptor) into a solid deposit onto an electrode surface (e- donor).
Typically cathodic / reduction:
Rarely anodic / oxidation (e.g., selenium, tellurium, polyaniline, polypyrrole)
Cathodic deposition of copper
Applications: functional coatings (metals
Cu
Cu2++2e-
Cu
Cu2++2e-
WE
Cathode
CE
Anode
e-
All features must be electrically connected
Electrodeposit properties controlled by the electrolyte and electrode potential

## Slide 20
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
A Faradaic current converts solvated ions (e- acceptor) into a solid deposit onto an electrode surface (e- donor).
Typically cathodic / reduction:
Rarely anodic / oxidation (e.g., selenium, tellurium, polyaniline, polypyrrole)
Cathodic deposition of Bi2Te3
Applications: functional coatings (metals, alloys, supersaturated solid solutions
2H2O
4H+ + 4e- + O2
Bi2Te3 + 6H2O
2Bi3+ + 3HTeO2+ + 18e- + 9H+
WE
Cathode
CE
Anode
e-
All features must be electrically connected
Electrodeposit properties controlled by the electrolyte and electrode potential

## Slide 21
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
A Faradaic current converts solvated ions (e- acceptor) into a solid deposit onto an electrode surface (e- donor).
Typically cathodic / reduction:
Rarely anodic / oxidation (e.g., selenium, tellurium, polyaniline, polypyrrole)
Electropolymerization
Applications: functional coatings (metals, alloys, supersaturated solid solutions, polymers)
H2
2e- + 2H+
CE
Cathode
WE
Anode
e-
NH3
n
+ 2nH+ + 2ne-
NH
n
Conductive polymers:
polyaniline, polypyrrole, polyfuran
 Protective coatings, supercaps …
All features must be electrically connected
Electrodeposit properties controlled by the electrolyte and electrode potential

## Slide 22
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
A Faradaic current converts solvated ions (e- acceptor) into a solid deposit onto an electrode surface (e- donor).
Typically cathodic / reduction:
Rarely anodic / oxidation (e.g., selenium, tellurium, polyaniline, polypyrrole)
Electroforming
Applications: functional coatings (metals, alloys, supersaturated solid solutions, ceramics, polymers), surface texturing, 3D parts, microcomponents, nanostructures
All features must be electrically connected
Electrodeposit properties controlled by the electrolyte and electrode potential
Electrodeposition is conformal

## Slide 23
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Deposition is mediated by redox reactions between a reductant (e- donnor) and an oxidant (e- acceptor).
No external polarization needed, no counter electrode needed
Redox reaction
Applications: metallization of insulating parts, conformal coatings on complex geometries
Driving force

## Slide 24
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Deposition is mediated by redox reactions between a reductant (e- donnor) and an oxidant (e- acceptor).
No external polarization needed, no counter electrode needed
Autocatalytic plating
Red and Ox are both solvated species
Applications: metallization of insulating parts, conformal coatings on complex geometries, modification of surface chemistry, nanocomposites
Phosphorous is codeposited (amorphous)
Possible to incorporate particles (hardness, friction)
 Used for hard amagnetic coatings

## Slide 25
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Deposition is mediated by redox reactions between a reductant (e- donnor) and an oxidant (e- acceptor).
No external polarization needed, no counter electrode needed
Galvanic displacement
The reducting agent is the solid substrate
Applications: metallization of insulating parts, conformal coatings on complex geometries, nanocomposites, corrosion and tarnishing protection, core-shell structures
The most noble metal displaces the less noble metal
Self-limiting process
 Modification of the surface chemistry, core-shell structures

## Slide 26
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Deposition is mediated by redox reactions between a reductant (e- donnor) and an oxidant (e- acceptor).
No external polarization needed, no counter electrode needed
Rate of electroless plating
Autocatalytic vs galvanic displacement
Applications: metallization of insulating parts, conformal coatings on complex geometries, nanocomposites, corrosion and tarnishing protection, core-shell structures
Autocatalytic plating:
The growth rate depends on the bath chemistry
Galvanic displacement:
The growth rate depends on the surface chemistry

## Slide 27
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Electrochemical reactions induce local changes of chemical conditions leading to the precipitation of solvated species.
A local increase of ionic strength leads to metal oxide/hydroxide precipitates.
Typically the pH but also the oxidation state or coordination
Three ways of precipitating FexOy
Applications: electroplating of oxides, catalysis
Hematite photoelectrocatalyst decorated nanostructures for solar water splitting

## Slide 28
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Electrochemical reactions induce local changes of chemical conditions leading to the precipitation of solvated species.
A local increase of ionic strength leads to metal oxide/hydroxide precipitates.
Typically the pH but also the oxidation state or coordination
Precipitation of ZnO nanorods
Applications: electroplating of oxides, catalysis, functional coatings (photonics, hydrophobicity,

## Slide 29
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Electrochemical reactions induce local changes of chemical conditions leading to the precipitation of solvated species.
A local increase of ionic strength leads to metal oxide/hydroxide precipitates.
Typically the pH but also the oxidation state or coordination
Precipitation of TiO2 nanolayers
Applications: electroplating of oxides, catalysis, functional coatings (photonics, hydrophobicity, dichroic, biocompatibility…)
Interference colors

## Slide 30
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Forced migration and desolvation of charged particles (colloids) in an electric field.
Charged particles dispersed in an electrolyte (low ionic conductivity)
Any material that can develop a surface charge (zeta-potential)
Charged particles and colloids: the DLVO theory
Applications: dielectric coatings
Interaction energy
Van der Waals attraction
Electrostatic repulsion
Secondary minimum
Reversible aggregation
Energy barrier
EPD potential
Primary minimum
Irreversible aggregation
Particle distance
Too stable > no primary minimum
Unstable dispersion

## Slide 31
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Forced migration and desolvation of charged particles (colloïds) in an electric field.
Charged particles dispersed in an electrolyte (low ionic conductivity)
Any material that can develop a surface charge (zeta-potential)
Electrophoretic deposition: cathodic or anodic
Applications: dielectric coatings, paints, nanocomposite materials,
separation of colloids (by size or chemical nature)
Particles with ζ < 0 mV migrate towards the anode
Anodic EPD
Particles with ζ > 0 mV migrate towards the cathode
Cathodic EPD

## Slide 32
Additive processes
Electrolytic deposition
Electroless deposition
EC-induced precipitation
Electrophoretic deposition
Forced migration and desolvation of charged particles (colloïds) in an electric field.
Charged particles dispersed in an electrolyte (low ionic conductivity)
Any material that can develop a surface charge (zeta-potential)
Electrophoretic vs electrolytic deposition
Property | Electroplating | Electrophoretic deposition
Moving species | Ions | Solid particles
Deposition mechanism | Charge transfer Electrocrystallization | Solvation sphere displacement Particle aggregation
Electrolyte conductivity | High | Low
Preferred solvent | Water | Organic solvents
Voltage | Few hundreds mV | Several tens V
Growth rate | < 50 µm/h | Hundreds of µm/h possible
Deposited materials | Only conductive materials | Any colloidal solid
Deposit morphology | Compact | Powder / need binding
Applications: dielectric coatings, paints, nanocomposite materials,
separation of colloids (by size or chemical nature)

## Slide 33
Applications of electrodeposition (electroplating)
Advantages:
Versatility, ambient and near-ambient conditions
Relatively cheap and simple
Electrodeposits are conformal: possible to electroplate or electroform 3D parts
Electrodeposition only occurs on conductive surfaces: masking process/localized ECD
Possible to electrodeposit alloys and solid solution in a single step
Possible to electroplate complex materials (multilayers, nanocomposites…)
Easy to scale-up
Functional coatings, bulk materials, microcomponents, nanostructures, nanocomposites, and metamaterials

## Slide 34
Applications of electrodeposition (electroplating)
Drawbacks:
Limited to conductive substrates
Sometime complex to get the desired coating properties
  Electrolyte formulation
  Physical parameters optimization
Chemical wastes might be hazardous
Medium growth rate (rarely more than several µm/h)
Functional coatings, bulk materials, microcomponents, nanostructures, nanocomposites, and metamaterials

## Slide 35
Applications of electrodeposition (electroplating)
Materials selection:
Mechanical and tribological properties (e.g., hardness, wear resistance, friction)
Corrosion protection
Optical properties (reflectivity, colors (intrinsic, structural), metamaterials)
Electrical properties (semiconductors, electronic boards, MEMS)
Magnetic properties (diamagnetic, paramagnetic (…) gigantic magnetoresistance,)
(Photo-)(electro-)catalysts
Thermoelectric materials
Functional coatings, bulk materials, microcomponents, nanostructures, nanocomposites, and metamaterials
Select the material for your application
 can it be electrodeposited?

## Slide 36
In aqueous electrolytes, one can refer to Pourbaix diagrams:
Thermodynamically stable phases = f(E, pH)
What materials can be electrodeposited?
Applications of electrodeposition (electroplating)
pH < 8.8 or pH > 10.2
Example of Lead

## Slide 37
What materials can be electrodeposited?
ECD but with H2 evolution
Corrosion
Electrodeposition
pH < 8.8 or pH > 10.2
Example of Lead
Applications of electrodeposition (electroplating)
In aqueous electrolytes, one can refer to Pourbaix diagrams:
Thermodynamically stable phases = f(E, pH)

## Slide 38
What materials can be electrodeposited?
ECD but with H2 evolution
Binary diagram – case of Bi2Te3
Corrosion
Electrodeposition
pH < 8.8 or pH > 10.2
Example of Lead
Applications of electrodeposition (electroplating)
In aqueous electrolytes, one can refer to Pourbaix diagrams:
Thermodynamically stable phases = f(E, pH)

## Slide 39
ECD but with H2 evolution
What materials can be electrodeposited?
Binary diagram – case of Bi2Te3
Corrosion
Electrodeposition
pH < 8.8 or pH > 10.2
Example of Lead
The more the elements the more the complexity
 ECD window narrows
Applications of electrodeposition (electroplating)
In aqueous electrolytes, one can refer to Pourbaix diagrams:
Thermodynamically stable phases = f(E, pH)

## Slide 40
What materials can be electrodeposited?
Applications of electrodeposition (electroplating)

## Slide 41
What materials can be electrodeposited?
Transition metals, metals, semi-metals and metalloids
Applications of electrodeposition (electroplating)
Electrodeposited from aqueous electrolytes

## Slide 42
What materials can be electrodeposited?
Molten salts, organic solvents, ionic liquids
Applications of electrodeposition (electroplating)

## Slide 43
Organisation of the lecture
Chapter 1: Atomistic and kinetic aspects of electrodeposition
Chapter 2: Nucleation and growth mechanisms, effect of ECD parameters
Chapter 3: Electrodeposition of alloys and solid solutions
Chapter 4: Template-assisted electrodeposition: from 3D parts to nanostructures