## Slide 1
7 - Kinetics and atomistic aspects of electrodeposition

## Slide 2
Metal Cation
Mz+ +
Electrons
Deposited Metal
ze-
M0
From an ionic solution (electrolyte)
Aqueous
Organic
Molten salts
From an electronic conductor (electrode)
Metals
Semiconductors
Electrodeposit
I) Electrodeposition process: an overview
Reduction of metal ions from a solution

## Slide 3
Metal Cation
Mz+ +
Electrons
Deposited Metal
ze-
M0
From an ionic solution (electrolyte)
Aqueous
Organic
Molten salts
From an electronic conductor (electrode)
Metals
Semiconductors
Electrodeposit
I) Electrodeposition process: an overview
Reduction of metal ions from a solution
Metal
e-
Mz+

## Slide 4: I) Electrodeposition process: an overview
Typical 3-electrodes setup
Measure the substrate potential with a reference electrode
The current passes between the working electrode (cathode) and the counter electrode (anode)

## Slide 5: I) Electrodeposition process: an overview
Typical 3-electrodes setup
Measure the substrate potential with a reference electrode
The current passes between the working electrode (cathode) and the counter electrode (anode)
Electrode-electrolyte interface (double layer)
Charge transfer and mass transfer
Atomistic aspects of electrocrystallization
Nucleation and growth
Structure and properties of deposits

## Slide 6: II) Metals and metallic surfaces
Metal M: definition
A lattice of cations Mz+ in a cloud of free electrons
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Only valence electrons contribute to the electronic cloud
Valence electrons are free of movements
Metal bonds: interaction of all valence electrons with all cations

## Slide 7: II) Metals and metallic surfaces
Metal M: Defects
A lattice of cations Mz+ in a cloud of free electrons
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
About 1022 atoms in 1 cm3 of metal  large number  unavoidable defects
Point defects (0D): vacancy defects, interstitial defects
Line and planar defects: dislocations, grain and twin boundaries, stacking faults

## Slide 8: II) Metals and metallic surfaces
Sommerfeld: quantum description of the free electron
(1919)
The metal is considered as quantum electron gas / ion interactions neglected
The electron is described by a wave function
Schrödinger equation:
Kronig-Penney: Ion lattice only considered as a periodic potential
electron behaves as a free electron but me becomes m* (effective mass)
The wave function becomes with u(x) the crystal periodic function
At the crystal boundaries hence the probability density
There is an excess of positive charges at the external atomic layers
Electronic charge imbalance typically extends over 2-4 monoatomic layers

## Slide 9: III) Metal-electrolyte interface
Surface charge development
When immersed in an electrolyte, ions and dipoles will reorganize at the interface
2) Reorientation of dipoles and redistribution of ions:
 formation of an electrochemical double layer
+
If Mz+ leaving the lattice > Mz+ bonding to the lattice
Metal develops an excess of negative charges
+
+
+
+
+
+
1) There can be spontaneous exchanges of Mz+ between the electrode and the electrolyte
-
-
-
-

## Slide 10
Negative
metal
Positive electrolyte
+
++
+
+
-
-
-
-
-
d
Helmholtz double layer capacity
ФM
ФE
ΔФ
Dielectric constant ε
Solvated ions
Positive charges are attracted
Negative charges are repulsed
Problem: measured Cdl is not necessarily constant when ε and d are constant
III) Metal-electrolyte interface
Helmholtz model (1879)

## Slide 11: III) Metal-electrolyte interface
Gouy-Chapman model (1910-1913):
Excess charges are redistributed in the solution: diffuse layer
- Boltzman statistics and potential dependency
Ф
with
Diffuse layer thickness: dd = K-1 (for water: 0.3 nm and 3 nm for 1 M and 10-2 M Na+Cl-)
Diffuse layer capacitance:
Problem: works only for diluted solutions and low potentials

## Slide 12: III) Metal-electrolyte interface
Stern model (1924):
Combinaison of Helmoltz and Gouy-Chapman models
Ф
H and GC capacitance in series:
Low concentrations:
High concentrations:

## Slide 13: III) Metal-electrolyte interface
Grahame model (1947):
Some ions can lose their solvation sphere and specifically interact with the electrode surface: existence of immobile inner and outer Helmholtz planes
Ф
ФOHP
ФIHP
Zeta-potential:
Determining factor for colloids
and electrophoresis

## Slide 14: IV) Electrode potential
Electrode, solution, and cell potential
Metal M
Solution
Ф
ФM
ФSol
Direct measurements of ФM and ФS are not possible

## Slide 15: IV) Electrode potential
Electrode, solution, and cell potential
Metal M1
Solution
Ф
ФM
ФSol
Need an additionnal electrode
Metal M2
ФM’
V
is the difference of Nernst potentials

## Slide 16: IV) Electrode potential
Electrode, solution, and cell potential
Metal M1
Solution
Ф
ФM
ФSol
Need an additionnal electrode
Metal M2
ФM’
V
)

## Slide 17: V) Electrodeposition mechanism and kinetics
Overview
Let us use an electrolyte that contains solvated cations
And let us apply a >
Overpotential:
Metal M1
Solution
Ф
ФM
ФSol
Need an additionnal electrode
Metal M2
ФM’
V
Electrodeposition at the cathode:

## Slide 18: V) Electrodeposition mechanism and kinetics
Overview
Electrodeposition is governed by 5 fundamental processes
Mass transfer from the bulk solution to the interphase t
Chemical reactions in the electrode region
Adsorption and diffusion of adions
Charge transfer
Crystallisation
Current independent
Tafel law

## Slide 19: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
where F is the Faraday constant
and are kinetic constants that satisfy the Arrhenius law
1st order kinetics

## Slide 20: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
where F is the Faraday constant
and are kinetic constants that satisfy the Arrhenius law
1st order kinetics
Chemical
Potential independent
Electrochemical
Potential dependent

## Slide 21: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
where F is the Faraday constant
and are kinetic constants that satisfy the Arrhenius law
1st order kinetics

## Slide 22: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
At equilibrium:
= i0
-iOx
iRed

## Slide 23: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
At equilibrium:
= i0
=
where F is the Faraday constant
1st order kinetics

## Slide 24: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
At equilibrium:
= i0
=
Exchange current
where F is the Faraday constant
and are kinetic constants that satisfy the Arrhenius law
1st order kinetics

## Slide 25: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
Out of equilibrium:
-iOx
iRed

## Slide 26: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
where F is the Faraday constant
and are kinetic constants that satisfy the Arrhenius law
1st order kinetics
Out of equilibrium:

## Slide 27: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
where F is the Faraday constant
and are kinetic constants that satisfy the Arrhenius law
1st order kinetics
Butler-Volmer equation
Out of equilibrium:

## Slide 28: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
Effect of the exchange current i0
Effect of the transfer coefficient α
Butler-Volmer equation

## Slide 29: V) Electrodeposition mechanism and kinetics
1) Charge transfer: current-voltage relation
Out of equilibrium:
Butler-Volmer equation
High overpotential approximation: (cathodic)
Tafel equation:
Low overpotential approximation:
 and 
Linear approximation:

## Slide 30: V) Electrodeposition mechanism and kinetics
2) Mass transfer limitation
The current density jc is related to the molar flow:
Cations are transfered to the electrode by convection, migration, and diffusion

## Slide 31: V) Electrodeposition mechanism and kinetics
2) Mass transfer limitation
The current density jc is related to the molar flow:
Cations are transfered to the electrode by migration, diffusion, and convection
Migration: All ions j will contribute to the ionic conductivity:
where is the ion mobility
Migration current of cation c: for large

## Slide 32: V) Electrodeposition mechanism and kinetics
2) Mass transfer limitation
The current density jc is related to the molar flow:
Cations are transfered to the electrode by migration, diffusion, and convection
Migration: All ions j will contribute to the ionic conductivity:
where is the ion mobility
Migration current of cation c: for large
Diffusion: Fick’s laws for molar flows: and
For linear diffusion:

## Slide 33: V) Electrodeposition mechanism and kinetics
2) Mass transfer limitation
The current density jc is related to the molar flow:
Cations are transfered to the electrode by migration, diffusion, and convection
Migration: All ions j will contribute to the ionic conductivity:
where is the ion mobility
Migration current of cation c: for large
Diffusion: Fick’s laws for molar flows: and
For linear diffusion:
Convection: Forced agitation of the electrolyte

## Slide 34: V) Electrodeposition mechanism and kinetics
Nernst diffusion layer for a planar electrode
2) Mass transfer limitation

## Slide 35: V) Electrodeposition mechanism and kinetics
Nernst diffusion layer for a planar electrode
t increases
High overpotentials 
Solution to Fick’s second law:
Cottrell law:
2) Mass transfer limitation

## Slide 36: V) Electrodeposition mechanism and kinetics
3) Chemical-electrochemical reactions
Example: reduction of a metalorganic complex [MLx]z+
1) [MLx]n+ → Mz+ + xLm- complexation constant independent of potential
2) Mz+ + ze- → M0 the slower process defines the reaction kinetics
Can you express the new Nernst potential Eeq(MLn+/M0, Lm-) as a function of:
E0(Mz+/M0) the standard potential for the metal M
pKd = -log Kd the complex dissociation constant
and the concentrations and

## Slide 37: V) Electrodeposition mechanism and kinetics
3) Chemical-electrochemical reactions
Example: reduction of a metalorganic complex [MLx]z+
1) [MLx]n+ → Mz+ + xLm- complexation constant independent of potential
2) Mz+ + ze- → M0 the slower process defines the reaction kinetics

Eeq(MLn+/M0, Lm-) < Eeq(Mz+/M0)

## Slide 38: V) Electrodeposition mechanism and kinetics
4) Adion diffusion and electrocrystallisation
Real surfaces are not ideal surfaces
Density of metal surface atoms 1015 cm-2
Density of dislocations 104 – 108 cm-2
Perfect flat surface,terrace Emerging screw dislocation Vacancy in a terrace Adatom in a terrace
A ledge: (mono)atomic step
Vacancy in the ledge
Kink: a ledge in the ledge
Simple defects

## Slide 39: V) Electrodeposition mechanism and kinetics
4) Adion diffusion and crystallisation
Bockris (1958):
The activation energy depends on surface site
Perfect flat face,terrace Emerging screw dislocation Vacancy in the terrace Adatom in the terrace
A ledge: monoatomic step
Vacancy in the ledge
Kink: a ledge in the ledge
Simple defects

## Slide 40: V) Electrodeposition mechanism and kinetics
4) Adion diffusion and crystallisation

## Slide 41: V) Electrodeposition mechanism and kinetics
4) Adion diffusion and crystallisation
Direct transfer to the kink
Indirect transfer to the step- edge site other than a kink, the transfered metal ion diffuses along the step edge until it finds a kink

## Slide 42: V) Electrodeposition mechanism and kinetics
4) Adion diffusion and crystallisation
Metal ion transferred from solution to the flat face of terrace region
From this position, diffuses on the surface, seeking a position of lower energy
Final position is a kink site

## Slide 43: V) Electrodeposition mechanism and kinetics
5) Nucleation and growth
Nucleation sites = defects on the electrode surface
Two nucleation regimes: progressive or instantaneous
Two growth modes: 2D or 3D
Layer by layer growth (2D)
3D growth of nuclei

## Slide 44: V) Electrodeposition mechanism and kinetics
5) Nucleation and growth
Competition between nucleation and growth processes is strongly influenced by the electrodeposition kinetics
44
Nucleation and growth modes and the effect of electrodeposition parameters will be described in the next chapter.