## Slide 1
Electrochemistry for Materials Technology
8 - Nucleation and Growth
Effect of electroplating parameters

## Slide 2: I) Solvation of ions
1) Dissolution of a metal salt in polar solvents
Solvent dipoles screen the electrical charge of the ions
Electrical neutrality of the electrolyte is preserved:
with q the charge and the number density

## Slide 3: I) Solvation of ions
2) Ion solvation
3 types of interactions:
Ion-ion:
Ion-dipole:
Dipole-dipole:
with g(r) the radial distribution function
A hard solvation sphere is formed
Metal cations are hydrated
Hydration number depends on the Pauling’s ionic radius

## Slide 4: II) Cation-surface interaction
1) Adsorption on a planar surface
A negative potential is imposed to the substrate
Interactions cathode (-) — cations (+)
Displacement of the hydration shell and transfer of the cation to the surface
Symmetrical transfer: only the outer solvation shell is displaced
Need to disrupt the inner shell to transfer the cation to the surface
Cation transfer
Symmetrical transfer

## Slide 5: II) Cation-surface interaction
3) Real surfaces
Real surfaces are not ideal surfaces
Density of metal surface atoms 1015 cm-2
Density of dislocations 104 – 108 cm-2
Perfect flat face,terrace Emerging screw dislocation Vacancy in the terrace Atom on the terrace
A ledge: monoatomic step
Vacancy in the ledge
Kink: a ledge in the ledge
Simple defects

## Slide 6: II) Cation-surface interaction
4) Different adsorption sites
Let us consider the initial state [M (H2O)6] z+ an octahedral metal hydrate
Ledge
Ledge kink
Ledge vacancy
Plane vacancy
Plane
— 5H2O
— 4H2O
— 3H2O
— 2H2O
— H2O
[M (H2O)] z+
[M (H2O)2] z+
[M (H2O)3] z+
[M (H2O)4] z+
[M (H2O)5] z+

## Slide 7: II) Cation-surface interaction
5) Coordination number = neighbouring metal atoms
Adion at a surface vacancy: C.N. = 9
Adion at a plane surface site: C.N.= 3
Adion at a monoatomic ledge site: C.N. = 5
Adion at a polyatomic ledge site: C.N. = 6
Adion at kink sites: C.N. = 5 or 6
Adion at edge vacancy sites: C.N. = 7 or 8

## Slide 8: II) Cation-surface interaction
6) Consequence on the electrical activation energy
The electrical activation energy depends on surface site
Perfect flat face,terrace Emerging screw dislocation Vacancy in the terrace Adatom in the terrace
A ledge: monoatomic step
Vacancy in the ledge
Kink: a ledge in the ledge
Simple defects

## Slide 9: II) Cation-surface interaction
7) Potential energy considerations
Energy barrier lowest for adsorption on planar surface
Final state most stable at a ledge
Adsorption Energy barriers
Adion diffusion barrier
Bockris et al.

## Slide 10: II) Cation-surface interaction
8) Most probable pathway
1
2
3
4
5
Dashed line = Free energy profile

## Slide 11: III) Nucleation and growth process
1) Homogeneous nucleation: spherical nucleus
Formation of a monoatomic cluster cα followed by the progressive addition of N atoms to the cluster:
Free energy variation during nuclei formation is a function of the number of atoms:

## Slide 12: III) Nucleation and growth process
1) Homogeneous nucleation: spherical nucleus
Formation of a monoatomic cluster cα followed by the progressive addition of N atoms to the cluster:
Free energy variation during nuclei formation is a function of the number of atoms:
the surface energy, S the surface, the chemical potential, V and Vm the volume and molar volume
)
)

## Slide 13: III) Nucleation and growth process
1) Homogeneous nucleation: spherical nucleus
Formation of a monoatomic cluster cα followed by the progressive addition of N atoms to the cluster:
Free energy variation during nuclei formation is a function of the number of atoms:
the surface energy, S the surface, the chemical potential, V and Vm the volume and molar volume
For a spherical nucleus
)
)

## Slide 14: III) Nucleation and growth process
1) Homogeneous nucleation: spherical nucleus
Formation of a monoatomic cluster cα followed by the progressive addition of N atoms to the cluster:
Free energy variation during nuclei formation is a function of the number of atoms:
the surface energy, S the surface, the chemical potential, V and Vm the volume and molar volume
For a spherical nucleus
Critical nucleus size RC and VC: is maximum, =0
Differenciation:
)
)
Free energy variation vs nucleus radius
Unstable  Stable
Nucleation  Growth

## Slide 15: III) Nucleation and growth process
1) Homogeneous nucleation: spherical nucleus
Formation of a monoatomic cluster cα followed by the progressive addition of N atoms to the cluster:
Free energy variation during nuclei formation is a function of the number of atoms:
the surface energy, S the surface, the chemical potential, V and Vm the volume and molar volume
For a spherical nucleus
Critical nucleus size RC and VC: is maximum, =0
)
)
Free energy variation vs nucleus radius
Unstable  Stable
Nucleation  Growth

## Slide 16: III) Nucleation and growth process
1) Homogeneous nucleation: spherical nucleus
Formation of a monoatomic cluster cα followed by the progressive addition of N atoms to the cluster:
Free energy variation during nuclei formation is a function of the number of atoms:
the surface energy, S the surface, the chemical potential, V and Vm the volume and molar volume
For a spherical nucleus
Critical nucleus size RC and VC: is maximum, =0
hence and
)
)
Free energy variation vs nucleus radius
Unstable  Stable
Nucleation  Growth

## Slide 17: III) Nucleation and growth process
2) Homogeneous nucleation: real nuclei
Cylindrical
Hemispherical
Conical
Facetted
Expression of the critical volume still holds:
with the shape factor ()
Anisotropy of the crystal properties
Growth on high surface energy crystal plane is favored

## Slide 18: III) Nucleation and growth process
2) Homogeneous nucleation: real nuclei
More convenient to determine the critical number of atoms nC than RC
Cylindrical
Hemispherical
Conical
Facetted
Expression of the critical volume still holds:
with the shape factor ()
Let us consider the volume occupied by an atom
and

## Slide 19: III) Nucleation and growth process
2) Homogeneous nucleation: real nuclei
More convenient to determine the critical number of atoms nC than RC
Cylindrical
Hemispherical
Conical
Facetted
Expression of the critical volume still holds:
with the shape factor ()
Let us consider the volume occupied by an atom
is related to the overpotential:
and

## Slide 20: III) Nucleation and growth process
2) Homogeneous nucleation: real nuclei
More convenient to determine the critical number of atoms nC than RC
Let us consider the volume occupied by an atom
is related to the overpotential:
and
Increasing the overpotential decreases the critical size of nuclei !!!
Cylindrical
Hemispherical
Conical
Facetted
Expression of the critical volume still holds:
with the shape factor ()

## Slide 21: III) Nucleation and growth process
3) Heterogeneous 3D nucleation:
Nucleation occurs on a foreign substrate:

## Slide 22: III) Nucleation and growth process
3) Heterogeneous 3D nucleation:
and
Nucleation occurs on a foreign substrate:
The contact angle is related to the surface energies via the Young equation:
Surface
Adhesion
Stronger adhesion decreases the critical size of nuclei !!!

## Slide 23: III) Nucleation and growth process
4) Heterogeneous 2D nucleation:
Nucleation occurs on a foreign substrate (only a few atoms thick):
r
a

## Slide 24: III) Nucleation and growth process
4) Heterogeneous 2D nucleation:
Nucleation occurs on a foreign substrate (only a few atoms thick):
and
r
a
The critical size of nuclei decreases for higher overpotential and stronger adhesion !!!

## Slide 25: III) Nucleation and growth process
5) Nucleation mechanism:
Weak adhesion:

## Slide 26: III) Nucleation and growth process
5) Nucleation mechanism:
Weak adhesion:
3D nucleation process
2D nucleation process

## Slide 27: III) Nucleation and growth process
5) Nucleation mechanism:
Weak adhesion:
3D nucleation process
2D nucleation process
Strong adhesion:
2D nucleation can occur above Eeq
Limited to 1 or 2 monolayers
Enables electrochemical atomic layer epitaxy (ECALE)
Underpotential Deposition (UPD)

## Slide 28: III) Nucleation and growth process
6) Nucleation kinetics
Nucleation law:
There exists a uniform probably that a surface site is converted into a nucleus
A surface has only a limited number of available nucleation sites N0
The number of sites N(t) occupied at time t follows a linear kinetics:
where kn is the nucleation constant

## Slide 29: III) Nucleation and growth process
6) Nucleation kinetics
Nucleation law:
There exist a uniform probably that a surface site is converted into a nucleus
A surface has only a limited number of available nucleation sites N0
The number of sites N(t) occupied at time t follows a linear kinetics:
where the nucleation constant kn strongly depends on i/η
Instantaneous nucleation: all sites are occupied in a short induction time τ
Progressive nucleation: site occupation is linear with time

## Slide 30: III) Nucleation and growth process
6) Growth of single nucleus
The growth rate normal to a surface
Hemispherical 3D cluster
with the hemisphere radius:
thus
Cylindrical 2D cluster
with the cylinder radius:
thus

## Slide 31: III) Nucleation and growth process
6) Nucleation models
t < tmax: no mass transfer limitation, no overlapping

## Slide 32: III) Nucleation and growth process
6) Nucleation models

## Slide 33: III) Nucleation and growth process
6) Nucleation models
Accounting for overlapping: Bewick, Scharifker and Hills (1962, 1983)

## Slide 34: III) Nucleation and growth process
6) Nucleation models
DL charge

## Slide 35: III) Nucleation and growth process
6) Nucleation models
Accounting for overlapping: Bewick, Scharifker and Hills (1962, 1983)

## Slide 36: III) Nucleation and growth process
6) Nucleation models
Accounting for overlapping: Bewick, Scharifker and Hills (1962, 1983)

## Slide 37: III) Nucleation and growth process
6) Nucleation models

## Slide 38: III) Nucleation and growth process
6) Nucleation models
Successive nucleation and overlapping of 2D layers
Polylayers growth

## Slide 39: IV) Electrodeposit characteristics
Microstructure and morphology
Microstucture:
Atoms are arranged in 3 dimensions with a certain periodicity degree
Monocrystalline: periodicity extends on the whole solid
Polycrystalline: periodicity is interrupted at grain boundaries
Nanocrystalline: periodicity extends over a few nanometers
Amorphous: periodicity breaks at short distance (lattice parameter)
Ductility ↗
Hardness ↗ Brightness ↗ Brittleness ↗
Resistivity ↗

## Slide 40: IV) Electrodeposit characteristics
Microstructure and morphology
Low overpotentials
High overpotentials
Morphology:

## Slide 41: IV) Electrodeposit characteristics
Dendritic growth:
Related to crystal
symmetry and mass
transfer limitation
Microstructure and morphology

## Slide 42: V) Effect of electroplating parameters
Final morphology and microstructure is determined by:
Nucleation rate and mechanism
Growth rate and growth orientation
Effect of the overpotential
Fast growth rate: Nanocrystals: fast nucleation
        Dendrites: slow nucleation (depletion)
Overpotential increases
ic = imt
ic ilim
ic = ia
No nucleus reaches its critical size: no deposition
Slow growth rate: crystal growth > nucleation rate
Monocrystalline or coarse grain structure
ic = ict
Medium growth rate: crystal growth ≈ nucleation rate
Polycrystalline, equiaxed structure
ic = imix
Fast growth rate, possible side reactions
Powdery deposits

## Slide 43: V) Effect of electroplating parameters
Effect of the overpotential
Final morphology and microstructure is determined by:
Nucleation rate and nucleation mechanism
Growth rate and growth orientation

## Slide 44: V) Effect of electroplating parameters
Effect of the overpotential
|i|
η
η = 0
H+/H2
Cyclic voltammetry of an electrodeposition system
Mz++ze- M0
Mz++S+ze- MS

## Slide 45: V) Effect of electroplating parameters
ic ≈ ia No nucleus reaches its critical size: no deposition
Effect of the overpotential
η
Under Potential Deposition
1-2 atomic layers
ic = ict Slow growth rate:
Crystal growth > nucleation rate
Monocrystalline or coarse grain structure
ic = imix Medium growth rate:
Crystal growth ≈ nucleation rate
Polycrystalline, equiaxed structure
ic = imt Fast growth rate:
Nanocrystals: fast nucleation
Dendrites: slow nucleation (depletion)
η = 0
H+/H2
ic ilim Fast growth rate, possible side reactions
Powdery deposits
|i|

## Slide 46: V) Effect of electroplating parameters
Influencing parameters
Mz+ concentration
Temperature
Polarization
Current density
Agitation
Supporting electrolyte
Additives _ _ _ _ _ _ _ _ _ _ Inhibits or accelerates electrocrystallization
Dopants _ _ _ _ _ _ _ _ _ _ _ Modify the electrodeposit properties
pH _ _ _ _ _ _ _ _ _ _ _ _ _ _ Ion type and solvation, ionic conductivity, surface tension
Substrate _ _ _ _ _ _ _ _ _ _ Induction process, adhesion, epitaxy
Affects electrocrystallization kinetics
Affects j/jlim
Others: sound waves, electromagnetic waves, magnetic field

## Slide 47: V) Effect of electroplating parameters
Influencing parameters
Simultaneous effects of inhibition and current density

## Slide 48: V) Effect of electroplating parameters
Influencing parameters
Simplified diagram

## Slide 49: V) Effect of electroplating parameters
Additives: Brighteners
Brighteners: weak inhibitors  increases micro-throwing power
2-Methylsulfanylethyl sulfite: C3H7O3S2-
Organosulfur molecules
(e.g. thioethers, phenolsulfonic acid)
Adsorb and inhibit low overpotential regions
Micro-leveling: reduces surface roughness
Grain refining: hardness but tensile stress

## Slide 50: V) Effect of electroplating parameters
Additives: Levelers
Levelers: strong inhibitors  increases macro-throwing power
Adsorb on low overpotential regions, the lower the potential the stronger the inhibition
Quaternary amines, amino compounds, macro molecules (e.g. polyvinylpyrrolidone)
Throwing power ↗

## Slide 51: V) Effect of electroplating parameters
Additives: Wetting agents
Wetting agents: decreases the surface tension
Ensure a good wetting of the substrate
Prevent trapping of gas bubbles (e.g., H2 evolving at the cathode)
Reduces the compressive stress in ultra-thin coatings
Typically, anionic and non-ionic surfactants (e.g., SDS, polyethylene glycol)

## Slide 52: V) Effect of electroplating parameters
Additives: Accelerators & Suppressors
Accelerators:
Decreases the electrochemical activation energy via intermediate states
Catalysts
Suppressors:
Increases the electrochemical activation energy by stabilizing cations
Complexing agents (e.g., EDTA, citrates)

## Slide 53: V) Effect of electroplating parameters
Additives: Stress suppressors
Stress suppressors:
Chemisorption and incorporation in the metal lattice — induce compressive stress
Compensate for tensile stress
Typically, saccharine, acetates, salicylates…
But also inorganic additives

## Slide 54: V) Effect of electroplating parameters
Origin of internal stress

## Slide 55: V) Effect of electroplating parameters
Origin of internal stress
Primary contributions to internal stress:
Heterogeneous nucleation – substrate-deposit interactions
Difference of lattice parameters:
Capillary forces:
as > ad
Compressive
as < ad
Tensile
Compressive
Less compressive
Prevailing for ultrathin deposits

## Slide 56: V) Effect of electroplating parameters
Origin of internal stress
Secondary contributions to internal stress:
Growth – internal structure of the deposit
Interstitial incorporation/elimination:
Grain overlapping (tensile) N(t) (Nuclei density)
Thermal expansion/contraction
Other point and plane defects
Prevailing for thick deposits
Incorporation:
Compressive
Elimination:
Tensile

## Slide 57: V) Effect of electroplating parameters
Pulse and reverse pulse plating
Application of a periodic electrical signal between two electrodes
Typically: a succession of rectangular pulses in the millisecond-second ranges
Alternatively: any other type of wave shapes (e.g., square, triangular, sine, steps)
Electric signal
Some important characteristics
Frequency:
Duty cycle:
Average I:
Average η:

## Slide 58: V) Effect of electroplating parameters
Pulse and reverse pulse plating
What happens during a cathodic pulse?
ic
t
icp
i0
ηc
t0
tDL
η0
EDL charging
tDL≈ 1 ms
tno
Nucleation
Induction time
τc
Nuclei overlapping
Charge transfer  mass transfer
tc
Nuclei reached their max size
Celmin and δmax

## Slide 59: V) Effect of electroplating parameters
Pulse and reverse pulse plating
What happens during the off-time?
ic
t
icp
i0
ηc
t0
tdlc
η0
EDL charge
tDL≈ 1 ms
tno
Nucleation
Induction time
Nuclei overlapping
Charge transfer  mass transfer
tc
Nuclei reached their max size
Celmin and δmax
tdld
EDL discharge
Interphase relaxation:
Surface (subcrit. nuclei, adions)
Diffusion layer, Cel ↗
Slowly returns to equilibrium
tmax

## Slide 60: V) Effect of electroplating parameters
Pulse and reverse pulse plating
Effect of pulse parameters
Off-time:
- long: and very slow growth rate
- short: Interphase is only partially relaxed
Cathodic peak current density or overpotential:
- high: instantaneous nucleation: for
short transition between charge, mix, and mass control
- low: progressive nucleation:
deposition is controlled by charge transfer
Cathodic pulse time:
- long: and/or
- short: and/or
- : no critical nuclei is formed  no deposition

## Slide 61: V) Effect of electroplating parameters
Pulse and reverse pulse plating
Two consecutive cathodic pulses:
ic
t
icn
i0
t0
tn
tn+tg
icg
High i/η instantaneous nucleation
Lower i/η
Compact growth

## Slide 62: V) Effect of electroplating parameters
Pulse and reverse pulse plating
Reverse pulse plating:
ic
t
icn
ia
t0
icg
i0
tc
ta
Electrocrystallization
Electrodissolution  overgrowth (edges and apex)
Relaxation

## Slide 63: V) Effect of electroplating parameters
Pulse and reverse pulse plating
Advantages of pulse plating:
More parameters to control the morphology and microstructure
Possible to tune the micro- and macrothrowing powers: leveling without levelers
A way to simultaneously control grain size and internal stress
Drawbacks of pulse plating:
More parameters = more complexity
Slow electrodeposition
Lower efficiencies