## Slide 1
Electrochemistry for Materials Technology
Chapter 3. Electrodeposition of alloys and solid solutions

## Slide 2
Protective & decorative | Corrosion resistant | Magnetic alloys | Heat resistant allloys | Electronic & jewelry | Antifriction
NiZn NiAu NiCd NiSn AuCu AuAg CuSn | ZnCd ZnSn CrNi CrRe | NiCo NiFe CoW CoPt FePt | CrMn CrW CrMo WFe | PdNi AuNi AuCo | PbAg InPb PbCu AgSn
Some examples of electrodeposited alloys

## Slide 3: I) Alloys and solid solutions
SS-type
Bi2-xTe3+x
Phase diagram for metallurgy only useful for predicting the phase-type
Localized electrocrystallization enables single phases with wider composition range
Highly dispersed supersaturated solid solutions can be electroplated
Metastable: decompose upon annealing

## Slide 4: I) Alloys and solid solutions
Intermetallic alloys:
A and B form a new lattice
Bimetallic:
No mixing of A and B
Interstitial solid solution:
Smaller atoms in random interstitial sites
Substitutional solid solution:
B randomly replace A

## Slide 5: I) Alloys and solid solutions
Intrinsic internal stress due to differences of atom radii
Interstitial atom: Bi*  compressive stress
Substitution: Bax  compressive if rB > r tensile if rB < rA

## Slide 6: II) Electrodeposition of several elements
1) Direct deposition process
Both metal cations are reduced in a single step:
Particularity of direct electrodeposition mechanism:
Not possible to deposit only one cation selectively
x and y still depend on the overpotential and the mass transfer of individual species

## Slide 7: II) Electrodeposition of several elements
1) Direct deposition process
Both metal cations are reduced in a single step:
Indications by cyclic voltammetry

## Slide 8: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
i
E

## Slide 9: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
i
E

## Slide 10: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
The deposit composition will depend on partial currents iA(t) and iB(t):
Express the general equation that gives molar ratio !

## Slide 11: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
The deposit composition will depend on partial current iA(t) and iB(t):
and

## Slide 12: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
Co-deposition of A and B is carried out at overpotentials sufficiently high so that only mass transfer controls the kinetics.
What parameters will allow you to tune the composition?
i
E
EECD

## Slide 13: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
The deposit composition will depend on partial current iA(t) and iB(t):
and
Case 1: high overpotentials
Composition can only be tuned via concentrations

## Slide 14: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
Co-deposition of A and B with ηA >> ηB so that:
ECD of A is purely limited by mass transfer
ECD of B is in the linear Butler-Volmer region
Find the equation that predicts the coating composition!
i
E
EECD

## Slide 15: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
The deposit composition will depend on partial current iA(t) and iB(t):
and
Case 3: and
Depends on concentrations, ηB, and time composition gradient

## Slide 16: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
What morphology may you expect?
How could you correct it?
i
E
EECD

## Slide 17: II) Electrodeposition of several elements
3) The use of ligands
Let us consider cations Aa+ and Bb+, both complexed by Ligands Lα-.
Starting from the Nernst equation for each cation, can you find what parameter will affect the difference between their equilibrium potentials?

## Slide 18: II) Electrodeposition of several elements
3) The use of ligands

and
i
E

## Slide 19: II) Electrodeposition of several elements
3) The use of ligands

If both metals form complexes, then only depends on dissociation constants and stoichiometry numbers
A feasible solution may exist only if the less noble metal has higher Kd or Ox state
Often necessary to find a selective complexing agent

## Slide 20: II) Electrodeposition of several elements
3) The use of surface active substances

## Slide 21: II) Electrodeposition of several elements
4) The use of ligands
Variation of the partial current curve of component A upon complex formation
Here only cation Az+ is complexed by ligand. The difference between Eeq(By+/B) and Eeq(ALxn+/A,Lm-) will depend on Kd and [Lm-]

## Slide 22: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
Co-deposition of A and B is carried out at:
- low overpotentials for both cations: linearized Butler-Volmer
- No mass limitation: Cel = C0.
Express the ratio !
i
E
EECD

## Slide 23: II) Electrodeposition of several elements
2) Co-deposition process
Both metal cations are reduced independently:
The deposit composition will depend on partial current iA(t) and iB(t):
and
Case 2: low overpotentials (Butler-Volmer linear approx.)
Composition depends on exchange currents and overpotentials

## Slide 24: II) Electrodeposition of several elements
5) Anomalous co-deposition
The less noble metal becomes the more noble metal
The electrodeposit composition tendency towards overpotential reverts
Observed for numerous Ni intermetallic alloys (NiFe, NiCo…)

## Slide 25: II) Electrodeposition of several elements
6) Consecutive UPD layers
The nucleation of A on substrate S performs with Δσ < 0
Then a monoatomic layer of A on S can be deposited at E > Eeq
The nucleation of B on monolayer A occurs with Δσ < 0
Then a monoatomic layer of A on B can be deposited at E > Eeq
The nucleation of B on monolayer A performs with Δσ < 0
Then a monoatomic layer of B on A can be deposited at E > Eeq
.
.
.
.
Repeat as many time as necessary to reach the desired thickness

## Slide 26: III) Quick ECD optimizations
1) The Hull cell
The composition and growth rate of the electrodeposit may vary with the position xc
The deposit morphology and microstrucure may vary with the position xc
Quick optimization of the current density
Assessment of the macrothrowing power
Difficult to apply ideal agitation: studies normally performed under natural diffusion
Cathode surface area = 66.3 cm2

## Slide 27: III) Quick ECD optimizations
1) The Hull cell
Increasing [Cu2+]
[Ni2+] in different electrolytes

## Slide 28: III) Quick ECD optimizations
2) The rotating cylinder Hull cell

## Slide 29
3) The Haring-Blum cell
III) Quick ECD optimizations
Used to evaluate of the macrothrowing power:
Optimization of levellers!

## Slide 30: II) Electrodeposition of several elements
7) The Hull cell
Cu and Ni are codeposited at pH 9 in a Hull cell with a total current of 1 A
E0(Cu2+/Cu) = 0.16 V vs NHE, [Cu2+] = 0.05 M, jlim = 275 mA.dm-2
E0(Ni2+/Ni) = -0.23 V vs NHE, [Ni2+] = 0.2 M, jlim = 555 mA.dm-2
Can you estimate the composition profile along xc?
Can you predict the current efficiency?
We consider that only HER occurs as a side reaction and that jHER = jtot - jlim,Cu - jlim,Ni
Cathode surface area = 66.3 cm2

## Slide 31: II) Electrodeposition of several elements
7) The Hull cell
Let us define limit conditions:
  1) There exist a value xc above which 5.1 – 5.24 log xc ≤ 0
    xc(1) = 10(5.1/5.24) = 9.403 cm
  2) E0(Cu2+/Cu) >> E0(Ni2+/Ni): if IC ≤ jlim(Cu) then only copper is deposited
  xc(2) = 10((5.1-0.275)/5.24) = 8.333 cm
  3) Eeq(H+/H2) = E0(H+/H2) – 0.059 pH = 0.531 V vs NHE << E0(Ni2+/Ni)
  HER only occurs when IC > jlim(Cu) + jlim(Ni)
  xc(3) = 10((5.1-0.275-0.555)/5.24) = 6.530 cm
xc
10.2 cm
xc(1)
xc(2)
xc(3)
xc
0 cm

## Slide 32: II) Electrodeposition of several elements
7) The Hull cell
xc
10.2 cm
xc(1)
xc(2)
xc(3)
xc
0 cm
xc > xc(1) : no deposition
xc(1) > xc > xc(2): only copper is deposited at the rate
xc(2) > xc > xc(3): copper and nickel are codeposited:
and
xc < xc(3): The deposit composition is constant:
ECD is accompanied by HER:
ECD efficiency =

## Slide 33: II) Electrodeposition of several elements
7) The Hull cell
xc
10.2 cm
xc(1)
xc(2)
xc(3)
xc
0 cm

## Slide 34: II) Electrodeposition of several elements
7) The Hull cell
In reality, the distribution of the current results from three contributions:
1) The primary current: ionic conduction
Ohm’s law of the electric potential through the ionic conductor:
The electrode potentials are constant Va and Vc
The potential distribution in the electrolyte is a solution of Laplace equation
2) The secondary current: reaction kinetics
The overpotential:
Butler-Volmer for charge tranfer limitations:
3) The ternary current: mix kinetics and transport
2) Butler-Volmer for mix control:
3) Cotrell for pure diffusion:
Typically, simulations are performed to determine the exact current distribution