## Slide 1
Exercise4: Nucleation and growth
What are the 4 nucleation and growth models?
What property and parameters determine:
  The nucleation and growth mode?
  The number density of available nucleation sites?
  There exists a special case named « underpotential deposition ». Define it!
The induction time is the formation of critical nuclei and their growth as discrete islands on the substrate.
  3.1. Show that the current that crosses a single hemispherical nucleus and a single cylindrical nucleus varies with t2 and t, respectively.
  3.2. Considering that nucleation follows a linear kinetics model , express the total current as a function of the time for the 4 scenarios. (no overlapping)

## Slide 2
Exercise4: Nucleation and growth
What are the 4 nucleation and growth models?
  3D instantaneous
  3D progressive
  2D instantaneous
  2D progressive

## Slide 3
Exercise4: Nucleation and growth
What are the 4 nucleation and growth models?
  3D instantaneous
  3D progressive
  2D instantaneous
  2D progressive

## Slide 4
Exercise4: Nucleation and growth
What property and parameters determine:
  The nucleation and growth mode?
    The overpotential (controlled)
    The surface energy variation, hence the adhesion energy of the deposit on the substrate (intrinsic)
  The number density of available nucleation sites?
    The number density of surface defects of the substrate (partially controlled)
    The overpotential (controlled) because adion coordination
  There exists a special case named « underpotential deposition ». Define it!
    Strong substrate/deposit affinity 
    Cations are reduced at
    Limited to 1-2 monoatomic layers

## Slide 5
Exercise4: Nucleation and growth
What property and parameters determine:
  The nucleation and growth mode?
    The overpotential (controlled)
    The surface energy variation, hence the adhesion energy of the deposit on the substrate (intrinsic)
  The number density of available nucleation sites?
    The number density of surface defects of the substrate (partially controlled)
    The overpotential (controlled) because adion coordination
  There exists a special case named « underpotential deposition ». Define it!
    Strong substrate/deposit affinity 
    Cations are reduced at
    Limited to 1-2 monoatomic layers

## Slide 6
Exercise4: Nucleation and growth
What property and parameters determine:
  The nucleation and growth mode?
    The overpotential (controlled)
    The surface energy variation, hence the adhesion energy of the deposit on the substrate (intrinsic)
  The number density of available nucleation sites?
    The number density of surface defects of the substrate (partially controlled)
    The overpotential (controlled) because adion coordination
  There exists a special case named « underpotential deposition ». Define it!
    Strong substrate/deposit affinity 
    Cations are reduced at
    Limited to 1-2 monoatomic layers

## Slide 7
Exercise4: Nucleation and growth
What property and parameters determine:
  The nucleation and growth mode?
    The overpotential (controlled)
    The surface energy variation, hence the adhesion energy of the deposit on the substrate (intrinsic)
  The number density of available nucleation sites?
    The number density of surface defects of the substrate (partially controlled)
    The overpotential (controlled) because adion coordination
  There exists a special case named « underpotential deposition ». Define it!
    Strong substrate/deposit affinity 
    Cations are reduced at
    Limited to 1-2 monoatomic layers

## Slide 8
Exercise4: Nucleation and growth
The induction time is the formation of critical nuclei and their growth as discrete islands on the substrate.
  3.1. Show that the current that crosses a single hemispherical nucleus and a single cylindrical nucleus varies with t2 and t, respectively.
Perfect 3D hemisphere
Perfect 2D cylinder (only lateral growth)

## Slide 9
Exercise4: Nucleation and growth
The induction time is the formation of critical nuclei and their growth as discrete islands on the substrate.
  3.1. Show that the current that crosses a single hemispherical nucleus and a single cylindrical nucleus varies with t2 and t, respectively.
The growth rate normal to a surface can be found through the Faraday law:
Perfect 3D hemisphere
Perfect 2D cylinder (only lateral growth)

## Slide 10
Exercise4: Nucleation and growth
The induction time is the formation of critical nuclei and their growth as discrete islands on the substrate.
  3.1. Show that the current that crosses a single hemispherical nucleus and a single cylindrical nucleus varies with t2 and t, respectively.
Perfect 3D hemisphere
Perfect 2D cylinder (only lateral growth)
The growth rate normal to a surface can be found through the Faraday law:
Perfect 3D hemisphere
Perfect 2D cylinder (only lateral growth)

## Slide 11
Exercise4: Nucleation and growth
The induction time is the formation of critical nuclei and their growth as discrete islands on the substrate.
  3.1. Show that the current that crosses a single hemispherical nucleus and a single cylindrical nucleus varies with t2 and t, respectively.
  3.2. Considering that nucleation follows a linear kinetics model , express the total current as a function of the time for the 4 scenarios. (no overlapping)
Perfect 3D hemisphere
Perfect 2D cylinder (only lateral growth)
Progressive nucleation
Intantaneous nucleation

## Slide 12
Exercise4: Nucleation and growth
Copper depositions below -150 mV vs SCE demonstrated 3D instantaneous nucleations. Integrating the quantity of charge at tmax gives:
SEM observations showed that the contact angle was 90°, making perfect hemispherical nuclei.
1) Express the maximum radius of nuclei and their density under the assumption that Nuclei are ideally packed on the surface (compact hexagonal arrangement)
 | Instantaneous | Progressive
3D |  | 
2D |  | 
 | Instantaneous | Progressive
3D |  | 
2D |  | 
Accounting for overlapping, Scharifker and coworkers established the following equations:
2) For a 1 cm2 substrate, you integrated Qmax and found 12.7 mC, 10.5 mC, and 8.3 mC at -150 mV, -175 mV, and -200 mV, respectively. What can you conclude? (z=2 and Vm=7.09 cm3.mol-1)

## Slide 13
Exercise4: Nucleation and growth
Maximum radius of hemispherical nuclei and nuclei density:
4.1. Assumption: Nuclei are ideally packed on the surface (compact hexagonal arrangement)
rmax
Hexagonal cell surface area: hence
Volume of the hemisphere inscribed in the hexagonal cell:

## Slide 14
Exercise4: Nucleation and growth
Maximum radius of hemispherical nuclei and nuclei density:
4.1. Assumption: Nuclei are ideally packed on the surface (compact hexagonal arrangement)
Hexagonal cell surface area: hence
Volume of the hemisphere inscribed in the hexagonal cell:
Qmax is related to the electrodeposit volume by the Faraday law:
replacing N0 and Vmax

## Slide 15
Exercise4: Nucleation and growth
Maximum radius of hemispherical nuclei and nuclei density:
4.1. Assumption: Nuclei are ideally packed on the surface (compact hexagonal arrangement)
Hexagonal cell surface area: hence
Volume of the hemisphere inscribed in the hexagonal cell:
Qmax is related to the electrodeposit volume by the Faraday law:
replacing N0 and Vmax
Hence: and

## Slide 16
Exercise4: Nucleation and growth
Maximum radius of hemispherical nuclei and nuclei density:
4.1. Assumption: Nuclei are ideally packed on the surface (compact hexagonal arrangement)
4.2. For a 1 cm2 substrate, you integrated Qmax and found 12.7 mC, 10.5 mC, and 8.3 mC at -150 mV, -175 mV, and -200 mV, respectively. What can you conclude?
 | -150 mV / -12.7 mC | -175 mV / -10.5 mC | -200 mV / -8.3 mC
Maximum radius rc | 7.72 nm | 6.38 nm | 5.04 nm
Density of nuclei N0 | 4.85E+11 cm-2 | 7.09E+11 cm-2 | 1.13E+12 cm-2
Hexagonal cell surface area: hence
Volume of the hemisphere inscribed in the hexagonal cell:
Qmax is related to the electrodeposit volume by the Faraday law:
replacing N0 and Vmax
Hence: and

## Slide 17
Exercise4: Nucleation and growth
Maximum radius of hemispherical nuclei and nuclei density:
4.1. Assumption: Nuclei are ideally packed on the surface (compact hexagonal arrangement)
4.2. For a 1 cm2 substrate, you integrated Qmax and found 12.7 mC, 10.5 mC, and 8.3 mC at -150 mV, -175 mV, and -200 mV, respectively. What can you conclude?
 | -150 mV / -12.7 mC | -175 mV / -10.5 mC | -200 mV / -8.3 mC
Maximum radius rc | 7.72 nm | 6.38 nm | 5.04 nm
Density of nuclei N0 | 4.85E+11 cm-2 | 7.09E+11 cm-2 | 1.13E+12 cm-2
Hexagonal cell surface area: hence
Volume of the hemisphere inscribed in the hexagonal cell:
Qmax is related to the electrodeposit volume by the Faraday law:
replacing N0 and Vmax
Hence: and