## Slide 1
Exercise1: Pourbaix diagram
What represent the vertical, horizontal, and diagonal lines. Why are their duplicated lines?
What are the diagonal dashed lines? Write the reactions? Name the space defined between them.
Write the reactions that occur at the transitions 1, 2, 3, 4, 5, and 6
Determine their slope.
From the Pourbaix diagram, propose boundary conditions on E, pH and [Bi3+] for the electrodeposition of Bi0
You want to electrodeposit bismuth from an aqueous electrolyte and you want to choose the ideal pH.
You decide to refer to the E-pH thermodynamic equilibriums found in Pourbaix diagram.
You find the Pourbaix diagram for Bi3+ in pure water at ambient conditions:
1
2
3
4
6
5

## Slide 2
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C,

## Slide 3
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Electrochemical window of water
Acidity constants
At 25 °C,

## Slide 4
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C,
Acid-base equilibria
Redox

## Slide 5
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
Acid-base equilibria
Redox Cu+I/Cu0
At 25 °C, [Cu]=10-6 mol/L
(S)

## Slide 6
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
Acid-base equilibria
Redox Cu+II/Cu+I
At 25 °C, [Cu]=10-6 mol/L
(S)

## Slide 7
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
Acid-base equilibria
Redox Cu+II/Cu0
<
𝐷𝑖𝑠𝑝𝑟𝑜𝑝𝑜𝑟𝑡𝑖𝑜𝑛𝑎𝑡𝑖𝑜𝑛
At 25 °C, [Cu]=10-6 mol/L
(S)

## Slide 8
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
Acid-base equilibria
Redox Cu+II/Cu0
At 25 °C, [Cu]=10-6 mol/L
(S)

## Slide 9
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
Acid-base equilibria
(S)
At 25 °C, [Cu]=10-6 mol/L
Passivation
Immunity
Corrosion
Corrosion

## Slide 10
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
>
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
Redox

## Slide 11
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
>
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
Redox

## Slide 12
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
>
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
Redox

## Slide 13
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
>
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
Redox

## Slide 14
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
(S)
Redox

## Slide 15
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
(S)
Redox

## Slide 16
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
(S)
Redox

## Slide 17
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
(S)
Redox

## Slide 18
How to build a Pourbaix diagram (E-pH)
Nernst Potentials
Acidity constants
At 25 °C, [Cu]=10-6 mol/L
Acid-base equilibria
Passivation
Immunity
Redox
Corrosion
Corrosion
(S)

## Slide 19
Exercise1: Pourbaix diagram
What represent the vertical, horizontal, and diagonal lines. Why are their duplicated lines?
Vertical: acid-base reactions which do not depend on the potential without electron transfer
Horizontal: redox reaction which do involve neither H+ nor OH-
Diagonal: redox reactions in which hydroxide or hydrogen are involved
Line duplicates show the effect of Bi3+ concentration
You want to electrodeposit bismuth from an aqueous electrolyte and you want to choose the ideal pH.
You decide to refer to the E-pH thermodynamic equilibriums found in Pourbaix diagram.
You find the Pourbaix diagram for Bi3+ in pure water at ambient conditions:
1
2
3
4
6
5

## Slide 20
Exercise1: Pourbaix diagram
2) What are the diagonal dashed lines? Write the reactions? Name the space defined between them.
You want to electrodeposit bismuth from an aqueous electrolyte and you want to choose the ideal pH.
You decide to refer to the E-pH thermodynamic equilibriums found in Pourbaix diagram.
You find the Pourbaix diagram for Bi3+ in pure water at ambient conditions:
1
2
3
4
6
5
The bottom diagonal dashed line represents the equilibrium potential for H2 evolution
The top diagonal dashed line represents the equilibrium potential for O2 evolution
The space between is the electrochemical window of water where it is neither reduced nor oxidized

## Slide 21
Exercise1: Pourbaix diagram
3) Write the reactions that occur at the transitions 1, 2, 3, 4, 5, and 6
You want to electrodeposit bismuth from an aqueous electrolyte and you want to choose the ideal pH.
You decide to refer to the E-pH thermodynamic equilibriums found in Pourbaix diagram.
You find the Pourbaix diagram for Bi3+ in pure water at ambient conditions:
1
2
3
4
6
5

## Slide 22
Exercise1: Pourbaix diagram
4) Determine their slope.
You want to electrodeposit bismuth from an aqueous electrolyte and you want to choose the ideal pH.
You decide to refer to the E-pH thermodynamic equilibriums found in Pourbaix diagram.
You find the Pourbaix diagram for Bi3+ in pure water at ambient conditions:
1
2
3
4
6
5
 horizontal line

no electron exchanged:  vertical line



Apply the Nernst equation !!!
The activity of solvents, solids, and gases are taken as 1

## Slide 23
Exercise1: Pourbaix diagram
5) From the Pourbaix diagram, propose boundary conditions on E, pH and [Bi3+] for the electrodeposition of Bi0
1
2
3
4
6
5
The direct reduction of Bi3+ is prefered  no local pH change

## Slide 24
Exercise1: Pourbaix diagram
5) From the Pourbaix diagram, propose boundary conditions on E, pH and [Bi3+] for the electrodeposition of Bi0
1
2
3
4
6
5
The direct reduction of Bi3+ is preferred
no local pH change during ECD
pH < 2
Bi3+ concentration should be high
Increase by
Increase deposition rate
Limited by the salt solubity
Applied potential above
To avoid evolution
(bubble formation, ECD efficiency, local pH increase)

## Slide 25
Bismuth is electrodeposited from a degased aqueous electrolyte ([Bi3+] = 10-2 mol.L-1, [HNO3] = 1 M) on an 1 cm2 working electrode at a sufficiently large overpotential
Exercise2: electrodeposition rate and current efficiency
Argon
The quantity of reduced cations is linked to the quantity of coulombs by the
Faraday law: Quantity of charge (coulomb) quantity of matter
Faraday constant
Propose a protocole to measure the diffusion coefficient of Bi3+.
Knowing that 10-5 cm2.s-1, express the deposition rate of bismuth in mol.s-1 as a function of time under purely mass limiting regime and in the absence of convection.
Calculate the thickness of the deposit obtained after 1000 s of electroplating (MBi = 208.98 g.mol-1 and = 9.79 g.cm-3).
After an electrodeposition of 1000 s, a total of 0.4 C was integrated from the chronoamperometry data. Calculate the electrodeposition efficiency.
What could have happened to the other electrons? How could you improve the efficiency?
What parameters could allow you to tune the growth rate? What could be the trade-offs?

## Slide 26
Exercise2: electrodeposition rate and current efficiency
Propose a protocole to measure the diffusion coefficient of Bi3+.
Cottrell law:
The Cottrell law can be used to measure the diffusion coefficient of Bi3+
Let us apply a sufficiently large cathodic overpotential to the cathode so that the reaction is only limited by mass transfer.
Now, let’s plot the recorded current versus t-1/2
i
t-1/2
We should obtain a straight line crossing the origin of the plot.
can be calculated from its slope s:

## Slide 27
Exercise2: electrodeposition rate and current efficiency
Propose a protocole to measure the diffusion coefficient of Bi3+.
In electrochemical deposition, no steady state is reached !!!
A better protocole is the Sand-Bard method that corrects surface modifications
Current impulses > |ilim|
Potential
time
Surface effects (EDL, contaminants…)
τ
At the transition time τ, the flow of Bi3+ becomes insufficient to sustain the current
The potential jumps to the next reduction potential
Sand equation:
Bard surface correction

## Slide 28
Exercise2: electrodeposition rate and current efficiency
Propose a protocole to measure the diffusion coefficient of Bi3+.
In electrochemical deposition, no steady state is reached !!!
A better protocole is the Sand-Bard method that corrects surface modifications
Potential
time
Surface effects (EDL, contaminants…)
τ1
τ2
τ3
τ4
At the transition time τ, the flow of Bi3+ becomes insufficient to sustain the current
The potential jumps to the next reduction potential
Sand equation:
Bard surface correction

## Slide 29
[Bi3+] = Csol = 10-2 mol.L-1 = 10-5 mol.cm-3, A = 1 cm2, and 10-5 cm2.s-1
Cottrell law:
Faraday law:

Exercise2: electrodeposition rate and current efficiency
2) Knowing that 10-5 cm2.s-1, express the deposition rate of bismuth in mol.s-1 as a function of time under purely mass limiting regime and in the absence of convection.

## Slide 30
[Bi3+] = Csol = 10-2 mol.L-1 = 10-5 mol.cm-3, A = 1 cm2, and 10-5 cm2.s-1
Cottrell law:
Faraday law:


Exercise2: electrodeposition rate and current efficiency
2) Knowing that 10-5 cm2.s-1, express the deposition rate of bismuth in mol.s-1 as a function of time under purely mass limiting regime and in the absence of convection.

## Slide 31
[Bi3+] = Csol = 10-5 mol.cm-3, A = 1 cm2, 10-5 cm2.s-1, MBi = 208.98 g.mol-1, and = 9.79 g.cm-3
Cottrell law:
Faraday law:
Let us integrate:
mol

Exercise2: electrodeposition rate and current efficiency
3) Calculate the thickness of the deposit obtained after 1000 s of electroplating (MBi = 208.98 g.mol-1 and = 9.79 g.cm-3).

## Slide 32
[Bi3+] = Csol = 10-2 M, A = 1 cm2, 10-5 cm2.s-1, MBi = 208.98 g.mol-1, and = 9.79 g.cm-3
Cottrell law:
Faraday law:
mol
Only 81.65 % of the electrons participated to the ECD of bismuth.
Exercise2: electrodeposition rate and current efficiency
4) After an electrodeposition of 1000 s, a total of 0.4 C was integrated from the chronoamperometry data. Calculate the electrodeposition efficiency.

## Slide 33
Capacitive current (double layer charging) but negligible for long DC electroplating
Uncontrolled side reactions:
 Reduction of dissolved oxygen
 Hydrogen evolution
 Co-deposition of other metals
 Partial reduction of metal ions
 Reduction of surface oxides
 Partial redissolution or detachment of the deposit (corrosion)
Solutions: Argon degassing, optimize the bath formulation (pH, precursors, concentrations), optimize electroplating conditions (electrode potential, temperature, convection), optimize the surface state of the substrate
Exercise2: electrodeposition rate and current efficiency
5) What could have happened to the other electrons? How could you improve the efficiency?