Exercise 2.1 (Extinction coefficients of semiconductors)

Semiconductors are used in optoelectronic devices due to their advantageous optical properties. In the figures below the optical constants n and k are given as a function of wavelength.

- For each example below, calculate the necessary film thickness to absorb 90% of the incident radiation intensity at 700 nm (reflectance and interference can be neglected).

- Calculate the reflective loss of incident radiation due to reflection using :

R=nrel-12+krel2(nrel+1)2+krel2

- Discuss the optical constants of the different materials, with a view to their use in photovoltaics.

Exercise 2.2 (total reflection, penetration depth)

In a Fourier Transform Infrared Spectrometer in ATR mode, IR light is coupled into a diamond window. At the diamond/air interface, total reflection occurs. If a fine powder is pressed onto the diamond window, the infrared spectrum of the powder can be measured.

- Explain the working principle of this method. How can the sensitivity be increased?

- Determine the minimum angle θIto be used, assuming a diamond/air interface.

- Calculate the penetration depth of the evanescent wave induced by total reflection for a typical IR wavenumber (1500 cm-1) and a typical incidence angle of 45°.

- This method can also be used for liquids. How does the penetration depth depend on the refractive index of the liquid? Use a typical incidence angle of 45°.