## Slide 1
Quantum transport in Mesoscopic systems
(PHYS-462)
Laboratory of Quantum Physics: Topology and Correlations

## Slide 2: Outlines
Introduction to moiré superlattices
Electronic structures
Fractal energy spectrum under magnetic field
Twisted bilayer graphene

## Slide 3: Outlines
Introduction to moiré superlattices
Electronic structures
Fractal energy spectrum under magnetic field

## Slide 4: Family of Atomic Layers
Graphene hexagonal BN
TMDs
Phosphorene

## Slide 5: van der Waals Superlattice
A. K. Geim and I. V. Grigorieva, Nature 499, 419 (2013)
graphene
hBN MoS2 WSe2
Fluorographene
layer by layer stacking of 2-D lattices
→ extra periodicity along in-plane direction !!

## Slide 6: Moiré Pattern
Interference of periodic patterns
lattice period
difference in lattice period difference in lattice orientation
moiré interference in macroscopic world

## Slide 7: Moiré Superlattice: Graphene/hBN
a0 = 0.246 nm
Graphene
a0 = 0.250 nm
hexagonal BN
a0
LM =
(1+ ε )
ε 2 + 2 (1+ ε )(1− cosθ )
(ε: lattice mismatch,
θ : lattice misorientation)
LM
Related theory:
Kindermann et al, PRB 86, 115415 (2012).
Wallbank et al, PRB 87, 245408 (2013).
Jung et al, arXiv:1312.7723 (2013).
Moon and Koshino, PRB 90, 155406 (2014).

## Slide 8: Moiré Superlattice: Twisted Bilayer Graphene
a0 = 0.246 nm
Graphene
Related theory:
J. M. B. Lopes dos Santos et al., PRL 99, 256802 (2007).
S. Shallcross et al., PRL 101, 056803 (2008).
G. Trambly de Laissardière et al., Nano Lett. 10, 804 (2010).
E. J. Mele, PRB 81, 161405(R) (2010).
E. S. Morell et al., PRB 82, 121407(R) (2010).
Moon and Koshino, PRB 85, 195458 (2012).
Moon and Koshino, PRB 87, 205404 (2013).
Moon, Koshino, and Son, PRB 90, 155427 (2014).
M
a
L =
1
2 (1− cosθ )
0 (θ: lattice misorientation)
LM

## Slide 9: Lattice Period (Twisted Bilayer Graphene)
conventional materials: a0 ~ 0.1-1 nm
moiré superlattices: LM ~ 1-100 nm (*)
* tunable with interlayer registry
rotation angle (°)
moiré lattice constant (nm)
STM images (twisted bilayer graphene) from
J. Hass et al., PRL 100, 125504 (2008), G. Li et al., Nature Phys. 6, 109 (2010),
A. Luican et al., PRL 106, 126802 (2011), W. Yan et al., PRL 109, 126801 (2012),
I. Brihuega et al., PRL 109, 196802 (2012)

## Slide 10: Outlines
Introduction to moiré superlattices
Electronic structures
Fractal energy spectrum under magnetic field

## Slide 11: Regularly-stacked Bilayer Graphene
energy
AA-stack graphene
E =
linear (massless)
momentum dispersion
energy
AB-stack graphene
parabolic (massive)
momentum dispersion
( : interlayer coupling)
E =
Purpose:
role of interlayer interaction in moiré superlattice

## Slide 12: Effective Model
δ=0
δ
δ
Local structure
≈ non-rotated bilayer with shift δ
Interlayer coupling in moiré bilayer: U (δ (r ))
Moon and Koshino, Phys. Rev. B 87, 205404 (2013), Phys. Rev. B 90, 155406 (2014),
Moon, Koshino, and Son, Phys. Rev. B 90, 155427 (2014).
Moiré structures (incommensurate) ≈
Continuous patchwork of commensurate structures

## Slide 13: Brillouin Zone and Band Structure: Graphene
K’
K
K
K
K’
K’
Brillouin zone
Dirac cone

## Slide 14: Band Structures

## Slide 15: Lowest (Degenerate) Conduction Bands
K
(1)
K(2)
K
r(1)
Kr(2)
+1
w=0
+1
-1
w=0
-1
80
60
40
20
0 meV
from monolayer K
from monolayer K′
arxiv:1605.05475

## Slide 16: Band Structures: Twisted Bilayer Graphene
Moon and Koshino, Phys. Rev. B 85, 195458 (2012), Phys. Rev. B 87, 205404 (2013).
L
Fermi velocity
See also: J. M. B. Lopes dos Santos, N. M. R. Peres, and A. H. Castro Neto, PRL 99, 256802 (2007), S. Shallcross,
S. Sharma, and O. A. Pankratov, PRL 101, 056803 (2008), G. Trambly de Laissardière, D. Mayou, and L. Magaud, Nano Lett. 10, 804 (2010), E. J. Mele, PRB 81, 161405(R) (2010), E. Suárez Morell et al., PRB 82, 121407 (2010).

## Slide 17: Outlines
Introduction to moiré superlattices
Electronic structures
Fractal energy spectrum under magnetic field

## Slide 18: Moiré Superlattice in Magnetic field
How the spectrum looks like?
E (meV)
E (meV)
B
B (tesla)
hybridized by U(δ(r))
B (tesla)

## Slide 19: How Nature
Electron energy
f e
Electron energy
al e
Zeitschrift für Physik
Electron in Periodic Lattice
allowed energies
e-
orbidden nergies
“energy bands” (finite widths)
Felix Bloch
52, 555 (1929)
Zeitschrift für Physik
Electron in Magnetic Field
lowed
e- nergies
“energy levels” (discrete)
Lev Landau
64, 629 (1930)*
...(*age 22)
harmonizes the two?

## Slide 20: Electron in a Periodic Potential AND a Magnetic Field
D.
Ph
P. G. Harper,
Proc. Phys. Soc. A68, 879 (1955)
E. Brown,
Phys. Rev. 133, A1038 (1963)
Zak,
J.
P
D
P
Magnetic flux
Energy
hys. Rev. 134, A1602 (1963)
M. Ya. Azbel,
J. Exptl. Theoret. Phys. 46, 929 (1964)
. Langbein,
hys. Rev. 180, 633 (1968)
R. Hofstadter,
ys. Rev. B 14, 2239 (1976)

## Slide 21: Hofstadter Butterfly
Energy (in unit of band width)
Φ magnetic flux
Φ0 magnetic flux quantum
B magnetic field
D. R. Hofstadter,
Phys. Rev. B 14, 2239 (1976)
1
0
Φ ⎛ = BA ⎞
Φ ⎜
h / e ⎟
0 ⎝ ⎠
e-

## Slide 22: Fractal (Self-Similar) Energy Spectrum
1
2
2 3 4 5
3 4 5 6
1
0
1 1 1 1
6 5 4 3
−10
−8
−4
−6
−2
0
2
4
6
8
10
6 5 4 3
2924 19 14
2
9
3 4 5 6
13 17 2125
1
4
−1.5
1
5
−1.0
−0.5
0
0.5
1
1.5
5
24
29 24 19 14
139115 91 67
9
43
13
62
17 21 25
81 100119
4
19
−0.15
−0.1
−0.05
0
0.05
0.1
0.15
24
115
139115 91 67
666551 436 321
43
206
62 81 100 119
297 388 479 570
19
91
−0.015
−0.01
−0.005
0.005
0.01
0.015
0.02
0
−0.02
1st generation 2nd generation
4th generation
3rd generation

## Slide 23: Condition to Observe Hofstadter Butterfly
B (T)
lB (nm)
1
10
⁞
10,000
25.7
8.11
⁞
0.257
lB = / (eB)
magnetic length
L (~ 0.1 nm)
unit cell size
The two scale are quite different !!

## Slide 24: Φ = BA ∝ O (1) Φ0 h / e
2,800 T, puls
d, blowing off the lab (bunker)
esy of Dr. Chuck Mielke (LANL)
45 T, continuous, NHMFL, USA
730 T, pulsed, destructive (but not destroying the lab),
ISSP, Japan
e ,
VNIIEF, Russia
image court
Hofstadter Butterfly by High Magnetic Field
2,800 T
B ~ O(104 T) for usual crystalline solids [L ~ O(0.1 nm)]
1
spectrum obtained by blowing off the facility
Φ / Φ 0 (∝ B )
Energy (in unit of band width)
0
~80,000 T

## Slide 25: Hofstadter Butterfly by Large Lattice
Φ = BA ∝ O (1)
Φ0 h / e
B0 (Tesla)
feasible magnetic field
Unit cell length (nm)
ordinary crystalline lattice

## Slide 26: Hofstadter Butterfly by Large Lattice
d,
.
Φ / Φ0 ≥ 1 R. Bistritzer and A. H. MacDonal (strong field regime) Phys. Rev. B 84, 035440 (2011).
Φ / Φ0 ≥ 0 Moon and Koshino,
(entire regime) Phys. Rev. B 85, 195458 (2012)
Hofstadter butterfly at moderate B !
Moiré S
superlattice stacking of
uperlattice
by incoherent atomic lattices
θ = 0°
θ = 4°
θ = 8°

## Slide 27: Bilayer graphene / hBN
C. R. Dean, L. Wang, P. Maher, C. Forsythe,
F. Ghahari, Y. Gao, J. Katoch, M. Ishigami,
P. Moon, M. Koshino, T. Taniguchi, K. Watanabe,
K. L. Shepard, J. Hone, and P. Kim,
Nature 497, 598 (2013).
Monolayer graphene / hBN
B. Hunt, J. D. Sanchez-Yamagishi, A. F. Young,
M. Yankowitz, B. J. LeRoy, K. Watanabe,
T. Taniguchi, P. Moon, M. Koshino,
P. Jarillo-Herrero, and R. C. Ashoori, Science 340, 1427 (2013).
( : theory)

## Slide 28: Quantum Hall Effect in Twisted Bilayer Graphene
Y. Kim, P. Herlinger, P. Moon, M. Koshino, T. Taniguchi, K. Watanabe, J. Smet, arXiv:1605.05475 (2016)